Keratin Based Material For Perspective Bio-Application

Doctoral dissertation in Chemical Engineering by:

Hossein Rajabinejad

in the partial fulfillment of Erasmus Mundus Joint Doctorate programme:

Susainable  Management and Design for Textile

Jointly Organized by:

Gheorghe Asachi Technical University of Iasi, Romania

Politecnico di Torino, Italy

Soochow University, China

Supervisors:

Prof. Claudio Tonin - Prof. Stelian-Sergiu Maier- Prof. Yan Chen

(2013-2017)

Acknowledgments

This work presented in the thesis was carried out at the Gheorghe Asachi Technical University of Iași, Romania, Politecnico di Torino, Italy and Soochow university China under Erasmus  Mundus Joint Doctorate Programme, Sustainable Management and Design for Textiles (SMDTex). All universities are gratefully acknowledged for their generous support in preparation and completion of the thesis, without which it might never have been done.

My sincere thanks go to my supervisors Professor  Stelian-Sergiu Maier, Claudio Tonin for their support, advice and trust, wihout which this thesis would never have been completed. I wish you to thank Professor Carmen Loghin, Professor Giorgio Rovero, Professor Yan Chen and Professor Ada Ferri for all tremendous support and efforts in conncetiong resarch work carried out in Romania, Italy, and China. I wish you to thank  Dr. Ingrid-Ioana Bucişcanu, Dr. Marina Zoccola, Dr. Alessia Patrucco for for all invaluable suggestions and efforts and accordingly guiding in furthur rsearch process and papers prepration. My thanks goes to Dr. Rosalinda Caringella, Alessio Montarsolo for supporting research actitveits.

I want to thank my SMDTex colleages especially Dr. Vijay Kumar for all valuale suggestion and fruitful discusions. I am thankful to several other colleagues in all universities and institutes where I stayed during PhD, for their great support throughout this journey.

A special thanks to my family. Words cannot express how grateful I am to my Mother, my sister Tahereh, my brother Mohammad and my Brother-in-law Prof. Nabi and nephew and niece. Last, but by no means the least, in memory of my father, who he has been always presented.

# Abstract

Keratin has natural characteristic for applying in biomaterial field as a biocompatible matrix like tissue regeneration, proliferation, and cell adhesion or drug career in the shape of microcapsules or microsphere. Because of the amino acid inherent structure, keratin extraction needs to be well designed to meet the particular requirement for applying in desired applications such as integrate with different molecules, drug releases, wound healing or biocompatible film. Keratinous sources such as wool, feathers are valuable by-products that abundantly present in nature. Although wool has valuable material in especially in textile industry, massive amount of low-grade wool cannot be utilized in textile and inevitably end up as a waste stream. Because of  high cystine content of keratin, solubilization and extraction of keratin is a problematic process compared with other natural polymers such as collagen and chitosan.  Using keratin in different level especially in large-scale requires understanding final properties of keratin which is strongly depends on producing procedure.. The interest towards drug career and microcapsules based on non-toxic, biodegradable and biocompatible polymers, such as proteins, is increasing considerably.

In this work, keratin from wool fibers was extracted with oxidation, reduction, sulfitolysis, and superheated water hydrolysis methods. The effect of each method on obtained keratin properties are discussed and particularly reported how each extracted keratin influenced by the extraction process. In particular, all different samples of extracted keratin were characterized by molecular weight determination, FT-IR and NIR spectroscopy, amino acid analysis, and thermal behavior and the archived data were compared with reporting of previous studies with the emphasis of advantage and limitation of each extraction method.

In the other part of the study, special attention are given to produce microcapsule and film from keratin-based material in line with biomaterial application. Microcapsules were prepared using water-soluble keratin, known as keratoses, with the aim of encapsulating hydrophilic molecules. The obtained keratin via oxidizing extraction of pristine wool, were utilized as shell part of the microcapsules which produced by sonication method. Production of the microcapsules was carried out by a sonication method.

The microencapsulation and dye encapsulation yields were obtained by UV-spectroscopy. In addition, morphological structure of microcapsules was studied by light microscopy, SEM, and AFM and thermal properties of microcapsules were investigated by DSC.

The molecular weights of proteins analyzed with gel-electrophoresis indicates the extracted keratoses has suitable molecular weight range for bio-application, and also the results confirmed that the hydrophilic dye (Telon Blue) was introduced inside the keratoses shells. The final microcapsules diameter ranged from 0.5 to 4 µm.

One part of the experimental work is dedicated to producing keratin blend film with polyvinyl alcohol (PVA). PVA has been chosen because of its biocompatible and biodegradable properties which make this polymer as a promising candidate in the bio-field area. Blend of Polyvinyl alcohol (PVA) and keratoses were prepared with the aim of producing bio-compatible material proper for film and fiber structure mainly to improve the mechanical properties of obtained keratoses. Aqueous solution of keratoses and PVA was prepared for solution casting method. Blended films were characterized by, SEM, FT-IR spectroscopy and Differential scanning colorimetry and tensile properties.

The work highlights various reported about keratin nature and characteristic which can be significant data in promoting and/or implementing keratin in different biomaterial fields.

Table of content

1 Introduction	1

1.1 What is Keratin?	1

1.2 Wool keratin	2

1.3 Overview of chemistry and structure	7

1.4 Solubilization pathways and methods	10

1.5 Novel approaches to keratin solubilization	14

1.6 Enzyme-aided hydrolysis	16

1.7 Biomaterial application	19

1.8 Microcapsule and film	27

1.9 The Goals	30

2 Purification and Extraction of keratin	31

2.1 The purpose of the present chapter	31

2.2 Preliminary discussion on extraction pathways	31

2.2.1	Oxidative methods	32

2.2.2	Reductive methods	34

2.2.3	Sulfitolysis methods	39

2.2.4	Chemical-free hydrolysis	40

2.3 Materials and methods	42

2.4 Extraction pathways	42

2.4.1	Oxidative extraction	42

2.4.2	Reductive extraction	43

2.4.3	Sulfitolysis extraction	43

2.4.4	Superheated water hydrolysis	43

2.5 Characterization	44

2.5.1	Extraction yield	44

2.5.2	Molecular weights determination:	44

2.5.3	Amino acids analysis:	45

2.5.4	Fourier Transform Infrared Analysis (FT-IR):	45

2.5.5	Near Infrared (NIR) analysis:	45

2.5.6	Differential Scanning Calorimetry (DSC):	45

2.5.7	Thermogravimetric analysis (TGA):	46

2.6 Results and discussion	47

2.6.1	Extraction yield	47

2.6.2	Molecular weight (SDS-Page)	48

2.6.3	Amino acid Analysis	50

2.6.4	FT-IR Spectroscopy	62

2.6.5	NIR Spectroscopy	64

2.6.6	Thermal behavior	66

2.7 Conclusions	69

3 Film and microcapsule	71

3.1 The aim of this part	71

3.2 Preliminary discussion	71

3.3 Materials and methods for producing microcapsules	75

3.3.1	Keratoses oxidizing extractions	75

3.3.2	Preparation of microcapsules	76

3.3.3	Measurement and characterization methods	76

3.4 Result and discussion	78

3.5 Materials and methods for producing blend film	84

3.5.1	Preparation of PVA/KOx blend films	84

3.6 Blend film characterization	85

3.6.1	Morphological structure	85

3.6.2	Thermal analysis	89

3.6.3	FTIR analysis	90

3.6.4	Mechanical properties	93

3.7 Conclusion	97

4 Conclusions	99

Reference	101

List of Figures

Figure ‎1-1-Wool fiber morphological structure	5

Figure ‎1-2-Keratin biopolymer  exploitation by wool solubilization: methods and applications	6

Figure ‎1-3-Two-phase model for keratin fiber	8

Figure ‎1-4 Schematic diagram of keratin solubilization pathways	12

Figure ‎2-1-Dependence of keratin macromolecule charge on pH, and affinity for charged species	32

Figure ‎2-2-Gel-electrophoresis pattern of the samples	49

Figure ‎2-3-Schematics of disulfide bond scission in alkaline oxidative medium	54

Figure ‎2-4 Fourier transform infrared spectra	63

Figure ‎2-5-Near infrared spectra	65

Figure ‎2-6-Second derivative near infrared spectra	66

Figure ‎2-7-Differential scanning calorimetry curves	67

Figure ‎2-8-Thermogravimetric analysis of extracted keratins.	68

Figure ‎3-1– Transmitted Light Microscope images of keratoses	79

Figure ‎3-2- SEM images of keratoses microcapsules	81

Figure ‎3-3- AFM images of microcapsules	81

Figure ‎3-4- Calibration Curve Telon Blue	82

Figure ‎3-5-Calibration Curve of Keratoses	83

Figure ‎3-6-DSC thermograms of keratoses and keratoses microcapsules	84

Figure ‎3-7-Visual appearance of PVA/KOx films.	86

Figure ‎3-8-SEM pictures of PVA/KOx films	88

Figure ‎3-9-DSC curves of blend films with different ratios PVA/KOx.	90

Figure ‎3-10-FTIR spectra of blended films of PVA/KOx with different ratios.	92

Figure ‎3-11- The stress-strain properties of different KOX/PVA blend films	95

List of Tables

Table ‎1-1-Feasible solubilization methods and biomedical applications of wool solubilization products	24

Table ‎2-1 Extraction yield of different extracted samples	47

Table ‎2-2-Amino acid analysis:  keratoses, kerateine, sulfo-kerateine and hydrolysed keratin compared to amino acid analysis of original wool.	52

Table ‎3-1- Thickness of blended films	89

Table ‎3-2-Tensile strength, elongation at break and modulus of PVA/KOx blend films.	96

# Chapter 1

# Introduction

## What is Keratin?

Keratins are a group of fibrous proteins produced in some epithelial cells of reptiles, birds, and mammals. These proteins are abundantly present in nature and constitute the major part of mammalian and reptilian nails and horns, claws, mammalian hair and hooves, wool, bird feathers, reptile and fish scales, bird beaks, and the outermost layer of skin in most animals. Over the years, keratin has been extracted from all low-value mentioned sources. [1]

Renewable resources are mainly regarded as sources of biopolymers, which are gaining ground in the world of emerging materials due to their properties: availability, biodegradability, versatility, and similarity to synthetic polymers. Also, one of the sustainable development commandments is a rationalization of material demand, by making use of renewable resources and by waste materials processing or recycling. Amongst animal-derived renewable resources, wool, hair, feather and other keratinous biological materials hold a significant quantitative share, but are regarded as unwanted wastes and are disposed of in landfills, burnt or processed by primitive methods, for low-grade applications. Keratin waste from breeding, butchery or textile industries have been estimated worldwide to be more than 5,000,000 ton/year [2], [3], but due to its intrinsic insolubility and complicated morphological structure it is difficult to be extracted, purified and processed into useful forms. This is why keratins have not been exploited to the same extent as other proteins such as collagen or silk [4], [5].

The investigation of the structure and properties of keratins were very intense in the middle of the 20th century, and many works conducted in that period are considered to be definitive [6], [7]; many basic studies and practical procedures for keratin solubilization were established in the same period, and further studies brought slight modification of the original method [8]. Noticeable interest in the production of materials with valuable applications from keratin solubilizes emerged starting with the 1970’s [9] and was followed by the first report on a solubilized keratin used as biomaterial [10]. Since then, keratinous resources and keratin have been the constant subject of research, within the scope of biopolymers valorization especially from renewable resources.

Lately, the development of biopolymers as green alternatives to synthetic macromolecular compounds put keratinous resources in a new light, and the unique characteristics of keratin made it very attractive to the biopolymer field. Lucrative and efficient processes to solubilize and extract keratins are demanded, with economic and environment benefits. The solubilization products can find a wide range of uses, starting from animal feed and going to advanced materials for biomedical applications.

## Wool keratin

One of the most important sources of keratin is wool from the waste of the textile industries or coarse wool not suitable for spinning. Since the middle of the past century, when the synthetic fibers have begun their rise, wool has lost its importance in the textile sector and became a marginal fiber. High amounts of non-marketed raw wool have turned from an income source into a waste, and are burnt or landfilled as a waste stream. With increasing demand for sustainable resources, wool was reconsidered as an underrated, underused renewable resources, worthy of a better exploitation. Recently, intensive research has been done on wool and its potential non-conventional applications. Innovative solutions for wool waste valorization are reported in the specialty literature, and different kinds of wool-based in bio-field products are patented and marketed. Two main directions to add value to wool waste have been developed: in applications that exploit the natural fiber properties and in applications that use the keratin biopolymer extracted from the fibers.

Wool is a valuable natural fiber and has a long history as raw material for textile purposes. It was amongst the first commodities to be traded internationally and is still essential to the agricultural economies of many countries. Between the 17th and the first half of the 20th centuries, wool textile sector was a leading ranking global industry, but competition from synthetic fibers, combined with consumer preferences shifting in favor of lighter weight and casual products, has negatively impacted the demand for the woolen products. Wool production has also been constrained by its poor environmental performance, related to sheep grazing and fiber industrial processing, which is energy, water and resource intensive, and produces wastewater with high pollution loadings. With respect to these figures, wool is currently perceived as a marginal fiber, reserved mainly for luxury products.

Market reports record only the traded wool, which enters the manufacturing chain and is processed into different consumer products in the textile industry. The statistics do not take in consideration the raw wool that is produced in sheep farms, (i.e. shorn off sheep) but is not on the market, from different reasons: low quality not suitable for textile manufacturing, lack of potential buyers even for high grade wool, lack of wool collecting, washing and trading facilities etc..

The share of wool in total world fiber supply fell, in volume terms, from 9.9% in 1960 to 3.2% in 2000 [11]. In the 2011/2012 season, when wool production fell to reach the lowest in 70 years, the share of the wool fibers on the global market was of 1.3%, while the synthetics share was of 61.4%. In 2013, world wool production lifted by 3% and has been keeping a steady/stationary trend, with about 1.16 million metric tons of clean wool per year.

In the last years, sheep shearing was sometimes only an animal welfare activity with no profit for the farmer, and the shorn wool turned from an income source into a burden.

Apart from the raw wool which does not enter the textile process chain, the wool supply chain produces vast amounts of pre-consumer and post-consumer woolen wastes. Wool waste of different proveniences has become an issue of solid waste management, requiring rational actions.

With little prospect for growth in wool supply for the textile sector, the opportunity lies in benefiting from wool’s advantage as a natural, renewable and biodegradable fiber, by finding unconventional uses and processing ways/technologies to obtain added-value products. These uses exploit either the natural fiber qualities or the keratin biopolymer, which is the main constituent of wool fiber [12].

Washed wool contains dominantly pure protein, and it is formed by a histological structure which is made of three main morphological components, namely the cuticle, the cell membrane complex and the cortex. The cuticle of the wool fiber consists of a thin envelope of flat overlapping ‘cuticle cells’ arranged like roof tiles surrounding the cortex, which is made up of spindle-shape ‘cortical cells’ oriented parallel to the fiber axis. The cell membrane complex, sometimes referred to as intercellular cement, performs the function of cementing cortical and cuticle cells together. In Figure ‎1-1 , a schematic of the morphological wool fiber structure is reported.

Figure ‎1-1-Wool fiber morphological structure [13]

Keratin extracted from wool shows many interesting and peculiar properties, often depending on the extraction method used, that makes keratin an interesting material in many sectors like biomedical, filtering, cosmetic, agricultural, etc. [14]. As a biomaterial, wool keratin is biocompatible, biodegradable and able to support cell attachment and spreading [15]. Indeed wool keratins contain several peptide binding motifs, such as leucine-aspartic acid-valine (LDV) and glutamic acid-aspartic acid- serine (EDS), which support attachment of a wide variety of cell types [16].

These proteins are characterized by a high sulfur amount and by the presence of strong disulfide bonds and higher cysteine content typically from 4 to 28 residues per 100 in keratin when compared with 0 to 2 residues per 100 for other proteins which make them water-insoluble and resistant to different chemical agents.

Figure ‎1-2-Keratin biopolymer exploitation by wool solubilization: methods and applications

The first pathway mainly makes use of low quality raw wool, but can also use pre-consumer and post-consumer wastes. Applications are mainly directed towards technical textiles, for which function is the key factor, and fiber fineness is unimportant. Recovery of keratin proteins by solubilization seems to be the most advanced way of raw wool fibers valorization. The recovered keratin biopolymer is susceptible of further processing into value-added materials and products, with applications mainly in the regenerative medicine and cosmetics. An overview of wool solubilization pathways and main application areas of keratin forms thus obtained is presented in Figure ‎1-2.

There are different viewpoints to classify keratins. They have been classified as “hard keratin” and “soft keratin” according to their physical and chemical properties, particularly to the sulfur amount; type I or acidic keratin and type II or neutral-alkaline keratin on the basis on the predominant amino acids; α-keratin and β-keratin on the basis of their secondary structure. Keratin can also be distinguished according to their biosynthesis and their molecular weight [17]–[19].

## Overview of chemistry and structure

Wool is a natural protein material whose unique properties rely on its chemical composition and morphological characteristics. The histological structure of wool fiber comprises the cuticle, the cortex and the cell–membrane complex. The cuticle is a scaly outer layer, with barrier function against external physical and chemical damage. The cuticle surface is hydrophobic, due to the presence of fatty acids covalently bonded to the protein substrate. As the cortex is hydrophilic, the fiber has a core-shell structure, with a hydrophobic outer surface wrapping a hydrophilic core [20].

Keratins are exclusively intracellular fibril-forming proteins, confined to the epithelial tissues of vertebrates [21]. Even if all epithelial cells are able to biosynthesize keratins in the form of intermediate filaments [22], only specialized tissues produce keratinous morphological structures that can be exploited to extract keratins. In this respect, vertebrate integuments are the main representatives. There are two structural components of the integuments that contain keratins: the epidermis, and the epidermal products (hair, wool, nails, feathers, reptilian scales, etc.). The foremost structural function of keratins consists in generating a supracellular scaffold that connect cells and stabilize morphological structures of epithelial origin. To fulfill such a function, during the phylogenetic evolution, some of the keratin species have acquired particular molecular characteristics, which sketch the physicochemical portrait of keratins, especially of those playing structural roles. For example, feather keratins have a specific structure which includes proteins with a much lower degree if the fibrous organization and lower molecular weight and also an inherently lower cystine content than wool and other hard alpha keratin sources [23].

Figure ‎1-3-Two-phase model for keratin fiber [24]

Commonly, keratins are classified according to five criteria: [17], [19]: (i) the morphological entities of animal body which comprise them (intracytoplasmatic or “soft”, and morphologic or “hard” keratins), (ii) the primacy of biosynthesis (“primary” or normally synthesized in basal keratinocytes, and “secondary” or optionally synthesized), (iii) the predominant amino acids in their composition (“type I” or acidic, and "type II” or neutral-alkaline), (iv) the X-ray pattern (“alpha keratin” which includes α-helix-rich domains, “beta keratin” consisting in β-sheet packed macromolecules, and “gamma keratin” which represents the low molecular weight keratin-associated proteins (KAPs), which hold the keratin intermediate filaments (KIFs) together by embedding them in a protein matrix, and (v) the average molecular weight (MW): “low molecular weight keratins” (LMWK) with a molecular mass less than 40 kDa, “intermediate molecular weight keratins”(IMWK), of 40 to 57 kDa, and “high molecular weight keratins” (HMWK), of more than 57 kDa; the range of the MW values for α-, β- and γ-keratins are 40-68 kDa, 10-22 kDa and 10-18 kDa, respectively.

At the molecular level, there are considerable differences between keratins of different animal species and different intraspecies histologic localization [17]. Folding, supramolecular association and spatial packing of various keratin macromolecules are dictated by the amino acids composition and sequence. As an example, mammalian hair predominantly contains α-keratins, while in avian feathers and reptilian scales β-keratins prevail. Mutual conformational transitions between the α-helix domains and the denser β-sheet form can occur in wool or hair, depending on the mechanical stretching and hydration state of the keratin fiber [25].

Keratins are medium-sized polypeptides having, in average, 400 to 644 amino acids. In terms of colloidal chemistry, they are amphoteric polyelectrolytes with defined values of isoelectric domains (pHi), which depend on the types and numbers of constituent amino acids (acidic, type I: 40-64 kDa, pHi 4.7-6.1; neutral-basic, type II: 52-68 kDa, pHi 5.4-8.4) (Coulombe et al., 2013).

The sequence of amino acids in the α-keratin macromolecule shows a characteristic structural motif: the succession of heptad repeats (seven amino acids constrained to form two consecutive turns in the helix structure) along the polypeptide chain (Fuchs and Hanukoglu, 1983). The first and the fourth amino acid in every heptad have small nonpolar side chains (leucine, isoleucine, methionine, and valine) and are placed on the same face of the helix, creating a continuous hydrophobic lateral stripe, which permits a longitudinal assembling as pairs of helices. The pairs further generate spatial aggregates of increasing complexity, which conclude by forming filamentary assemblies / intermediate filaments, and finally bundles of microscopic diameters and mesoscopic lengths. The unit cell of these aggregates is the “keratin monomer” having the MW ≈ 10 kDa [26]. In the case of β-keratins, a large number of hydrogen bonds are formed, in a regular manner, between the amino and carboxyl groups of peptide bonds on adjacent polypeptide chains, which facilitates a long-range parallel alignment into spatial structures of folded sheets type. By supramolecular assembling, the pleated sheets generate strongly binded, dense, and planar morphological structures of extended dimensions [27].

As compared with other fibrous proteins like collagen and fibroin, the main peculiarity of keratins consists of the high content of disulfide covalent bridges that crosslink adjacent polypeptide chains, and consolidate their supramolecular aggregates. The amount of cysteine is strictly dependent on the bio-morphological function of keratins, and ranges between 16.6-18.0% in human hair, 11.0-13.7 in sheep wool, 10.5 - 15.7 in cattle horn, and about 2.11% in feather keratin (given as grams per 100 grams of dry keratin) (Peplow et al., 2007). Depending on the disulfide bridge distribution, two kinds of keratins can be distinguished: (a) low-sulfur keratins (LSK) located in IFS and correspond to α-keratins and (b) high-sulfur keratins (HSK) identified with KAPs and found in the interfibrillar matrix, together with the high tyrosine containing proteins  [28].

According to the two-phase model proposed for keratin fibers [29], wool or hair are regarded as natural fiber-reinforced composite elastomers in which the interfibrillar matrix made up of KAPs is equivalent to the continuous phase, and the rod-shaped intermediate filaments are analogous to the reinforcement fibers. Recently, a three-phase model has been proposed for describing the behavior of fibrous hard α-keratins, in which the interface, made of non-helical tail domains of keratin, scaffolds the intermediate filaments and controls the thermal properties of the α-helix [30].

Wool has a homogenous macroscopic morphology, while feathers exhibit a complex morphology with structural and reactivity differences between constituent parts. Physical processing of feathers is more difficult because it implies rachis and barb separation, but the pleated β-keratin of feathers is much more prone to chemical or enzymatic attack than the “rope-shaped” wool or hair keratin [27].

## Solubilization pathways and methods

The present part reviews the conditions in which the same reactions determine the solubilization of the keratinous substrate. Due to keratins intrinsic hydrophobicity and presence of multiple interchain disulfide bridges that impart toughness to the keratinized entities and naturally evolved to be robust and resistant to degradation, which make these sources are practically insoluble in water and usual solvents. Chemical, physicochemical and/or microbiological processes must be applied to initialize and perform solubilization. Firstly, in development of keratin material in especially in the advanced application is the isolation of that protein in different forms that can be further manipulated by the desired application.

Keratin can be extracted by: (i) unprotected solubilization, which unsystematically detaches keratins macromolecules or parts of them, by degrading both the backbone peptide bonds and the interchain disulfide bridges, and (ii) protected solubilization, which leaves keratin macromolecules almost intact, by preferential cleavage of the disulfide bridges, and by extensive disruption of the intermolecular hydrogen bonds. Except for severe hydrolysis treatments (when low molecular weight peptides and amino acids are obtained), both ways confront with the difficulty of maintaining the solubilized polypeptides in a colloidal state, as stable aqueous solutions. Freshly solubilized keratins are prone to precipitation because of their hydrophobicity and disulfide bridges tendency to reassemble from the newly resulted sulfhydryl groups. As a consequence, a complex mixture of supramolecular aggregates results, which tend to associate and separate as flocks. In an unprotected way, the isolation and soluble form of keratin can be achieved easily by conventional methods of hydrolysis, using acid, high-temperature water, alkali or enzymatic digestion of the peptide bonds to create a mixture of peptide and amino acids. In this way, none of the secondary or tertiary structure of the core protein has retained, and it considers it as harsh processing that destroys many unique characteristics of the protein. Keratin from greasy waste wool hydrolyzed with superheated water has been used for the preparation of organic fertilizers with a nitrogen release in the soil depending on the hydrolysis temperature and time [31], [32].

An outlook of the keratin solubilization pathways and methods, together with the nature of the mainly involved processes and the resulted keratin forms is given in Figure ‎1-4.

Figure ‎1-4 Schematic diagram of keratin solubilization pathways

The extraction process must produce quasi-native keratin macromolecules, which preserve these attributes to a great extent. The  feasible  chemical methods for the extraction of quasi-native keratins are: reduction with thiols in denaturing media, which results in keratin forms known as “kerateines” [33], [34] sulfitolysis with alkali metal sulfites in denaturing media, which results in keratin forms known as “S-sulfo-kerateines [35], [36] oxidation with peroxy compounds, which results in sulfonated keratins known as “keratoses” [6], [37] The solubilization techniques were set up in the middle of the 20th century, but are still in use with minor improvements. Recently, an environmentally friendly method has been developed , which uses ionic liquids (ILs) as solubilizing agents and results in kerateine-like proteins [38] which can be regenerated into films [39], [40] or nanofibers [41].

Particularly, as abovementioned, keratin can be obtained by different extraction methods. Keratin extraction may take place after cleavage of disulfide bonds, and this can be achieved by various methods such as oxidation, reduction, ionic liquid or sulfitolysis.

By oxidative extraction using peracetic or performic acids, which oxidize cystine to cysteic acid, keratoses are obtained [6]. Keratoses are water-soluble and cannot participate in cross-linking reactions with the reformation of the disulfide bridges. For this reason, these biomaterials can degrade relatively fast in vivo as compared with other extracted keratin, i.e., in the order of days to weeks [42]. Reductive wool extraction with an aqueous mixture of urea and thiols has been proposed by many authors [34], [43]. The reaction mechanism consists of two reactions of nucleophilic displacement and the thiol groups obtained (cysteine residues) are rapidly oxidized by air. Sulfitolysis describes the cleavage of a disulfide by sulfite to give a thiol and a S-sulfonate anion (or Bunte salt). The sulfitolysis of cystine has been extensively studied by Cecil and his coworkers [44]. While using the previous protein extraction methods, the molecular weight of extracted proteins remains unchanged; wool protein hydrolysis leads to the breaking of peptide bonds with the formation of low molecular weight peptides. Wool hydrolysis can be achieved by basic or acidic conditions; complete acidic hydrolysis of wool keratin was used to study the chemical composition of wool fibers [45] while partial hydrolysis under controlled alkaline process conditions, with the aim of tailoring the extent of the peptide length, seem to focus the attention of many researchers [46]. Green processes, solvent-free, have been proposed for the hydrolysis of keratin. These treatments include hydrolysis with superheated water [47], [48] and enzymes [49].  In the case of less demanding applications, such as pharmaco-cosmetic or agricultural, nonspecific partial degradation provided by unprotected solubilization is acceptable.

## Novel approaches to keratin solubilization

One of the most serious shortcomings concerning the chemical-based methods for extracting keratin is that large amounts of toxic, non-recyclable reagents are required, in laborious and time-consuming procedures. This makes the conventional solubilization methods environmentally unacceptable and economically inefficient. Environmentally friendly alternatives have been recently proposed for keratinous resources processing, of which hydrothermal and enzymatic hydrolysis have already been presented.

Lately, solubilization with ionic liquids (ILs) is being regarded as a green processing route for development of novel biopolymer materials from renewable resources. Attempts have been made to use ionic liquid to extract and separate biopolymers from biomass, such as lignin and cellulose from wood [50], collagen from native skin collagen fibers [51], or fibroin from silk [52]. Dissolved biopolymers can be regenerated into biopolymer-based materials (films, membranes, fibers or molded shapes) with common or advanced applications [53].

Successful attempts to dissolve and regenerate keratin from feather and wool in ILs have been lately reported. Imidazolium ILs such as 1-butyl-3-methylimidazolium chloride ([BMIM]Cl), were reported as novel solvents for the dissolution and regeneration of keratin from wool [54] and feathers [55], without the addition of other solvents or reagents. Keratin solubility in ([BMIM]Cl) is higher for feathers, which have a limiting solubility of around 500 mg/g solvent [38], while wool keratin exhibited a maximum solubility of around 200 mg/g solvent [55]. A water-soluble and a water-insoluble fraction result, of which the water-insoluble fraction is of interest.

Ionic liquids have been selected predominately to dissolve cellulose based on their hydrogen bond breaking ability. Mechanism of keratin dissolution using ionic liquids is more complicated and related to the structure and morphology of wool and feather. The dissolution of wool fibers, observed by polarized optical microscopy, showed that the cortex dissolves quickly, with partial destruction of the crystalline α-keratin segments, while the cuticle dissolves after a prolonged time, by an inside-outside mechanism [56]. Preferential dissolution of the cortex is mainly assigned to the destruction of the hydrogen bonds, which are predominant in the α-helical domains of microfibrils [29]. The extended time required to dissolve the cuticle is linked to the high content of disulfide bonds, which are less proned to the IL attack. For feathers, ATR-FTIR spectra indicate extensive cleavage of the –S–S– bridges, and lower but significant splitting of the peptide bonds, which is supported by the SDS-PAGE pattern of the water-soluble protein fraction in which the most intense bands appeared at 10 and 20 kDa, corresponding to keratin monomer and dimer [38]. The increase of solubilization temperature promotes peptide bond hydrolysis, with significant impact on the physicochemical characteristics of the regenerated keratin-based materials [57]. Pretreatment with reductive reagents significantly enhances the solubilization ability of ILs towards feathers [58], [59]. ILs can be conveniently recovered with high distillation yields (>96%) and reused [59], [60], which make this solubilization method attractive from an economical and environmental point of view. The water-and can be regenerated as a biopolymer material that is melt-processable, like classical synthetic thermoplastics, or can be casted from organic solvents [40], [57].

Other organic solvents can also be considered for green solubilization treatments, but further research is required in this respect. Dipolar aprotic solvents, of which dimethyl sulfoxide (DMSO) is the best-known, are extensively used in clinical practice as penetration enhancers for transdermal drugs, due to their ability to interact with keratin in the corneocytes and alter skin permeability. DMSO in high concentrations (> 60%) acts as denaturing agent. It disrupts the keratin filaments of the corneocytes and turns the α-helical conformation to the β-sheet one [61], [62]. It swells hair and promotes disulfide inexchange reactions in hair native keratins [63] and can be used as a folding agent of peptides and protein due to its ability to reform the disulfide bridges by mild oxidation of the thiol group [64]. Moshy (1961) [65] patented a process for obtaining a minimally affected, hydratable keratin protein starting from feathers solubilized in DMSO at temperatures exceeding 100 °C.

## Enzyme-aided hydrolysis

Certain fungi, actynomicetes and bacteria produce extracellular hydrolytic enzymes named keratinases, which stand apart from the conventional proteases due to their specificity towards a variety of insoluble keratin rich substrates, like feather, wool, hair, horns, hooves [66], [67]. Some of these keratinolytic microorganisms are natural constituents of soils, birds plumage, mammal hair etc.. Keratinases attack the highly recalcitrant keratin substrates during the natural biodegradation process; tremendous development of industrial biotechnology has driven the exploitation of this process into controlled systems, to obtain high-quality hydrolysates (with high nutritional value) from keratinous wastes, through cheap, environmentally friendly and mild processes [2].

Based on their keratinolytic abilities, microorganisms can be divided into two types: true keratinolytic, and potentially keratinolytic; only true keratinolytic microorganisms are able to fully solubilize hard keratin structures, so selection of active strains by screening tests of such microorganisms is mandatory for effective and efficient practical applications [68].

For biotechnological purposes, keratinases are extracted from controlled cultures of keratinolytic microorganisms, having keratin-rich substrates as nutrient source [69], [70]. The molecular weight of keratinases is mostly within the 30-50 kDa range [71], [72] so their access to the peptide bond is possible only after the loosening of the keratin microfibril packed structure, by cleavage of the disulfide bonds.

The mechanism of keratinolysis implies cleavage of both disulfide and amide bonds and differs from bacterial to fungal attack.

Kunert (1989) [73] found that fungal keratinolysis of wool proceeds through a two-step biochemical mechanism. Firstly, the cystine bridges are cleaved in a similar manner to chemical sulfitolysis by sulfite excreted into the medium. After keratin loosening by breaking the disulfide bonds, extracellular proteolytic enzymes hydrolyze the peptide bonds. A two-step mechanism was also proposed for bacterial keratinolysis, except that disulfide bridge seem to be attacked by a reductive mechanism and the whole process is faster. The peptide bonds are broken down to low MW peptides or even amino acids. The significant role of reducing agents in proteolysis of keratinous substrates is well documented in the literature.

Ignatova et al. (1999) [74] showed that in vitro addition of the reducing agent 1,4-dithiothreitol to split disulfide bonds stimulated the lysis of keratin by an extracellular keratinase isolated from a wool-degrading actinomycete. Studies on feather degradation by bacterium Bacillus licheniformis established that extracellular proteases cooperatively act with intracellular disulfide reductases to accomplish keratinolysis [75]. Extracellular keratinase cannot act alone; it necessarily needs a reduction-oxidation system. Commercial keratinases (Savinase) and even conventional proteases (subtilisin, chymotripsin and papain) are effective in the presence of alkaline sulfites [76], [77].

Enzymatic hydrolyzates exhibit particular properties, as compared with the conventional ones. Fakhfakh et al. (2013) [78] reported complete solubilization of wool by a new keratinolytic bacterium Bacillus pumilus A1, in slightly alkaline media (pH 10). The protein hydrolysate exhibited a high in vitro digestibility (97%) as compared with the untreated wool (3%), and antioxidant potential in terms of radical scavenging activity. The same Bacillus pumilus strain had similar keratinolytic activity on the chicken feather, despite the structural differences between feather and wool keratins [79]. Enzymatic hydrolysates of chicken feather and cow horn and hoof, obtained by using a protease derived from Bacillus subtillus, and having molecular weights between 1 and 10 kDa, also exhibited remarkable antioxidative properties, measured in terms of 1,1-diphenyl-2-picrylhydrazyl (DPPH) radical scavenging activity [80]; cysteine was reported to be responsible for high antioxidative activity [81]. Feather hydrolysates with high soluble protein content, obtained with the Chryseobacterium, were reported to exhibit antioxidant and antihypertensive activity [82].

Compared with the alkaline hydrolysis which results mainly in peptides of higher molecular weight, the hydrolysate resulted from enzymatic action mainly contains low molecular peptide fractions, and even amino acids [83].

The predominant amino acids released in feather hydrolysate were tyrosine, phenylalanine, and histidine, while the wool lysate was rich in aspartic acid, methionine, tyrosine, phenylalanine, histidine, and lysine [84]. Nutritionally essential amino acids such as phenylalanine and methionine, which are rare in wool keratin, were produced in considerable amounts as microbial metabolites [83]. Wool and feather enzyme hydrolysates preserved the α-helix and β-sheets conformations, respectively [76].

Two-stage hydrolysis combines chemical and enzymatic attack, the alkaline-enzymatic process being the most common. Chemical hydrolysis is applied as a preliminary solubilization treatment, and their combination often results in technological and economical benefits: solubilization yield, hydrolysis degree, and hydrolysate quality can be more efficiently controlled and tailored, in accordance with the desired end application [85]. Alkaline-enzymatic hydrolysis performed in similar conditions, resulted in a maximum solubilization yield of ≈ 60% for wool keratin [86], while the solubilization rate for feather keratin was of ≈ 90% [87]. In contrast, Eslahi et al. [76] reported higher solubilization of wool through enzymatic hydrolysis, in the presence of a reductant and surfactants.

Keratin enzymatic hydrolysates are obtained by a high efficiency under mild reaction conditions, environmentally friendly process and have characteristics that make them ideal candidates mainly for agricultural fertilizers [88], and supplements in animal feed [89].

## Biomaterial application

This section reports the new advanced material, concerning of application of keratin in perspective biotechnology.

In recent years, biopolymers consider it as a privileged material for the sustainable development and environmental sustainability concepts. Biopolymer material has found in the different feasible applications from biomaterial application to the industrial arena [90]. Biomaterials have been improved, and are continuing to be developed, along with the developing of new material to production processing, product quality and standardization in bio-application fields. With the demand of sustainable materials, the protein-based materials become a promising candidate as worthy material to exploit. Keratin, among all protein sources, has obtained attention as one of the biodegradable materials with abundantly present in nature and it can be extracted from low-value abovementioned bio-sources [91], [92]. Also, keratin has been considered as a source of durable biopolymer material and as an alternative of synthetic polymer, particularly in the advanced applications. Biological characteristics and practical considerations are both of importance to evaluate future applications of keratin.

In the area of biostudy, keratin has been defined by National Library of Medicine as a “class of fibrous proteins or scleroproteins important both as structural proteins and as keys to the study of protein conformation. The family represents the principal constituent of epidermis, hair, nails, horny tissues, and the organic matrix of tooth enamel”.

This significant amount of keratin sources in the environment is of notable for considering material as the proper potential for advanced technology. A Recent development [93], [94] has identified that keratin in the body plays not only physical roles but also its essential in the transportation in signaling peptide. Wool and avian keratin sources, also have the particular limitation of consumer perception. In particular, the significant difference in keratin structure and cystine content limit their functionality and use for the development of robust material. However, keratin protein is well fitted to the development of the advanced application. New standardization criteria are encouraging of development of biopolymer as an alternative to the oil-derived synthetic material. Keratin has significant proportion in medical treatment as such wounds or hard tissue injuries to nutritional applications. Different studies have carried out to investigate keratin sources physicochemical structure both in macroscopic and microscopic characteristics. One of the most relevant content which can be useful in some application is the cystine. Treatment of a range of diseases such as HIV, chronic bronchitis, and cardiovascular disease is associated with cystine, having some known of biological function, with providing oxidative protection to cells. The focus of this chapter is the consideration of the advanced applications of keratin, especially in the biomaterial fields. The manipulation of keratin for considering in the advanced application is not straightforward, and this difficulty has been the main reason that keratin protein has not been commercially exploited as material in a way that other biopolymers such as collagens, cellulose have been. For developing keratin material beyond limited application, a series of process for isolation of keratin proteins that maintain core feature of the protein its structure needs to be improved. In this process, the hydrolyze do not occur on the peptide bonds and allow the keratin protein remain on native structure and form.  This protected isolation maintain the keratin chemical complexity as native keratin, and substantial fibrous proteins remain naturally form robust and ordered material, and also amino acids component presence in abundance; consequently, advanced applications in a range of areas can be developed.

Keratin can be used for enhancing the repair of tissue for different organ of the body. Some studies have carried out to use keratin for providing better “healing properties” in bone damage. Bone mainly consists of fibrous protein, a mineral composites such as collagen and calcium, so using alternative protein fibroin and mineral composite for bone augmentation is quite reasonable as short time frame; [28]. Moreover, a study on repairing and improving the soft tissue structures have been gaining ground. Keratin has been counted as a proper candidate to apply in the soft tissue, such as to fill spaces for tissue enhancement or intervertebrate discs in the spine. In addition, considering keratin in other biological area has been interested. In particular, keratin characteristic has been studied and used as regenerative medicine, cell therapies, and regenerated tissue, in nerve generation.

Also, keratin-based protein is a major part of skin structure, that is why another field of advanced application from keratin have been developed successfully in wound dressing from acute to chronic  [93], [95]. Among different keratin and other protein species, wool keratin because of its structure having a high degree of homology and substantial similarity in structure shows the proper performance when compared with skin structure.

Keratin also has been developed to the ingestible material in advanced applications. Using ingestible keratin is recorded almost 100 years ago with the different area such as an enteric coating of pharmaceutical tablets; however, various types of oral supplements and liquid beverage with a variety of ingredient have emerged on the market. Mostly, these materials are used in the area of joint health, targeting the high-growth aging population, and the high sulfur content of the protein are significant element in the performance of the products in term of oxidative stress.

Extraction of proteins from natural sources has a solid research foundation and resulted in biomaterials currently used for biomedical purposes [96]. Keratin as a versatile biopolymer, becomes very attractive for advanced applications, despite the difficulties related to solubilization and extraction from the keratinous sources. These bio-applications are based on keratin properties: intrinsic biocompatibility, biological activity, cell adhesion, self-aggregation and crosslinking ability, cytocompatibility (in terms of cell attachment, viability, and proliferation), biodegradability.

Keratin is able to bind charged species such as heavy metal ions (copper, chromium, lead, mercury, etc.). It also can be used to remove formaldehyde and other Volatile Organic Compounds (VOC) from the environmental [39]. Moreover, it has a various application in cosmetic industries for the treatment of the skin and hair [97]. Also, scaffolds obtained from fibrils and the cell growth for cell cultivation have been developed. The production of sponge was careid out by disruptionof the histological structure of the ﬁbres through mild alkali treatment, followed by ultrasonication, casting and salt-leaching. [15].

Keratin forms which preserve the structural organization of the native keratin and are prone to suitable physical states, became attractive candidates for tissue engineering applications for the obtaining of scaffolds for tissue engineering, even if they exhibit lower cytocompatibility (in terms of cell adhesion, cell viability and cell proliferation) than collagen or gelatin [98]. Besides human hair [99] wool is becoming a preferred source of keratins for bio-medical applications. Cosmetic applications of keratin solubilizes are directed mainly to proprietary hair-care products, owned by the producing companies.

Hydrolysis conducted under certain conditions can also produce soluble protein forms useful for biomaterial fabrication [100]. Kerateines and S-sulfo-kerateines preserve hydrophobicity and ability to regenerate the starting keratin through crosslinking, while keratoses are hydrophilic and loose the crosslinking ability. Organic peracidic are highly specific their attack on disulfide bonds and preferred for advanced applications [101], and it is more stable and offer the advantage of low cost and availability but exerts certain hydrolytic attack on peptide bonds and oxidize some lysine and arginine residue [7].

Thus, biomaterials with different physical configurations and functions in relation to the living bodies can be fabricated, as given in Table ‎1-1.

Table ‎1-1-Feasible solubilization methods and biomedical applications of wool solubilization products

| Solubilization method | Solubilization product/ physical state and characteristics | Application | Reference |
| --- | --- | --- | --- |
| Reduction | Kerateine-sodium alginate/high porosity sponge | Cell culture | [102] |
|  | Multilayer films by the layer-by-layer method | Biocompatible surface for tissue engineering | [103] |
|  | Kerateine, sponge-like porous hydrogel | Scaffold for animal cell culture | [104] |
|  | Kerateine/Hydrogel | Drug carrier Cell culture substrate | [105] |
|  | Kerateine/injectable and cytocompatible gel | Pulp-dentin regeneration | [106] |
|  | S-carboxymethylated) kerateine/PCL-keratin nanofibrous mats | Scaffold for vascular tissue engineering | [107] |
|  | Kerateine reduced with L-cysteine/ hydrophilic PCL-keratin nanonets | Cell culture substrate with enhanced cell adhesion and proliferation properties | [108] |
| Oxidation | Keratose/hydratable fibers or powder | Wound dressing, filler for implant applications | [109] |
|  | α-keratose/stable hydrogel | Cell scaffolding for adhesion and proliferation of fibroblasts | [110] |
|  | Keratose/matrix composition | Acellular scaffold for nerve regeneration | [95] |
|  | Keratose and sulfonated keratine homologs/ solution | Additive in self-care products | [111] |
| Sulfitolysis | S-sulfokerateine/ microparticles (~6 µm) | Microparticulate drug delivery system | [112] |
|  | S-sulfokerateine/filler in poly(L-lactic) acid based biocomposite films | Culture media for human bone-marrow mesenchymal stem cells | [113] |
|  | S-sulfokerateine/photo-active film with antibacterial activity | Wound healing and tissue engineering | [114] |
|  | S-sulfokerateine doped with polydopamine nanoparticles/ sponge with tunable morphology | 3-D scaffold for cell culture, with antioxidant properties Tissue engineering, drug delivery | [115] |
|  | photofunctionalized S-sulfokerateine/sponge with tunable porosity | 3D scaffold for human fibroblast cells growth, with antimicrobial activity | [116] |
| Mild alkaline hydrolysis | Nanoparticles | Biomimetic keratin/hydroxyapatite nanocomposite for osteoblast culture and bone tissue regeneration | [117] |
|  | Microfibril sponges | Extracellular matrix-mimetic biomaterial/scaffold | [15] |
| Ionic liquids | Keratin-cellulose-chitosan composite films | Drug delivery substrate | [118] |
|  | α-keratin, powder | Electrospun nanofibers for bandages or hydrogels/ wound healing | [41] |
|  | Keratin-cellulose blend regenerated by casting | Scaffold for biomimetic hydroxyapatite mineralization | [119] |

To meet the final application requirements, the keratins resources, sources, and processing pathways must be considered when the ranges of possible transformation are chosen for converting a “biological material” to an “engineered” one.

Biomedical applications of proteins require minimal deviation from the native state and consequently impose severely constraints regarding the methods of isolation, extraction and purification; in this case, protected solubilization approaches and techniques must be employed. The primary target is to preserve the macromolecule integrity, and the ability of the new-born groups derived from disulfide bonds splitting to re-crosslink and regenerated keratin supramolecular structures.

Bio-oriented applications exploit the intrinsic biocompatibility, biodegradability, and biochemical stability properties of keratins [120], whereas technological ones make use of their stiffness, strength, and resistance against aggressive environmental agents [90]. It must be noted that most of the processes mentioned in Figure ‎1-4 are currently in use in wool chemical technology, with the aim of imparting specific properties to the in-process wool with minimal damage.

## Microcapsule and film

One of the foremost domain of applying keratin in bio-field is related to the drug carrier and the film for different unique applications. Nowadays, the application of microcapsules and bio-related film have increased to include advanced manufacturing technologies associated with high-level design for cosmetics, wound healing, pharmaceuticals, agrochemicals, composite materials and other high-tech products and processes. Encapsulation consists of surrounding a selected material, which constitutes the core, with some solid shell of a different compound, the nature of which is based on the proposed application. Examples of encapsulation purposes could be to protect materials inside the core against oxidation or reduction, to allow safe handling of toxic materials, to keep core materials from evaporation, or to mask unpleasant odors and flavors. Nevertheless, one of the most useful properties of microcapsules for cosmetic and pharmaceutical application is the capability to release the core materials slowly for prolonged periods of time [121]–[126]. Protein microcapsules have attracted particular attention because of their potential for the treatment of disease as a drug carrier. Different types of protein can be used for fabricating microcapsules like α-amylase with good enzymatic activity compared with native α-amylase [127]. In addition, many studies on microencapsulation have focused on the use of biodegradable and biocompatible synthetic or natural polymers and how their molecular structure could be tailored according to the desired applications. For instance, polylactic acid (PLA) and polylactic-co-glycolic acid (PLGA) were utilized for the microencapsulation of therapeutics and antigens. Moreover, polysaccharides (chitosan, dextran, hyaluronic acid, starch, alginate) and proteins (keratin), have also been proposed [128]–[134] due to the presence of functional groups suitable for chemically enhanced encapsulation [127]. There is also an emerging interest in the encapsulation of hydrophobic molecules. Hydrophobic material with a protein carrier can be entrapped by sonochemical methods with significant dimension [129], [135].

Notably, the cysteine amino acids residues form disulfide bonds (cysteine residues) cause a compact three-dimensional structure which confers to the keratin proteins a high resistance to chemical and enzymatic attack [136].

Water-soluble keratin is one of the properties which can be quite helpful for applying in the biomedical application. Extracted keratin via oxidation and sulfitolysis methods lead to the water-soluble products with high molecular weight. All these characteristic cause to consider keratoses have a great potential to use for the tissue engineering, drug delivery, and regenerative medicine applications. Different studied presented application for keratoses such as biocompatible fillers for implant application [109], matrix for peripheral nerve regeneration [95], hydratable powders for viscoelastic hydrogels that support cell adhesion and proliferation [110], wool-derived oxidized keratin kit for wound repair and burn healing [137], [138]. Also, Oxidized keratin derivatives show good blood and cardiovascular compatibility and can induce vasodilation [139], or promote angiogenesis  [140]. Due to the affinity of cysteic acid residues for soluble charged species, keratoses can find environmental applications as adsorbents for heavy metals [141]. Cosmetic uses are mainly related to hair treatment commercial products.

On the other hand, producing different blend materials from keratin have been reported. Some research related to the keratin film reported poor mechanical properties. Moreover, this is always concern about toxicity in the bio-field and food packing.  Poly (vinyl alcohol) is synthetic hydrophilic and biodegradable polymer with a wide range of applications in the food packing, variety of coatings and pharmaceutical industries [142]. PVA is a partially crystalline polymer, and this crystalline phase contains plate-like single crystals (lamellae) which are bound to each other by disordered polymer chain forming of amorphous polymer phase [143]. This polymer is proper for resistance to the organic solvent, thermal stability, and appropriate adhesive properties. Recently PVA has been used in the biomedical field and for application such as drug delivery, wound healing, ultrafiltration and tissue engineering scaffolds. This polymer has a significant chemical stability and good-film forming capacity [144], [145]. Because of its biocompatibility, PVA/protein films are produced for different application such as food packing, tissue engineering, and drug delivery system. Various studies have been devoted to cross-link protein blend film  or protein belnd film/ PVA with various agents [90], [146].

Films produced from keratin have relatively poor mechanical properties and fragile structure causing application and process restriction. Several work has been developed to improve different properties of keratin films by blending keratin with the natural and synthetic polymers [147]. As most of the synthetic polymers are not biodegradable, blending two biodegradable polymers may have a positive impact in environmental perspective and would be proper for bio-application [90].

## The Goals

Keratin has some instinct ability and great potential to for applying in bio-application. Moreover, because of its complex structure, keratin can be tailored and finely tuned to meet the precise final application requirements.

The purpose of this study mostly dedicates in investigation physicochemical properties of keratin and compares them with previous studies. Part of the thesis focus on the different essential available pathways for the solubilization, extraction, and purification with highlighting on their pros and cons as well as some the mechanism of action and physiological feature of keratin. The effects of each method on the physicochemical structure have discussed and also the character of the different keratin-based material significantly reported how obtained keratins are affected by the each purification process. The achieved results were compared with earlier studies with the aim of emphasis possibility available in line with developing a bio-application approach.

The other section of the thesis, chapter 3, is specifically looking into the study on the particular application of keratin biomaterial in the shape of drug carrier and film. The keratoses, one of the high-quality obtained keratin, have been utilized for producing keratin-based microcapsules and film. The keratoses, with the high-cysteine keratin, readily underwent to oxidative polymerization to effort microcapsules and film. The newly developed microcapsules produced and characterized. Taking advantage of the high-cysteine content of keratoses, we had applied the sonication to produce microcapsules. On the other hand, keratoses film without any additives is quite fragile, and the biodegradable synthetic polymers have been widely used in the medical fields due to the biodegradability and high processibility into different shapes. In the continue in chapter 3, the new form of the keratoses blend film with PVA with various ratios was developed to overcome of physical limitation of the keratin-based film.

# Chapter 2

# Extraction and Purification of keratin

## The purpose of the present chapter

This experimental section aims to extract keratin with different main methods: oxidation, reduction, sulfitolysis and superheated water hydrolysis. The produced keratin from critically characterized by various assays, as well as compared each physicochemical properties in details to suggest more suitable applications in the correlation of each extraction.

## Preliminary discussion on extraction pathways

Wool is contained predominantly three-dimensional keratin structure which constituted with different amino acids. Wool structure is insoluble in water, weak acids, and alkali solution and has a structure with resistant to the majority of the chemical and physical substances. Keratin has a high amount of cystine, serine, glycine, and proline which significantly affect on physicochemical properties of wool keratin. The main pathways utilized to purify and extract from the keratinous material are oxidation, reduction, sulfitolysis and hydrolyzation which as it mentioned each method displays unique properties. Keratin macromolecule acts as an amphoteric polyelectrolyte, whose overall charge depends on the pH of the surrounding aqueous media. The pH at which the net positive charge of the side chains is balanced by the net negative charge of the side chains and the macromolecule is electrically neutral, is called the isoelectric point (pI). Native proteins exhibit pI intervals rather than a pI point; keratins specific to hair or wool have a pI interval of 4.7–6.1 (see Figure ‎2-1).

Figure ‎2-1-Dependence of keratin macromolecule charge on pH, and affinity for charged species

### Oxidative methods

The basic recipe and working conditions for wool solubilization by organic peracids were established by Alexander et al. (1950) and Alexander and Earland (1952) [6], [148], and suffered slight modifications in current applications. As a definitive oxidation mechanism has not been yet established, the choice of an oxidation system is rather based on a pragmatic approach.

Most studies on oxidative solubilization of keratin are focused on wool and hair, for which several oxidizing agents are used: hydrogen peroxide, organic peracids, and inorganic persalts. At present, the most attractive seem to be the peracetic acid and peroxide inorganics (H2O2, perborates, percarbonates) /alkali system, which are efficient and environmentally friendly. Hydrogen peroxide decomposes without leaving unwanted secondary reaction products and acts as a “green chemical” [149]. The oxidative solubilization is the result of a cooperative effect of oxidative agent and alkali. With ordinary concentrations and temperature values (up to 10% H2O2, pH ≈13, room temperature), wool does not directly dissolve in the oxidizing media, but in subsequent alkali media, so dissolution proceeds through a two-stage process; the oxidative treatment increases alkali solubility by up to 6 times [150]. The hydrolytic effect of alkali on both peptide and cystine oxidation intermediates cannot be neglected [151]. Yamada et al. (1994) [152] patented a one-stage process for solubilizing animal hair or wool using hydrogen peroxide in high concentration (25 - 35%) in weak alkaline medium, at pH of 8-9, with a solubilization yield of up to 99.7% and a main keratin fraction having the MW in the 25-67 kDa range. Unlike other alkaline treatments, no lanthionine bridges derive as final products from the cystine group oxidation [153]. The destruction of disulfide bonds not only opens the structure of hair but provides additional hydrophilic centers in the form of cysteic acid residues, which significantly alters the swelling characteristic and lowers the isoelectric point of the keratin product [154].

Keratoses are water soluble, cannot participate in cross-linking reactions with the reformation of the disulfide bridges, and are susceptible to hydrolytic degradation due to the polarization of the backbone caused by the electrophilic properties of the cysteic acid. These characteristics lead to biomaterials that can degrade relatively fast in vivo as compared with kerateines, i.e., in the order of days to weeks [42]. Cytotoxicity assays indicated the non-toxic and non-immunogenic nature, and resorbability [37], which makes keratoses biologically compatible and suited for tissue engineering and regenerative medicine applications.

### Reductive methods

One of the benchmark reductive pathways for obtaining quasi-native keratins suitable for biomedical applications implies wool solubilization with 2-mercaptoethanol (2-ME), in solution buffered at pH 9.5, and 8 M urea as chaotropic agent; the alkali media induces partial unfolding of the highly packed keratin structure and favors the reduction reaction [34]. Further processing implies removal of reductant and denaturant from the reaction mixture by dialysis when unwanted aggregation between keratin peptides occurs. Cardamone (2010) studied the microstructure of keratin extracted from wool by reduction: from SDS-PAGE electrophoresis, protein homologs of molecular weight ≈ 40–60 kDa were isolated; MALDI-TOF/TOF spectrometry identified Type II microfibrillar component 7C, Type II intermediate filament, Type I microfibrillar 48 kDa component 8C-1, and Type I microfibrillar 47.6 kDa protein homologs; FTIR spectroscopy applied to examine secondary structure confirmed the relative content of α-helix/β-sheet/disordered regions for original wool (58.2%/37.9%/3.9%) and the higher content of β-sheet secondary structure and intact α-helical conformation of reduced keratin (36.7%/50.2%/13.1%).

Stable colloidal solutions, able to preserve crosslinking ability and form films with excellent mechanical properties were obtained when ≈50% of the cysteine groups were blocked by carboxymethylation [155], [156].

According to Schrooyen et al. (2001b) [157], the addition of sodium dodecyl sulfate (SDS) to the reduced keratin solution, prior to dialysis, inhibited the oxidation of –SH groups and prevented extensive aggregation of the keratin chains. Yang et al. (2007) studied the effect of concentration of extracted keratin on the rebuilding of disulfide bond during dialysis against deionized water and found that at high concentration (as much as 3.5 mg protein/mL) cross-linked networks are promoted in the aggregate, whereas at low concentration, intramolecular disulfur bond is preferred. This finding has a high potential for controlling the crosslinking between keratin chains without the addition of other chemicals, which is helpful to construct bio-macromolecular self-assemblies.

Several alternative techniques are presented in specialty literature with the aim of improving solubilization yield and kerateines stability. Thus, a stable aqueous solution of reduced keratins was prepared from wool, with an extraction yield of 48%, in the presence of additional SDS, in neutral media (pH ≈ 6.7); films subsequently obtained were insoluble in water and organic solvents but permeable to glucose, urea and sodium chloride and underwent slow biodegradation in vitro and in vivo, which made them promising biomaterials [158]. Japanese researchers conceived the so-called “Shindai method”, in the absence of surfactant and using urea and thiourea as denaturing media, at pH 8.5 and 50°C, for 1 to 3 days. The extracted protein fractions were composed of microfibril keratins with MW of 40-60 kDa, matrix with a MW of 10-20 kDa and HMW minor components (110-115 and 125-135 kDa), while the fraction produced by the conventional method was mainly composed of two protein doublets of keratins with a molecular mass of 40-60 kDa. This method proved to be highly effective for protein extraction from human hair, wool, and feathers, with extraction yields higher than 65 % [33]. At present, the Shindai method is considered the reference method for extraction of minimally denatured keratin factions, both for analytical and preparative purposes.

A modified Shindai method was proposed [159], in which reduction was preceded by a mild acidic pretreatment with HCl. The reduction was performed with a low urea concentration of 0.33 mol/L and resulted in keratin solubilizates with a molecular weight of about 20 kDa and high homogeneity; the yield of pure keratin was up to 90%. It is supposed that the acid attacks the amorphous matrix only, and exposes the intact microfibrils to reductive attack, which is in agreement with other works (Istrate et al., 2013).

Reductive methods are focused on the extraction of microfibrillar keratins; recently, Shindai solutions containing additional low molecular weight alcohols were reported to extract the keratin-associated proteins, while extraction of IFKs was suppressed [160].

Large scale application of thiol reduction is not feasible because the procedure uses strong-smelling reducing agents and other chemicals in high concentration, kerateines isolation is complicated and the whole process is time and labour intensive. Recently, the use of commercial cysteine as an eco-friendly reductant in a conventional reductive process for waste wool was reported. The quasi-native solubilized keratin was regenerated into fibers of 20 µm, with good tensile strength [161].

Sodium sulfide in alkali media is also an industrially convenient system, using a cheap reductive agent. The reduction mechanism is complex. The sodium sulfide dissociates into hydrosulfide and hydroxyl ions, which raise the pH of the reaction mixture.

The hydrosulfide anion, HS- reduces the protein disulfide bond by dissymmetrical splitting, as given in Equation ‎2-1:

Equation ‎2-1- Reduction of disulfide bond

The hydroxide ions can reduce the disulfide bonds to reactive dehydroalanine residues, which readily cross-link with the amino acid side chains of cysteine and lysine to form lanthionine and lysinoalanine, while the perthiocysteine residues decompose to form cysteine and sulfur [45]. Reduction proceeds together with alkali hydrolysis and can result in advanced splitting of the protein backbone and in the low-value oligopeptides as final products. For this reason, the potential of the sulfide-alkali system for converting the keratinous substrates into biomaterials for advanced applications must be carefully considered. Optically transparent and smooth films with reasonable mechanical properties were casted from keratin solution obtained by solubilization of avian feathers with sodium sulfide; for shorter treatment times of 5-6 h, SDS-PAGE quantification showed 68-70% 10 kDa monomer fraction, and 15- 9% dimer fraction.

Protection of the peptide groups limited the solubilization yield to 55% [162]. Keratin-cellulose and keratin-alginate solutions were successfully prepared with sodium sulfide reduced keratin powders, having medium molecular weight in the range 22 - 12.5 kDa, and water sorption capacity of up to 45%, from which fibrous materials with high absorbing properties for sanitary and cosmetic products were obtained [163]. A patented method produces stable dispersions of partially reduced and partially hydrolyzed keratin solubilizates from chicken feathers, using sodium sulfide in alkali; the resulting keratinous forms have MW between 1 kDa and 10.4 kDa, and can be used for obtaining biodegradable films, coatings, controlled release systems, adhesives, etc. [164].

Recrosslinking ability, hydrophobicity, and hydrolytic stability, in vivo and in vitro degradation, enabling of cell adhesion and proliferation, make kerateines a most valuable raw material for biomaterials [165]. Reduced keratins can be applied for producing films, sponges, high porosity scaffolds or bulk powders with valuable uses in regenerative medicine and tissue engineering; protein matrices are superior for tissue engineering, compared to matrices made from synthetic material due to their similarity to native extracellular matrices.

Keratin extracted by Shindai method from different keratin resources (human hair, wool, feather, and horns) and processed as films [158], [166] or porous scaffolds [167], [168] exhibited excellent mammalian cells attachment and proliferation. Mechanical and biocompatibility properties of films can be improved by preparing mixed keratin-polysaccharide films in the presence of a plasticizer [169]. Reduced keratin extracted from wool can act as a building block for multilayer films obtained by the layer-by-layer method, in conjunction with synthetic polymers [103]. An improved highly porous and flexible keratin sponge was developed from reduced keratin in the presence of calcium alginate beads; the keratin sponge was flexible even in dry state due to its high porosity (about 98.9%) and supported the attachment and the proliferation of mouse fibroblast at a satisfactory level [102].

Wool kerateine scaffolds with a homogeneously porous microstructure, pore size ≈100 μm, and high heat resistance were obtained by freeze-drying. Rapid cell growth on the sponge was observed for at least 7 days, and cells with no abnormal morphology were observed for 23-43 days; the maximum cell number was 7.4 million, ≈37 times higher than on the same area of a commercially available plastic culture dish [16], [104] (Tachibana et al., 2002). Ozaki et al. [104] reported the production of a sponge-like porous keratin hydrogel, from kerateine extracted with guanidine hydrochloride as a denaturing agent. The gel exhibited high porosity and mechanical strength, fast swelling and excellent attachment and growth of different animal cells. Drug release and cell proliferation supporting properties of hydrogels obtained by conventional chaotropic-assisted reduction can be modulated by the agent used for the subsequent blockage of cysteine residues [105].

### Sulfitolysis methods

As compared with reduction, sulfitolysis uses inexpensive, chemically benign and odor-free reagents. The attack is very specific to the cystine and cysteine residues in the protein, and hence the bioavailability of other essential aminoacids is preserved.

The dissolved S-sulfokerateines can be fabricated into different forms, with variable functionality. Biocompatible films from S-sulfokeratin were prepared by compression-molding [90] or by solvent casting [170] starting from wool solubilized by plain sulfitolysis in neutral denaturing media. The resulted S-sulfokeratin films supported the mammalian cell adhesion and proliferation, thus proving their biocompatibility. Films obtained from sulfitolyzed keratin were weaker and more elastic than films from reduced keratin. Blending keratin with another biopolymer can modulate the biological degradation rate [36]. Cilurzo et al. (2013) [112] reported regeneration of wool S-sulfokerateine in microparticles for drug delivery systems.

Feathers can also be used as starting materials for regenerating keratins by sulfitolysis. A highly porous, insoluble keratin sponge, with high oil adsorption capacity was obtained from pigeon feathers solubilized with Na2S2O5 in denaturing media, by an improved technique [171]. Biocompatible films or foams for wound healing applications can be produced starting from highly S-sulfonated keratin, by controlled re-crosslinking with different chemical agents [172].

Nomura et al. (2002) [173] found that S-sulfokerateines from pig hair act as a self-assembly promoter of type I collagen, and can control the strength of the collagen gel. Peplow et al. (2007) [28] patented a biocompatible material derived from S-sulfonated keratin intermediate filament and hydroxyapatite, which can be used as a bone replacement or as an internal fixation appliance in the treatment of bone fractures. In the field of recombinant protein pharmaceuticals, oxidative sulfitolysis was proposed as a time-saving and benign alternative to the reduction/alkylation method for high performance peptide mapping [174].

### Chemical-free hydrolysis

Lately, chemical-free hydrolysis is gaining ground, as a “green” or environmentally friendly alternative to conventional methods [32]. Moist heat and pressure in neutral media cleave the disulfide bridges but it also attacks the peptide backbone, so mixtures of oligopeptides and aminoacids will always result. Control of process parameters is difficult and determines a delicate balance between sufficient hydrolysis and over-processing. Two methods are in use for the chemical-free hydrolysis of keratinaceous materials such as a feather, wool or hair: steam hydrolysis/steam explosion, and superheated water.

Steam explosion is a process in which biomass is treated with hot steam (180 - 240 °C) under pressure (1 - 3.5 MPa) followed by an explosive decompression that results in an advanced rupture of the biomass structure. Wool subjected to steam explosion led to a mixture of water-soluble peptides and free amino acids and a solid residue with advanced disruption of the histologic structure, associated with breaking of disulfide bonds and decomposition of the high-sulfur-content protein fraction [175]. Superheated water has been shown to be effective in the hydrolytic dissolution of keratinous materials. Yin et al. [47] reported almost complete dissolution of the feather barbs after heating in water at 220 °C for 120 min, with total cleavage of cystine bridges. The resulting oligopeptides exhibited the ability to self-assemble in birefringent needle-like crystals which tend to nucleate heterogeneously and develop highly repetitive structures. The oligopeptides can be used as building blocks for the synthesis of a range of novel polymeric materials with advanced applications. Wool was hydrolyzed with superheated water at 150-180°C, using microwaves as a heating source; the soluble fraction was composed of aminoacids, low molecular weight polypeptides and proteins having MW in the low fraction range at around 8-3 kDa, a low content of cystine and lanthionine, and a mainly disordered secondary structure [48]. There is no clear evidence of a specific action of microwaves on keratin disruption, and apparently, microwaves are only a green heating method for water [176].

Properties of keratin hydrolysates must be related to their end uses. Drug-related and cell-culture applications require endotoxins removal, by ultrafiltration through membranes with a 50 kDa or even 10kDa molecular weight cut off [177]. Li et al. (2013) [178] showed that alkaline wool hydrolysate had no obvious negative effect on cell viability in vitro, no oral toxicity, no influence on body weight, feed consumption, blood chemistry, and hematology at any dose levels so that it can be safely used as a food ingredient or drug carrier. The high content of β-sheet or α-helical secondary structure, high solubility and chemical reactivity can make keratin hydrolysates viable starting materials for novel bio-based materials useful in industrial formulation and compositions with agricultural [179], zootechnical [1], environmental [180], [181], or cosmetic [182] uses; lower molecular weights considerably limits their uses for advanced biomedical applications. Alkaline hydrolysates from chicken feathers were proposed as green sizing agents on polyester/cotton blends and polyester, as they provided similar sizing performance to conventional poly(vinyl alcohol) and high biodegradability in active sludge treatment of wastewater [183].

Chemical and hydrothermal hydrolysis have several disadvantages related to products with poor characteristics as it concerns digestibility and nutrient quality, color and smell, mainly coming from non-specificity of the hydrolytic process and difficult control of process parameters [184].

## Materials and methods

Wool fiber, 22 μm mean diameter, in the form of top (fiber sliver obtained from raw wool by scouring, carding and combing processes) was supplied from The Woolmark Co., Italy. All chemicals were of analytical grade and purchased from Sigma-Aldrich, except otherwise specified.

The fiber sample was cleaned by Soxhlet extraction with petroleum ether to remove fatty matter and surfactants, washed with Milli-Q water, conditioned at 20 ⁰C, 65% R.H. for 24 h  and cut into snippets around 2 mm length before further treatments.

Keratin extraction processes were carried out by oxidation [185], reduction [186], sulfitolysis [147] and superheated water hydrolysis [48].

## Extraction pathways

In this section different extraction procedures of extracting of keratin from wool fiber has been reported.

### Oxidative extraction

For the oxidative extraction 4 g of wool were put an aqueous solution of 2% peracetic acid for 24 h at room temperature (fiber to liquid ratio 1:50), then the oxidized sample was washed with Milli-Q water, dried, treated in a Linitest apparatus with an aqueous solution of tris(hydroxymethyl)aminomethane (Tris) 1M for 2 h at 37 °C and filtrated through a 120 mesh sieve. The filtrate was adjusted to pH 7, dialyzed in the cellulose tube (molecular weight cut off 12.000–14.000 kDa) for 2 days against the circulating system of distilled water, then centrifuged (12.000 rpm, 15 min) to remove the precipitate.

### Reductive extraction

For the reductive extraction 4 g of wool were shaken in an aqueous solution (fiber to liquid ratio 1:25) of urea (8M), Tris (0.5M), dithiothreitol (DTT, 0.14M), and ethylenediaminetetraacetic acid (EDTA, 6mM) adjusted to the 8.6 pH with HCl in a Lintest apparatus for 2 h 30 min at 25 °C and then filtrated through a 120 mesh sieve. The filtrate was dialyzed in cellulose tube (molecular weight cut off 12.000–14.000 kDa) for 2 days against the circulating system of distilled water and filtered (5 µm pore size ) to remove insoluble parts.

### Sulfitolysis extraction

4 g of wool fibers were treated with 100 mL of aqueous solution containing urea (8M), sodium metabisulfite (0.5M), adjusted to pH 7 with NaOH (5M) under shaking using a Lintest apparatus for 2 h and 30 min at 65 ⁰C. The mixture was filtered through a 5 µm pore-size filter and dialyzed with the cellulose dialysis tube (molecular weight cut off 12.000–14.000 kDa) against distilled water in a circulating system for 2 days.

### Superheated water hydrolysis

Keratin hydrolysate was prepared by treating 40 g of wool in 150 ml superheated water, for 30 min at 170 °C, using a 400 ml ceramic autoclave placed in a microwave oven Milestone Ethos 1600 (Milestone S.p.A., Bergamo, Italy). At the end of the process, the autoclave was cooled, and the resulting product was filtered with a 120 mesh stainless steel sieve. The liquid phase was further filtered by a 0.65 μm pore size, tangential flow filter (Millipore Pellicon XL).

All keratin obtained with different extraction methods were freeze-dried for successive characterizations.

## Characterization

In this part characterization of extracted keratin from the different methods are reported.

### Extraction yield

The extraction yield of the protein from the wool sample was evaluated using the following equation:

Equation ‎2-2-Evaluation of extraction yield

where Y is the yield, WS is the dry weight of extracted samples obtained after freeze-drying, and WCW is the initial dry weight of the wool sample extracted.

### Molecular weights determination:

The molecular weights of samples were determined by SDS-PAGE analysis. Keratin freeze-dried samples were dissolved in a solution of dithiothreitol/urea in a buffer (pH 8.6), under a nitrogen atmosphere for 4 h. The SDS-PAGE was performed according to the Laemmli’s method [29] using XcellLock Mini-Cell (Invitrogen), on 12% polyacrylamide gels.

### Amino acids analysis:

All the produced keratin-based material were hydrolyzed in HCl 6N for 24 h at 110 °C under nitrogen atmosphere. Free amino acid residues were derivatized with 6-aminoquinolyl-N-hydroxysuccinimidyl carbamate (AQC, Waters) and eluted on a reversed-phase column. An Alliance High Performance Liquid Chromatograph (HPLC) (Waters) was used; the eluate was detected at 254 nm. The quantitative amino acid composition, expressed as mole % for each amino acid, was determined by external standard calibration using Amino Acid Standard H (Pierce), cysteic acid and lanthionine.

### Fourier Transform Infrared Analysis (FT-IR):

Spectroscopic evaluation of extracted samples was carried out by FT-IR, Nexus Thermo Nicolet Spectrometer 510P, in Attenuated Total Reflectance (ATR) mode. One hundred scans were taken from 4000 to 650 cm−1 with resolutions of 4 cm−1 and gain 8.

### Near Infrared (NIR) analysis:

NIR spectra were acquired in the spectral region between 10,000 and 3700 cm−1, with an FT-NIR spectrometer (Perkin-Elmer) System, model Spectrum IdentiCheck (Monza, Italy), equipped with an IdentiCheck Reflectance Accessory (ICRA). For spectra acquisition, samples were placed on the 12 mm round window of the instrument; a mirror was used to reflect the beam back to the integrating sphere.

### Differential Scanning Calorimetry (DSC):

DSC analysis was performed with a Mettler Toledo DSC 821 calorimeter calibrated by an indium standard. The calorimeter cells were flushed with 100 ml/min nitrogen. The runs were conducted on the conditioned samples (20 °C, 65% R.H.) from 30 to 400 °C, at the heating rate of 5 °C/min.

### Thermogravimetric analysis (TGA):

TGA was performed on a Mettler Toledo TGA 850 analyzer. The temperature range was from 30 to 450 °C with a heating rate of 5 °C min−1 in a nitrogen atmosphere. About 3 mg of samples were used in each test using Al2O3 crucibles. The data were collected on a computer with the Mettler Toledo STARe System.

## Results and discussion

In this part result and compared discussion are discussed.

### Extraction yield

The extraction yields (% w/w) were reported in Table ‎2-1.

Table ‎2-1 Extraction yield of different extracted samples

| Extracted keratin | Extraction Methods | Extraction yield (% w/w) |
| --- | --- | --- |
| Keratoses | Oxidation | 31±2 |
| Kerateine | Reduction | 29±3 |
| Sulfo-kerateine | Sulfitolysis | 32±2 |
| Hydrolyzed keratin | Superheated water hydrolysis | 31±3 |

In general, there are no significant differences in the extraction yield between different extraction methods.

Because of the separation of oxidized wool in different fractions on the basis of solubility, keratoses obtained are about the 30% of original wool [45]; yields ranging from 30-45% w/w were obtained by Yamauchi et al. [186] using reductive extraction of wool keratin, although other authors found bigger yields [187] using mercaptoethanol or thioglycolic acid as reductive agents [188].

Similar yields (around 30% w/w) were obtained for sulfitolysis, [147] while extraction yield using superheated water hydrolysis is related to temperature, reaction time and material to liquor ratio [48].

### Molecular weight (SDS-Page)

Organic peracids are highly specific in their attack on disulfide bonds and are preferred for advanced applications. Performic acid is the more powerful oxidizing agent for wool; it exhibits a minimal or no attack on the peptide bond and no racemization, although it partially degrades triptophan and methyonine residues; wool fiber extensively swells and partially dissolves, while α-keratin is converted to the β-configuration [189]. Peracetic acid is more stable and offers the advantages of low cost and availability but exerts certain hydrolytic attack on peptide bonds and oxidizes some of the lysine and arginine residues. Wool and hair oxidized with peracetic acids and solubilized in dilute alkali consist of three fractions, α-, β- and γ-keratose [187], [190]. The α-keratose fraction precipitates at pH 4 as a fraction with high MW and a low sulphur content (2.5%), and amounts to about 45% of the fiber mass; it exhibits an X-ray pattern similar to that of α-keratin, which suggests that it derives from the IFs. The insoluble fraction known as β-keratose has a low sulfur content (2.2%) and has been identified within the cortical-cell membranes. The γ-keratose remains in solution after α-keratose precipitation and is recovered by precipitation with a water-miscible organic solvent. Low MW γ-keratose is thought to derive from the extracellular matrix regions of the hair follicle, and have molecular weights in the 10-15 kDa range.

Figure ‎2-2 shows the electrophoresis pattern of all keratin extracted samples compared with original wool as a reference. The wool sample (lane 2) shows two important protein fractions at 67 and 43 kDa which corresponds to low-sulfur (LS) proteins of intermediate filaments present in the wool cortex and the protein fraction of high-sulfur (HS) proteins in the cuticle and different bands at molecular weight lower than 10 kDa, corresponding to the high glycine, tyrosine protein of the matrix between cuticular and cortical cells [175].

Figure ‎2-2-Gel-electrophoresis pattern of the samples. Lane (1) molecular weight standard, (2) original wool, (3) keratoses, (4) kerateine, (5) sulfo-kerateine, (6) hydrolyzed keratin

In the keratoses sample (Lane 3), the most notable bands visible are at about 60 and 54 kDa, and they are originating from the LS protein of the cortex as already mentioned by other authors [37]. In fact, due to the specifically attach of organic peracidic acid to the −S−S− bond, the main chains of peptide bonds remain with low damage and the HS protein in keratoses sample is paled.

The electrophoresis patterns of kerateine and Sulfo-kerateine (Lane 4 and 5 respectively) show not significant degradation; in fact, the two extracted keratins via reduction and sulfitolysis ways showed the same molecular weight distribution of the original wool [147].

When hydrogen peroxide in alkali media is used as oxidation agent, 90% of the keratin solubilizate contain protein fragments with MW between 3.5 and 12 kDa, which proves the low specificity and higher severity of the H2O2 attack  [191].

The electrophoresis patterns of superheated water hydrolyzed sample show that the strong bands of LS proteins disappeared and bands of high protein density appeared in the low fraction range at around 14–3 kDa. The loss of high molecular weight keratins indicates that the chemical structure of wool was significantly affected by the high temperature of the hydrolysis treatments with the cleavage of peptide bonds [175].

In previous research, SDS-PAGE electrophoresis of the alkaline hydrolysate detected peptide fragments of ≈6–8 kDa [46]. Recently, Tsuda and Nomura (2014) [192] showed that both feather and wool keratin preserved their original secondary structure after alkaline hydrolysis, but feather hydrolysate contained more hydrophobic amino acids than wool hydrolysate, which can help direct the hydrolysates towards the most suitable end uses.

### Amino acid Analysis

The amino acid amount of all extracted samples compared with original wool is presented in Table ‎2-2. Wool is essentially pure protein (keratin) and hydrolysis yields the amino acids commonly present in the hydrolysates of most proteins. However, the relative amounts of these amino acids may vary from one sample to another, in relation to sheep breed, diet, health, etc.. During HPLC preparative hydrolysis of keratins with HCl, several amino acid residues undergo various degrees of degradation and conversion. Tryptophan residues are completely destroyed by the acidic conditions, methionine, cystine, cysteine and tyrosine undergo partial degradation, while asparagine and glutamine residues are completely converted to aspartic and glutamic acid, respectively; cystine and cysteine are detected as 1/2 cystine.

During different extraction processes, cystine disulfide bonds are cleaved, and new residues are formed according to the extraction process.

Table ‎2-2-Amino acid analysis:  keratoses, kerateine, sulfo-kerateine and hydrolyzed keratin compared to amino acid analysis of original wool.

| Amino acid | Wool fiber | Keratoses | Kerateine | Sulfo-kerateine | Hydrolyzed keratin |
| --- | --- | --- | --- | --- | --- |
| Cysteic acid | 0.2 | 7.8 | 0.3 | 0.4 | 0.2 |
| Aspartic acid | 9.3 | 10.5 | 9.6 | 8.4 | 8.8 |
| Serine | 11.7 | 11.6 | 11.0 | 11.9 | 10.7 |
| Glutamic acid | 15.6 | 17.7 | 15.6 | 14.6 | 19.5 |
| Glycine | 7.3 | 6.7 | 8.1 | 8.1 | 9.0 |
| Histidine | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 |
| Arginine | 5.9 | 6.0 | 6.4 | 6.1 | 5.9 |
| Threonine | 6.8 | 7.0 | 6.6 | 7.5 | 6.2 |
| Alanine | 5.7 | 5.8 | 5.6 | 5.2 | 8.3 |
| Proline | 3.1 | 3.2 | 3.2 | 4.2 | 3.7 |
| Lantionine | 0.4 | 0.6 | 0.6 | 0.7 | 2.3 |
| 1/2Cystine | 9.5 | 0.0 | 8.1 | 10.6 | 0.5 |
| Tyrosine | 2.5 | 2.2 | 3.0 | 2.7 | 2.4 |
| Valine | 5.5 | 5.3 | 5.3 | 5.1 | 5.8 |
| Methionine | 0.4 | 0.1 | 0.3 | 0.2 | 0.5 |
| Lysine | 4.0 | 3.5 | 3.5 | 2.8 | 3.4 |
| Isoleucine | 2.9 | 2.7 | 2.8 | 2.6 | 2.9 |
| Leucine | 7.1 | 7.3 | 7.6 | 6.3 | 7.9 |
| Phenylalanine | 1.8 | 1.6 | 2.0 | 1.7 | 1.6 |

One of the main changes in amino acid composition among the samples is related to the conversion of cystine (and cysteine) to cysteic acid from original wool to keratoses. Cysteic acid is found in very small amount in original wool where it is formed by the oxidizing effect of solar light on the fleece. Due to the oxidation process for the cleavage of disulfur bonds, the ½ cystine residues are completely converted to the cysteic acid, and there is no present ½ cystine in keratoses. In keratoses, the amino acid composition can also be highlighted a reduction of those amino acids which present easily oxidizable sites (such as tyrosine from 2.5 to 2.2 mole%, lysine from 4.0 to 3.5 mole %, and methionine from 0.4 to 0.1 mole %).

Moreover glutamic acid, aspartic acid, leucine, arginine, which are the amino acids contributing to the α-helix assembling of the LS proteins, were more abundant in keratoses than in original wool, as confirmed by molecular weight distribution where especially low sulfur proteins of intermediate filament are present (see Figure ‎2-2). Only the lysine amount is not in agreement with this behavior. In keratoses, cysteic acid is present in a lower amount that ½ cystine in original wool probably due to the lower amount of cystine in low sulfur proteins extracted by oxidation from cortical cells [37]. Moreover, glycine and tyrosine, mainly found in low molecular weight proteins of the matrix between cuticular and cortical cells, are present in keratoses in a lower amount than in original wool.

Chemical oxidation of keratin disulfide bridge may proceed through both –S–S– and –C–S– scission, but it was shown that reaction occurs largely through the –S–S– cleavage (see Equation ‎2-3- Oxidation of keratin) and, in the presence of excess oxidizing agent, the ultimate products are always two cysteic acid residues, irrespective of the oxidative system [191], [193]:

Equation ‎2-3- Oxidation of keratin

In the keratoses, the increase of oxidized wool mass proves the formation of sulfonic groups [148]. The reaction proceeds through a series of unstable intermediates – partially oxidized cystine, from cystine monoxide to cystine tetroxide [193], according to the schematics in Figure ‎2-3

Figure ‎2-3-Schematics of disulfide bond scission in alkaline oxidative medium

The disulfide bond cleavage is accompanied by peptide chain fragmentation and side amino acid alteration. On the main chain, the oxidative cleavage of the –NH group and the –R–CH– residue may take place, with the generation of new ionizable groups, as given in Equation ‎2-4- The oxidative cleavage of the –NH group and the –R–CH–.

Equation ‎2-4- The oxidative cleavage of the –NH group and the –R–CH–

Amino acid side groups susceptible to oxidation are cysteine (the thiol group is oxidized and forms a disulfide bond –S–S–), methionine, tyrosine, and tryptophan. FTIR and HPLC analysis on oxidized wool keratin in acidic media from different studies confirmed that cysteic acid is the main oxidation product formed from cystine, methionine is converted to methionine sulphoxide, and tyrosine concentration decreases [194].

Isolation of keratin fractions and types for scientific purposes – elucidation of keratin hierarchical organization and biochemical properties – has been a constant preoccupation for scientists. A number of procedures have been reported to isolate hard α-keratins and their related proteins in a minimally denatured state, but most of the laboratory work on cystine involves reduction with thiols such as 2-mercaptoethanol (2-ME), 1,4-dithiothreitol (DTT), thyoglycolic acid (TGA). Basically, the disulfide bridge is symmetrically splitted in two cysteine residues (Equation ‎2-1) while leaving the microstructure almost intact:

Equation ‎2-5- Splitting two cysteine residues

The equilibrium shift is governed by solution pH, nature and concentration of thiols employed, the degree of protein denaturation, temperature and time  [192], [193].

Subsequent blockage of the sensitive –SH groups by nucleophilic displacement, usually by acetylation with iodoacetic acid or iodoacetamide (Equation ‎2-6) prevents disulfide bridges reformation and aggregation [195]:

Equation ‎2-6-nucleophilic displacement of –SH group

Both consumption of –SH groups by acetylation and use of extremely large excess of mercaptan relative to keratin cystine drive the reversible reaction almost to completion; for wool, a neutral thiol such as mercaptoethanol is preferable to thioglycollate as a reducing agent since ionic strength plays an important part in the reactivity and extractability of wool proteins; low pH values are preferred for disulfide-bond reduction since oxidation of thiol groups, peptide-bond splitting and lanthionine formation are minimized; the presence of denaturing/chaotropic agents is mandatory for disaggregation of the keratinous material [196].

The reaction of keratin with sulfites or disulfites involves a nucleophilic attack of sulfite ion on the disulfide bridge, which is asymmetrically split into one equivalent of a Bunte salt, containing the characteristic S-sulfo group, and one equivalent of a thiol:

Equation ‎2-7-Splitting asymmetrically of a Bunte salt

The rate of cystine cleavage with sulfites is optimal in the neutral - weakly basic range [197], [198]. In the specialty literature, the reaction products are called “S-sulfokerateines”.

Applications of this reaction for the regeneration in useful biomaterials must be related to an effective way to promote re-crosslinking and restore the disulfide bridge. Several ways to reconstitute the disulfide crosslink in sulfitolyzed keratin are in use:

a. the use of an appropriate oxidizing agent, which reacts only with the thiol group, to rebuild the disulfide bridges (Equation ‎2-8):

Equation ‎2-8- Rebuliding disulfide bridge

b. the reaction is reversible, and the removal of sulfite determines the reformation of disulfide bridges, but this was difficult to do in practice;

c. the S-sulfo group is labile in alkaline media when the Bunte salt hydrolyzes, and some disulfide linkages are restored;

d. the S-sulfocysteine function is highly reactive towards thiols and is readily reconverted to cysteine group, which reforms the symmetrical keratin –S–S– bridges and not a mixed disulfide [199], [200]. Thus, the disulfide/S-sulfonate groups ratio, which controls properties such as hydrophilicity or mechanical strength, can be regulated by reduction of S-sulfokerateine during processing into different materials [201].

From a practical point of view, the control of the cleavage degree and the final reaction products may be conveniently achieved by oxidative sulfitolysis, which basically proceeds according to Equation ‎2-8, but in the presence of appropriated oxidants and with oxidant: sulfite ratios that provide the reiteration of the reduction-oxidation cycle, until almost all sulfhydryl groups are converted to S-sulfocysteine. The process is usually conducted in the presence of thionates or alkaline cupric ions, as oxidizing agents.

Sulfitolysis of feather keratin using the Na2SO3: Na2S4O6 couple was first reported by Bailey and Cole (1959) [35]. The reaction mechanism is not entirely understood, but it is believed that the oxidizing agent is the trithionate, which forms as intermediate irrespective of the used thionate, following the proposed reactions (Equation ‎2-9), where n is an integer from 4 to 6 [202]:

Equation ‎2-9- Sulfitolysis reaction

The sulfite: thionate ratio controls the proportion of stable –S–SO3¯ groups in the solubilized keratin. For example at pH =7, an ammonium bisulfite: sodium tetrathionate molar ratio of 2.5: 1 determined a maximum sulfitolysis degree of 90 %, which corresponds to the “highly S-sulfonated kerateines”. The presence of denaturing agents is mandatory, as they play the same role as in reductive solubilization.

Solutions of cuprammonium/sulfite at pH 9-10.6 can dissolve large amounts of keratin in the absence of denaturing agents, with the cupric ion acting as a catalyst for oxidation with air oxygen [203]; the sole product of both cysteine and cystine is S-sulphocysteine (Eq. 9), which provides high rates of sulfonation [204].

Equation ‎2-10- Dissolving with cuprammonium/sulfite at pH 9-10.6

The process rate is prolonged, and the copper ion, which is tightly bound to the protein substrate [205] must be entirely removed prior to the use of keratin product for any subsequent application. Kelly et al. (2006) [206] patented a two-stage process for the obtaining of high molecular weight soluble S-sulfonated keratin forms, by oxidative sulfitolysis with sodium sulfite and cuprammonium hydroxide, without the use of chaotropic agents. Two intact protein fractions were isolated: the S-sulfonated keratin intermediate filament protein, having a MW distribution predominantly in the range 30-60 kDa, and the S-sulfonated keratin high sulfur protein having a MW predominantly in the range of 15-25 kDa. The process is economically and environmentally acceptable but is intricate and time-consuming.

Oxidative sulfitolysis introduces a S-sulfo functional group with solubilizing properties comparable to those of the sulfonic group, without the destruction of certain amino acid side chains that accompanies oxidation by peracids. The hydrophilic and ionizable S-sulfo groups preserve functionality and amenability to re-crosslinking, and the hydrophobic/hydrophilic character of the S-sulfokerateine can be easily controlled by the disulfide/S-sulfo group ratio. The SDS-PAGE electrophoretic pattern of S-sulfokerateine powder shows two higher MW bands at 45- 60 kDa related to the low sulfur keratin from microfibrils, and a low MW bands between 20-9 kDa, related to the high sulfur keratin from the matrix. FTIR spectra of sulfitolyzed keratin from wool showed the prevalence of α-helix secondary structures and random coil disordered portions, which explain the solubility of the regenerated keratin, while the reduced keratin showed the prevalence of β-sheet structures  [112]  .

Other differences in amino acid composition are found between original wool and hydrolyzed sample. In the hydrolyzed sample, the amount of ½ cystine was very low compared to the original wool. Most of the cystine was destroyed because of the temperature of the process [48] and only a very small amount of cysteic acid, characteristic of undamaged wool, was found. The loss of cystine associates with the thermal treatment and the cleavage of -S-S- bonds bring to the formation of lanthionine (2.3 mole%) through the formation of dehydroalanine and free sulfidryl groups. Dehydroalanine and the free sulfidryl group of cysteine can further react to form the irreversible cross-link -S- of lanthionine. H2S is also produced from the degradation of cystine. In addition, small changes detected in the amount of the other amino acids in the hydrolyzed sample can be correlated with their thermal stability and secondary with their solubility in water. Moreover, breaking of disulfide bonds as a result of cystine destruction combined with the breaking of peptide bonds shown by electrophoresis (see Figure SDS Page) caused a considerable amount of peptides and free amino acids to be dissolved in water.

Keratin hydrolysis determines the disaggregation of the protein structures at all hierarchical levels, which implies splitting of both amide (–CO–NH–) and disulfide (–S–S–) bonds. Molecular weights of the hydrolysis products cover a wide range, depending on the specific hydrolytic conditions; in severe conditions, the peptide backbone can be entirely broken down into the constitutive amino acids. Hydrolysis can be conducted in alkaline, acid, enzyme-aided or even neutral media, under hydrothermal effect.

Alkaline hydrolysis has been extensively used because of its high efficiency at large scale and low costs. Common alkali used for keratin hydrolysis are NaOH, KOH, and Ca(OH)2, but Sr(OH)2 also proved to be effective in practical applications [207]. The disulfide bridges are split by hydrolysis in strong alkali (–S–S– cleavage), or by β-elimination in dilute alkali (–C–S– cleavage), as given in Equation ‎2-11 [208]:

Equation ‎2-11- Splitting disulfide bridge by hydrolysis

The dehydroalanine reacts with a cysteine function to form the thioetheric lanthionine bridge Ker–CH2–S–CH2–Ker or with a lysine residue, to form a lysinoalanine bridge Ker–(CH2)2–CO–NH–(CH2)4–Ker. The new cross-links are favored by dilute alkali media and are very resistant to subsequent reductive attack. Unlike the pristine protein, the aminoacid composition of the hydrolyzed keratin is rich in methionine, lysine and glutamic acid, and poor in threonine, serine, cystine and arginine

Part of the helical segments suffers reorganization and part of the originally amorphous matrix, in which most of the disulfide bonds are located, refolds.

In wool, acid hydrolysis of peptide bond occurs at pH values lower than 2. Severe conditions, such as 6 M HCl at 110°C for 24 h converts wool completely to its constituent amino acids and this is why acid hydrolysis is currently used in protein analysis, for the determination of the primary structure. Tryptophan is destroyed by this procedure, while cystine, serine, and threonine are partially degraded. Peptide bonds on both sides of aspartic, glutamic and cysteic acid residues are more sensitive to hydrolysis than other peptide bonds. The acid hydrolysis of asparagine and glutamine residues to aspartic and glutamic acid residues is faster than the hydrolysis of peptide bonds [209]. Treatment in 4M HCl at 95°C for 24 h determines a hydrolysis degree of no more than 33 % and extensive splitting of disulfide bonds, with the formation of sulfhydryl and sulfate oxide groups; α-helix and β-sheet structures are still present, but compared with the alkaline hydrolysis, the amorphous polypeptides are predominant. The resulting keratin polypeptides exhibit nontoxicity and biocompatibility and can find applications as biomaterials for wound healing or drug delivery [100].

No significant changes were found between the amino acid composition of kerateine and sulfo- kerateine compared with original wool.

### FT-IR Spectroscopy

Figure ‎2-4 shows the infrared spectra of all extracted samples compared with the original wool spectrum.

The Infrared absorption spectra of all samples show characteristic absorption bands attributed to the peptide bonds (−CONH−). The vibration in the peptide bonds originate bands known as amide A, amide I, amide II, and amide III. The amide A band at 3282 cm-1 is connected with the stretching vibration of the N−H bond. Amide I, which is related mainly to the (C=O) stretching vibration, has an intense peak at 1630 cm-1. Amide II, which is related to the N−H band, has a peak at 1515 cm-1, while the amide III band at 1230 cm-1 is referred to the  in-phase combination of C−N stretching and N−H in-plane bending, with some attributed of C−C stretching and C=O bending vibrations [210].

Peaks that appear between 1200 and 1000 cm-1 are attributed to the S−O vibration (see Figure ‎2-4). In particular, these peaks are present in the spectra of keratoses and sulfo-kerateine in comparison with original wool. The absorption bands at 1174 cm-1 and 1040 cm-1 in the keratoses spectra are related to the asymmetrical and symmetrical S−O vibrations of sulfonate (SO3⁻) in cysteic acid [211]. Because of the complete oxidation of cystine to cysteic acid during the oxidation process to obtain keratoses, these two vibration bands appeared in the keratoses sample; while the absorptions bands of cystine monoxide (-S-SO-) and cystine dioxide (–S–SO2–) at 1078 cm-1 and 1120 cm-1 respectively, which are intermediate products in oxidation of cystine to cysteic acid, are nearly not present in keratoses.

In the sulfo-kerateine spectrum, two absorption bands are clearly visible at 1022 cm-1 and 1095 cm-1 assigned to the sulfur-oxygen vibration of sulfonate in the cysteine sulfonic acid (-S-SO3- Bunte salts).

Figure ‎2-4 Fourier transform infrared spectra of (a) wool, (b) keratoses, (c) kerateine, (d) sulfo-kerateine, (e) hydrolyzed keratin.

In previous studies, FTIR spectroscopy applied to examine secondary structure of keratin extracted from wool by severe alkaline hydrolysis (2% NaOH, for 3h, at 62 - 65°C) confirmed the macromolecule reorganization with alteration of the α-helix / β-sheet / disordered regions ratio (25.7% / 51.8% / 22.5%).

In the spectra of kerateine and hydrolyzed keratin, no evident differences were found in comparison with original wool spectrum.

### NIR Spectroscopy

Figure ‎2-5 shows the FT-NIR spectra of extracted samples compared with the original wool spectrum.

The absorption bands in the near infrared region (between 10,000 and 3700 cm-1) are the result of overtones and combinations originating in the fundamental mid-range infrared region of the spectrum. The bonds involved are generally C–H, N–H, O–H, etc.. Before NIR analysis, all the samples were previously stored for 24 h in a standard atmosphere (20 °C, 65% RH) in order to normalize the water amount.

The shoulder at 7000 cm-1 is related to the first overtone of O–H stretching vibration of water and the band at 5200 cm-1 is assigned to a combination of the O–H stretch and H–O–H bending vibration of the hydroxyl group from the water. The doublet at 5800 cm-1 is an overtone of the C–H stretch of protein side chains and lipids. The bands between 5000 cm-1 and 4000 cm-1 are attributed to the characteristic molecular conformation and amino acid composition of the keratin samples. In details, the bands between 5000 and 4500 cm-1 are related to the secondary structure of the proteins, and the bands from 4500 to 4000 cm -1 are mainly attributed to the nature of the protein side chains [3].

Figure ‎2-5-Near infrared spectra of (a) wool, (b) keratoses, (c) kerateine, (d) sulfo-kerateine, (e) hydrolyzed keratin.

By comparing spectral absorption of all samples, as can be seen, there are small differences in the achieved spectra, which are related to the hydration state of the samples (shoulder at 7000 cm-1 and bond at 5200 cm-1) [212].

Moreover, the second derivate spectra of wool and extracted keratin were compared (see Figure 5). The band at 4525 cm-1, which seems to be associated with the β-sheet structure, is similar and very low in all samples. Significant differences are visible in the region between 4500 to 4000 cm -1 that is considered to reflect the amino acid composition of samples [213].

Figure ‎2-6-Second derivative near infrared spectra of (a) wool, (b) keratoses, (c) kerateine, (d) sulfo-kerateine, (e) hydrolyzed keratin.

### Thermal behavior

In Figure ‎2-7, the DSC thermograms of wool extracted or hydrolyzed in different ways are shown and compared with original wool. In each thermogram, the first endotherm peak below 100 °C due to water evaporation is followed by peaks related to protein denaturation.

Figure ‎2-7-Differential scanning calorimetry curves of (a) wool, (b) keratoses, (c) kerateine, (d) sulfo-kerateine, (e) hydrolyzed keratin.

In original wool, the α-helix denaturation of cortical cells takes place at about 230 °C with a peak that includes the denaturation of α-helical crystalline material in the domain of both ortho and para cortical cells [214].

The analytical traces of extracted keratin are very different, both for the temperature and for the form of denaturation peaks. The thermogram of hydrolyzed wool does not show typical denaturation or degradation temperatures, such as keratoses or sulfo-kerateine traces, but broad peaks in a wide range at lower temperatures indicating that the thermal stability of hydrolyzed keratin is reduced with respect to keratoses or sulfo-kerateine. Similar results were obtained by Fortunati et al. comparing enzyme hydrolyzed keratin with sulfo-kerateine extracted from merino wool and brown alpaca fibers [113]. Also, kerateine, characterized by the re-oxidation of disulfur bonds from thiols, shows that peaks not well defined peaks in a broad temperature range.

The hydrogen and ionic bonds in sulfo-kerateine and keratoses proteins make them degrade at the precise temperatures with well-defined melting peaks, at about 240 °C for sulfo-kerateine and more than 300 °C for keratoses.

The higher thermal stability of keratoses and the lower thermal stability of hydrolyzed wool are confirmed by thermogravimetric analysis (see Figure ‎2-8).

Figure ‎2-8-Thermogravimetric analysis of extracted keratins.

## Conclusions

Keratin from wool ﬁbers was extracted by oxidation, reduction, sulﬁtolysis, and superheated water hydrolysis, and the diﬀerent extracts obtained were compared. Although extraction yields are quite similar, evident diﬀerences can be noticed in the time, cost, and environmental sustainability of the extraction methods. Among the selected extraction agents, sodium metabisulﬁte, used for sulﬁtolysis, seems to be the cheapest and least harmful agent in comparison with peracetic acid and dithiothreitol, utilized for oxidative and reductive extraction, respectively, being similar to the molecular weights of the products obtained. Superheated water hydrolysis highly decreases the molecular weight of the peptides obtained, with loss of the most temperature sensitive amino acids, but it is a cheap and environmentally friendly method, easy to implement on a large scale.

Although extracted keratins via oxidation, reduction, and sulﬁtolysis can be used in highly technological ﬁelds, such as the biomedical sector for scaﬀold production or the ﬁltration sector, where the mechanical characteristics of the proposed materials are also to be tailored, the hydrolysis of keratin represents one of the most promising ways to extend the practical application of keratin in the agricultural, animal feed, or cosmetic ﬁelds. Other characteristics, such as solubility, the presence of polar groups (e.g., the cysteic acid in keratoses), reformation of the disulfur bond capacity, can be considered to use keratin itself extracted in diﬀerent ways or extracted keratin in a blend with other polymers, for tailoring speciﬁc material characteristics.

# Chapter 3

# Film and microcapsule

## The aim of this part

The purpose of this chapter is the production of keratin-based microcapsules and film, following by physicochemical characteristic of produced microcapsule and film with perspective bio-application.

## Preliminary discussion

Numerous methods of microcapsule preparation have been investigated, which include solvent extraction, spray-drying, interfacial polymerization with emulsions and microemulsions, coacervation/precipitation, organic phase separation, emulsion cross-linking, ionic gelation, etc. [110], [122], [123], [215]–[218]. Among these methods, the sonication technique is considered as a proper approach to producing biocompatible protein microcapsules for those materials having the potential for employing this approach for fabricating microcapsules. The advantage of this method is that desired targeting material can be readily loaded into protein [132].

The shell part of the microcapsules is an essential compound for final products properties. For each application, the material utilized as the shell part functioning differently. Keratin, one of the type of proteins utilized, is a proper material for employing in bio-fields. Keratin can be extracted via different methods, and the final products of each keratin extraction process will have different characteristics. In the current study, water-soluble keratins obtained via oxidizing extraction of wool, known as keratoses, was successfully used for the encapsulation of hydrophilic molecules, using an easy detectable blue dye. The encapsulation process was carried out via sonication [37], [110], [161], [187], [219]–[221].

This correlation was described by the theory of Kolmogoroff, expressed in the following way:

Equation ‎3-1-Effect of different factors on Microcapsules

where dmax is the biggest drop size which can exist under turbulence, D is the diameter of the agitator (m), is the density of the continuous phase (kg/m3), N is the agitation rate (turns/s), σ is the interfacial tension between the dispersed phase and the continuous phase (N/m) and c1 is a constant. The value of the constant  is experimentally determined, and its value is affected by factors linked to the agitation conditions.

As it mentioned in pervious chapter, keratoses do not participate in cross-linking reactions and are susceptible to hydrolytic degradation. Keratoses degrade relatively fast in vivo and have higher molecular weight in comparison to other types of keratin. Due to their non-toxicity, biocompatibility, biodegradability and non-immunogenicity, keratoses are highly promising candidates for encapsulation of chemicals for cosmetic, pharmaceutical and biomedical fields [42], [120], [222]–[226].

Keratoses are produced as hydratable powders, which can be turned into viscoelastic hydrogels that support cell adhesion and proliferation [110], and may be useful as biocompatible fillers for implant applications [109], or matrix for peripheral nerve regeneration [95]. Hydrophilicity and gel strength can be controlled by combined oxidation-reduction treatment [227]. Wool-derived oxidized keratin has shown stimulatory effects on wound repair, as it promoted keratinocyte migration and induced production of basement membrane proteins [137]. Sterile keratose-based kits for wound and burn healing have been patented [138]. Oxidized keratin derivatives show good blood and cardiovascular compatibility and can induce vasodilation [139], or promote angiogenesis [140]. Due to the affinity of cysteic acid residues for soluble charged species, keratose can find environmental applications as adsorbents for heavy metals [141]. Cosmetic uses are mainly related to hair treatment commercial products.

The previous study about keratin microcapsules indicates that keratin capsules were stable in boiling water and different organic solvent and less leaky than myoglobin and BSA capsules. Although, subjected fragmentation might lose their shape under heating in a dilute aqueous solution of mercaptanol [228].

On the other part of this section blend films were prepared at different PVA/KOx ratios and investigated with Scanning Electron Microscopy, Fourier Transform Infrared Spectroscopy, Differential Scanning Calorimetry and tensile measurement for collecting knowledge for further processing and applications.

## Materials and methods for producing microcapsules

Keratoses were obtained via oxidizing extraction from pristine wool, 21 µm mean fiber diameter, in the form of top (the fiber sliver submitted to industrial scouring, carding, and combing) supplied by The Woolmark Co., Italy. The hydrophilic dye used to fill the microcapsules was Telon Blue BRL (N-aminophenylacetamide) from Dystar. Peracetic acid (36-40% wt. in acetic acid) and Tris(hydroxymethyl)aminomethane (≥ 99.9 %) used for the oxidizing extraction, and toluene (anhydrous 99.8%), utilized for the microencapsulation process, were purchased from Sigma-Aldrich®.

### Keratoses oxidizing extractions

Keratin was extracted via oxidizing extraction from pristine wool described in the previous chapter. Briefly, Extraction was carried out with peracetic acid (36-40% wt. in acetic acid) and Tris (hydroxymethyl)aminomethane (≥ 99.9 %)  following the method used by L. Burnett and S.A. Boyd [229]. Wool fibers, previously cleaned by Soxhlet extraction with petroleum ether, were immersed in peracetic acid at 2% w/v and left in a thermostatic water bath for 24 hours at 25 °C. Further, the fibers were washed to remove unreacted peracetic acid, dried at 90 °C and vigorously shaken in TRIS 1 M (121.14 g/l) at 37 °C for 2 h. The resulting solution of keratoses was filtered with a 120 mesh sieve, neutralized with hydrochloric acid and dialyzed for 48 h against fresh water, fed by a peristaltic pump to accelerate the osmosis process. At the end of the dialysis, the solution was centrifuged to remove insoluble keratin particles, frozen and lyophilized.

The hydrophilic dye used to fill the microcapsules was Telon Blue BRL (N-aminophenylacetamide) from Dystar.

Toluene (anhydrous 99.8%) from Sigma-Aldrich was used as the non-polar solvent to promote formation and emulsification of the keratoses microcapsules.

### Preparation of microcapsules

The procedure of encapsulation was performed following the method used by K. Yamauchi, A. Khoda [228]. An aqueous solution of keratoses 1.8% wt. concentration was added with 0.09 mg/ml hydrophilic dye. After complete dissolution, toluene was added in the proportion 1:0.5 v/v. Toluene (anhydrous 99.8%) was used as the non-polar solvent to promote formation and emulsification of the keratoses microcapsules. The solution (25 ml) was sonicated for 3 min with a Sonics Vibracell 750 (Cole Parmer) sonicator equipped with a stainless steel ½ inch “solid” probe. Power was adjusted to 150 W at the frequency 20 kHz at room temperature, leaving the solution under constant stirring with a magnetic plate. The resulting foamy emulsion was centrifuged for 15 min at 12000 rpm, in order to separate the foamy phase from the solvents that didn’t take part in the formation of microcapsules. Centrifugation originated a triple stratification with toluene on the top, the foam containing the microcapsules in the middle and the aqueous solution containing the residual keratoses and the dye not embedded in the microcapsules on the bottom.

### Measurement and characterization methods

The microscopic investigation was carried on microcapsules out with a DM-L Light Microscope (Leica) in the Transmitted Light mode. The specimens were prepared to mount some drops of emulsion on glass microscope slides; in some cases, the microcapsule emulsion was diluted with water for a better investigation.

Scanning Electron Microscopic (SEM) analysis was carried out on microcapsules with a LEO 435 VP SEM (Leica Electron Optics) at 15 kV, 30 mm working distance. Aluminum specimen stubs were used to mount the samples using a double-sided adhesive tape. Samples were sputter-coated with 20 nm thick gold layer in rarefied argon, with a K 550 Sputter Coater (Emitech) at 20 mA for 180 s.

Morphological and surface investigations were carried out on microcapsules with a Nano-R2 Atomic Force Microscope (Pacific Nanotechnology) and were evaluated from 4 µm images. The AFM imaging technique was the “Close Contact” mode with highly doped single crystal silicon probes (APPNANO) of 125 µm nominal length. Data were acquired by means of the SPM Cockpit Software, processed and analyzed by the Nanorule+ software, both equipped with the Nano-R2 system.

The microcapsules production yield was determined by difference with the amount of keratoses still remaining in the water solution (not belonging to the microcapsule) by an UV-vis spectrophotometer Lambda 40 (Perkin Elmer).

Thermal properties of keratoses and microcapsules were investigated by a Differential Scanning Calorimeter DSC 821 (Mettler Toledo), calibrated by an indium standard. A small amount of dried microcapsules were introduced inside an Al crucible and the analyses were performed at 10 °C/min heating rate, in the range 25-500 °C, flushing the calorimeter cell with 100 ml/min nitrogen.

## Result and discussion

When the biphasic solution of keratoses and toluene is vigorously agitated by sonication, the long and hydrophilic chains of keratoses came into contact with the toluene repulsing it and rolling up, resulting in spheres. During the process, the dye is entrapped in.

In order to detect the presence of hydrophilic dye inside the keratoses microcapsules, the foamy emulsion isolated from the solvents was analyzed by Transmitted Light Microscopy.

Figure ‎3-1 shows the images of the keratoses microcapsules at 200 (a) and 400 (b) magnification, after dilution in water. Microcapsules presented a varied range of size distribution, with diameters of few micrometers, influenced by many parameters including sonication power, time, and agitation speed [128], [230]–[232].

| (a) |  |
| --- | --- |
| (b) |  |

Figure ‎3-1– Transmitted Light Microscope images of keratoses microcapsules 200x (a) and 400x (b) after dilution with water.

At this observation, microcapsules have no sign of collapses or rupture due to no preparation of inspection process. Agitation during the development processes had a significant effect on the average microsphere diameter.

A smaller size of microsphere diameter, on average, was detected while the agitation power was increased–which can be considered as the most essential factor on microcapsules sizes.

SEM observation evidenced the ultrastructure, morphology and size distribution of the keratoses microcapsules.

Drops of the microcapsules emulsion were mounted directly on the specimen stubs surface and introduced in the sputter coater without previous drying to avoid the fracture of the shells. In this way, evaporation of the solvents occurred under high vacuum. Those deformations in the structure, as shown in Figure ‎3-2 (a), can be explained by that high vacuum preparation which leads to destroying a major proportion of the microcapsules.

SEM images presented in Figure ‎3-2 evidenced the presence of round-shaped vesicles (the keratoses microcapsules) with a wide range of size distribution, which also confirms the findings of the light microscopy investigations as stated previously. The diameters of the microcapsules were found to be in between 0.5 and 4 µm.

| (a) | (b) |
| --- | --- |

Figure ‎3-2- SEM images of keratoses microcapsules 1500x (a) and 3000x (b).

Figure ‎3-3 reports AFM images of the keratoses microcapsules after treatment under high vacuum to remove the solvents. The diameters of microcapsules were obtained in the range 0.3 - 1 µm with a rough surface. Furthermore, the SEM results reveal a wide size distribution of the microcapsules, which is similar to that of the results obtained from transmitted light microscopy tests.

Figure ‎3-3- AFM images of microcapsules

The microcapsule yield was determined by UV-vis spectrometry measuring the residual amount of keratoses and dye still found in the aqueous solution separated by centrifugation.

An aliquot of the balk solution was taken from the suspension to measure the UV absorbency. Absorbance was measured at the maximum peak corresponding to 215.1 nm for keratoses (UV field) and 607.8 nm for Telon Blue (visible field). The Figure ‎3-4 shows the calibration curve of Telon Blue, which is used for measuring the amount of Telon Blue inside microcapsule. Also, the Figure ‎3-5 presents the calibration curve of keratoses, which is utilized for measuring microcapsules efficiency.

Figure ‎3-4- Calibration Curve Telon Blue

The yield of microcapsules corresponded to 28.87 ± 3%.

Figure ‎3-5-Calibration Curve of Keratoses

The UV analysis was used to calculate the encapsulation yield of the dye, using the following equation:

Dye encapsulation yield%=dye encapsulated (g) initial amount of dye (g) ×100

where the initial amount of dye was the quantity of dye used in the encapsulation process, and the dye encapsulated was obtained by subtracting the quantity of dye remained in the solution from the initial amount of dye. The dye encapsulation yield was found to be 83.62±5 %.

The DSC thermograms, reported in Figure ‎3-6, show three main endothermic events in the thermal behavior of both, i.e., the keratoses and the microcapsules dried in vacuum. The peaks corresponding to water evaporation fell in the range 65-70°C for both samples. The denaturation peaks were found to be very close  (225°C for the keratoses and 233°C for microcapsules), while the degradation peak of microcapsules broadened and shifted to lower temperatures (297°C against 314 °C), probably because of interactions between keratoses and the dye inside the capsules.

Figure ‎3-6-DSC thermograms of keratoses and keratoses microcapsules

## Materials and methods for producing blend film

KOx were obtained via oxidizing extraction from pristine wool, 21 m mean fiber diameter, in the form of top (the fiber sliver submitted to industrial scouring, carding and combing),that was  supplied by The Woolmark Co., Italy.

PVA fibers were supplied from Citterio S.P.A. - Monza, Italy.

All the other reagents were purchased from Sigma-Aldrich®, unless otherwise specified.

### Preparation of PVA/KOx blend films

PVA fibers were cleaned by Soxhlet extraction using petroleum ether, washed with distilled water and conditioned at 20 °C, 65% r.h. for 24 h. PVA/KOx  solutions were obtained by dissolving KOx and PVA (5% w/w) in water as a common solvent. The pure solutions of PVA and KOx were mixed in different proportions (0/100, 10/90, 30/70, 50/50, 70/30, 90/10, 100/0 w/w PVA/KOx) under stirring at 65°C for 1h and cast on polyester plates at room temperature overnight to obtain regenerated PVA/KOx blend films.

## Blend film characterization

Blend film charactization has been carried out with different assays.

### Morphological structure

Blend films were successfully obtained at all PVA/KOx ratio except for films with a KOx amount of 100% and 90 % because at this KOx amount, films became fragile and hard to peel from the cast. The films are visually transparent especially those with higher PVA amount and as the KOx content increased the film's color tend to brownish (see Figure ‎3-7). The surface of the films of 100/0, 90/10, 70/30, 50/50, and 70/30 PVA/KOx look quite smooth, but with 100/0 PVA/KOx, the surface appearance becomes rigid. The morphology of the films are more irregular with increasing of the keratoses amount. As it shown in figure 2 the structure of the film becomes fragile with decreasing the PVA amount that in 0% and 10% PVA, producing the film is not possible and also film with this amount of PVA hardly peeled from the casts.

Figure ‎3-7-Visual appearance of PVA/KOx films. (1)100/0 PVA/KOx - (2) 90/10 PVA/KOx - (3) 70/30 PVA/KOx- (4) 50/50 PVA/KOx- (5) 30/70 PVA/KOx - (6) 10/90 PVA/KOx- (7) 0/100 PVA/KOx

Microscopic morphology was examined by SEM (see Figure ‎3-8). The SEM images show that the films have a dense and continuous structure, and in 100/0, 90/10, and 70/30 PVA/KOx void were not found in entire structures and the films show good structural integrity in total shape, and the phase separation does not appear in any blended film among these three samples. As the amount of keratoses increased (50/50, 30/70, and 10/90 PVA/KOx), the smoothness of the blend films become rough and fluctuating, with some fracture structure revealed with a higher amount of keratoses ratio. This suggests that the presence of keratoses probably effect on the crystallization of blended film and higher amount of keratoses causes phase separation and aggregation of each polymer in matrix. This phase separation also occurs in other study with similar two polymers without using cross-linker [146].

Figure ‎3-8-SEM pictures of PVA/KOx films. (1)100/0 PVA/KOx - (2) 90/10 PVA/KOx - (3) 70/30 PVA/KOx- (4) 50/50 PVA/KOx- (5) 30/70 PVA/KOx - (6) 10/90 PVA/KOx- (7) 0/100 PVA/KOx

The film thickness decreases by increasing the amount of keratoses in the blends from 0% to 30%. As the amount of keratoses increased, the thickness of the films increase.

Table ‎3-1- Thickness of blended films

| Film | Thickness |
| --- | --- |
| 100/0 PVA/KOx | 97.54 |
| 90/10 PVA/KOx | 64.99 |
| 70/30 PVA/KOx | 46.90 |
| 50/50 PVA/KOx | 53.97 |
| 30/70 PVA/KOx | 55.71 |

### Thermal analysis

Figure 4 shows the DSC traces recorded for the heating scan in the range 50 to 400 °C. In the blend films containing PVA/KOx, the curves display two main endothermic peaks. The first peak around 80 °C is related to the moisture evaporation and may be glass transition [233]. The endothermic peaks observed at 212 °C are related to the melting point of the PVA crystalline phase in the blend films which the peak become fading with decreasing of PVA amount and with increasing content of keratoses this peak shows the same temperature with all keratoses amount indicating there is no effect of keratoses on PVA crystallite structure.

From DSC with curves of 0/100 PVA/KOx, the peak at 295 °C was observed, indicating decomposition of keratoses and this decomposition did not appear in 100% PVA/0% keratoses. As the content of PVA increase, the decomposing and depolymerization peak was shifted to 300 °C, suggesting slightly higher stability of blend film than pure keratoses. As the keratoses contain different amino acids with hydrogen bonds, the melting energy in blend film causes increasing of the Tm in blend films. Basically, bending two mentioned macromolecule has no significant consequence on thermal properties.

Figure ‎3-9-DSC curves of blend films with different ratios PVA/KOx.

### FTIR analysis

Figure ‎3-10 shows the infrared spectra of all blend samples. The investigation of the keratoses films illustrates the typical bending and stretching vibration keratoses containing amino acid. In detail, the blend samples containing keratoses, there is a characteristic absorption which is related to the peptide bonds (−CONH−). The amide A has vibration at 3282 cm-1 in the peptide bonds connected with the stretching vibration of N−H bond. The amide I is related mainly to the (C=O) stretching vibration having an intense peak at 1630 cm-1. The amide II which is attributed to the N−H band has a peak at 1515 cm-1, and the amide III band at 1230 cm-1 is related to the in phase combination of C−N stretching and N−H in plane bending, with some attribution of C−C stretching and C=O bending vibration. The absorption bands at 1174 cm-1 and 1040 cm-1 in the keratoses spectra are related to the asymmetrical and symmetrical S−O vibrations of sulfonate (SO3-) in cysteic acid [211].

As it can seen, the location of the main characteristic absorption peaks in keratoses  remains in blend films.  With adding and increasing of PVA in keratoses film, the absorption peak at 2940 cm-1 appeared and broanded, this because this peak is related –H stretching and bending vibration of PVA [234].

The peaks present in blend film containing PVA are mainly related to the hydroxyl and acetate groups. The bands in 3270 cm-1 are attributed to the stretching O−H from the intermolecular and intramolecular hydrogen bonds. The other close vibrational bands are at 2840 and 2940 cm-1 and are related to the stretching C−H form alkyl groups. Moreover, O–H plane bending motion is coupled with the other molecular motions that involve frequencies in the range 600-1500 cm-1.

Figure ‎3-10-FTIR spectra of blended films of PVA/KOx with different ratios.

The bands at 1700 cm-1 are related to absorption of the C=O and C−O from residual acetate groups attributed to the producing PVA from hydrolysis of polyvinyl acetate. The intensity of the absorbtion band at 1144 cm-1 is related to the crystallinity degree of PVA. The presence of this band indicates that in blend films PVA maintains a certain degree of crystallinity as confirmed by the presence of melting peak in DSC curves.  With increasing PVA amount, new absorption bonds emerged at about 1330 cm-1 attributed to the CH−OH bending vibration of PVA.  With increasing PVA, in PVA/KOx blend films ,the absorption peak at 2940 cm-1 appeared and broaded, because this peak is related –H stretching and bending vibration of PVA [234]. In blend PVA/KOx films it seems that both PVA and KOx peaks are present or overlapped indicating no covalent interaction between the two components in the blend.

### Mechanical properties

The tensile strength and the modulus of cast films increase as increasing the amount of KOx in the blend until respectively 30% and 50% w/w. In blend film containing 70% of KOx these parameters decrease sharply. On the other hand PVA cast film elongation at break decreases by adding KOx in the blend films. The similar result had been reported by other studies. Dou et al. indicated that, without a crosslinking agent, the increase of PVA content causes both tensile strength and elongation to increase, proposing high probably the hydrogen bonds between keratin and PVA were generated in blend film structure. Also, it suggested that the improved mechanical properties of keratin and PVA blend film possibly caused by the increase of crystallinity of blend film because of increased crystallizable PVA[234]. However, in the gelatin, the other protein-based material, gelatin/PVA blend film revealed that increasing PVA concertation causes decrease of the tensile strength of blend film [235]. Figure ‎3-11 shows the tensile behavior of 5 blended, in terms of relative stress and strain.

Figure ‎3-11- The stress-strain properties of different KOX/PVA blend films

The mechanical properties of the obtained film are summarized inTable ‎3-2-Tensile strength, elongation at break and modulus of PVA/KOx blend films. The blend films of 10/90 and 0/100 PVA/KOx are too fragile for film fabrication.

Table ‎3-2-Tensile strength, elongation at break and modulus of PVA/KOx blend films.

| PVA/KOx | Tensile strengh (MPa) | Elongation at break (%) | Modulus at 0.5 mm elongation (MPa) |
| --- | --- | --- | --- |
| 100/0 | 18.1 | 148 | 2.1 |
| 90/10 | 21.4 | 80 | 3.7 |
| 70/30 | 24.7 | 37 | 10.7 |
| 50/50 | 23.1 | 6 | 16.4 |
| 30/70 | 5 | 9 | 5 |

## Conclusion

In this study, we have demonstrated the encapsulations of hydrophilic molecules into keratoses microcapsules using a sonication process. The keratoses were prepared via oxidizing an extraction of wool keratin and then analyzed by FTIR, HPLC, and SDS-PAGE. The results from SDS-PAGE shows that the molecular weights of the keratoses lie in the range of 38-62 kDa, and FTIR and  HPLC results confirm the suitability of extracted keratoses to use via sonication method for the fabrication of microcapsule shells. Resultant microcapsules validate that Telon Blue BRL dye (N-aminophenylacetamide) has been entrapped as a core part and that the keratoses have a suitable structure to be a shell part of the microcapsules. The size of fabricated microcapsules was determined between 0.5 and 4 µm, and the dye encapsulation yield shows that the majority of the dye became entrapped inside keratoses microcapsules. Consequently, keratoses microcapsules can be a valuable and promising carrier for different applications, due to their level of biodegradability and high encapsulation rate.

# Chapter 4

# Conclusions

With unique properties of biodegradability, biocompatibility, non-toxicity, cross-linking and self-assembling ability, keratin is a versatile biopolymer that can be modified and developed in various forms, which can find applications in different fields, from agriculture to cosmetics and regenerative medicine. In this study, keratins have been extracted from keratinous sources with different methods. Chemical methods can obtain different kinds of solubilizates with distinctive characteristics. The properties of obtained keratins significantly are related to the extraction procedure. Choosing the appropriate process for obtaining keratin based on final requirements needs to be considered. The oxidation, reduction, and sulfitolysis are the pathways which consider it as a benchmark with least damaging of disulfide bonds. In particular, in oxidation method, the amount of cystiene has been increased and different keratin fraction can be obtained. The production yield of each method shows almost the same amount.

Chemical pathways for keratin solubilization are not always convenient from a technological, economical or environmental point of view. Within the contemporary ecological development context, emerging biotechnological methods employing keratinolytic microorganisms or chemically-free alternatives start to play a key role in processing keratinous waste and resources.

Development of feasible pathways to create value-added materials and applications starting from materials with high potentials, such as keratin wastes and by-product, is a contribution to environmental sustainability and progress of different economical and social fields. Moreover, keratins are biodegradable and biocompatible and have potential to used in control release process. Further research is needed to take advantage of the keratin biopolymer potential fully.

This thesis reported the variety of keratin biomaterial and emphasized the properties of each keratin material. Particularly, keratin materials have different specific structure that makes it possible to apply in various particular tailored biomaterial by designing and modification of the structure and choosing proper extraction way.

# References

[1]	A. Gousterova et al., “Alkaline hydrolysate of waste sheep wool aimed as fertilizer,” Biotechnol. Biotechnol. Equip., vol. 17, no. 2, pp. 140–145, 2003.

[2]	A. A. Onifade, N. A. Al-Sane, A. A. Al-Musallam, and S. Al-Zarban, “A review: potentials for biotechnological applications of keratin-degrading microorganisms and their enzymes for nutritional improvement of feathers and other keratins as livestock feed resources,” Bioresour. Technol., vol. 66, no. 1, pp. 1–11, 1998.

[3]	M. Zoccola, A. Aluigi, and C. Tonin, “Characterisation of keratin biomass from butchery and wool industry wastes,” J. Mol. Struct., vol. 938, no. 1, pp. 35–40, 2009.

[4]	J. Glowacki and S. Mizuno, “Collagen scaffolds for tissue engineering,” Biopolymers, vol. 89, no. 5, pp. 338–344, 2008.

[5]	A. González, M. C. Strumia, and C. I. A. Igarzabal, “Cross-linked soy protein as material for biodegradable films: Synthesis, characterization and biodegradation,” J. Food Eng., vol. 106, no. 4, pp. 331–338, 2011.

[6]	P. Alexander and C. Earland, “Structure of Wool Fibres: Isolation of an α- and β-Protein in Wool,” Nature, vol. 166, pp. 396–397, Sep. 1950.

[7]	W. G. Crewther, R. D. B. Fraser, F. G. Lennox, and H. Lindley, “The chemistry of keratins,” Adv. Protein Chem., vol. 20, pp. 191–346, 1965.

[8]	E. O. P. Thompson and I. J. O’donnell, “Studies on reduced wool V. A comparison of the two major components,” Aust. J. Biol. Sci., vol. 18, no. 6, pp. 1207–1226, 1965.

[9]	C. A. Anker and P. I. Burchill, Process of preparing fibrous protein products. Google Patents, 1972.

[10]	Y. Noishiki, H. Ito, T. Miyamoto, and H. Inagaki, “Application of Denatured Wool Keratin Derivatives to an Antithrombogenic Biomaterial-Vascular Graft Coated with a Heparinized Keratin Derivative,” Kobunshi Ronbunshu, vol. 39, no. 4, pp. 221–227, 1982.

[11]	W. S. Simpson and G. H. Crawshaw, Wool: Science and Technology. CRC Press, 2002.

[12]	V. S. Pshezhetskii, A. A. Rakhnyanskaya, I. M. Gaponenko, and Y. E. Nalbandyan, “A differential scanning calorimetry study of polyvinyl alcohol,” Polym. Sci. USSR, vol. 32, no. 4, pp. 722–726, 1990.

[13]	“The structure of a Merino Wool - CSIRO Science Image - CSIRO Science Image.” [Online]. Available: http://www.scienceimage.csiro.au/library/textile/i/7663/the-structure-of-a-merino-wool-fibre/. [Accessed: 01-Sep-2017].

[14]	M. Zoccola, A. Aluigi, A. Patrucco, C. Tonin, R. Dullaart, and J. Mousquès, “Extraction, processing and applications of wool keratin,” Keratin Struct. Prop. Appl., 2012.

[15]	A. Patrucco et al., “Wool fibril sponges with perspective biomedical applications,” Mater. Sci. Eng. C, vol. 61, pp. 42–50, 2016.

[16]	A. Tachibana, Y. Furuta, H. Takeshima, T. Tanabe, and K. Yamauchi, “Fabrication of wool keratin sponge scaffolds for long-term cell cultivation,” J. Biotechnol., vol. 93, no. 2, pp. 165–170, 2002.

[17]	L. Alibardi, “Immunolocalization of alpha-keratins and feather beta-proteins in feather cells and comparison with the general process of cornification in the skin of mammals,” Ann. Anat.-Anat. Anz., vol. 195, no. 2, pp. 189–198, 2013.

[18]	H. Rajabinejad, I.-I. Bucişcanu, and S.-S. Maier, “PRACTICAL WAYS OF EXTRACTING KERATIN FROM KERATINOUS WASTES AND BY-PRODUCTS: A REVIEW.,” Environ. Eng. Manag. J. EEMJ, vol. 15, no. 5, 2016.

[19]	P. M. Royce and B. Steinmann, Connective tissue and its heritable disorders: molecular, genetic, and medical aspects. John Wiley & Sons, 2003.

[20]	C. Popescu and H. Höcker, “Hair--the most sophisticated biological composite material,” Chem. Soc. Rev., vol. 36, no. 8, pp. 1282–1291, Aug. 2007.

[21]	C. H. Brown, “Keratins in invertebrates,” Nature, vol. 166, no. 4219, pp. 439–439, 1950.

[22]	H. H. Bragulla and D. G. Homberger, “Structure and functions of keratin proteins in simple, stratified, keratinized and cornified epithelia,” J. Anat., vol. 214, no. 4, pp. 516–559, 2009.

[23]	R. Kelly, “14 - Application of wool keratins ranging from industrial materials to medical devices,” in Advances in Wool Technology, Woodhead Publishing, 2009, pp. 323–331.

[24]	X. Xiao and J. Hu, “Animal hairs as water-stimulated shape memory materials: mechanism and structural networks in molecular assemblies,” Sci. Rep., vol. 6, p. 26393, 2016.

[25]	L. Kreplak, J. Doucet, P. Dumas, and F. Briki, “New aspects of the α-helix to β-sheet transition in stretched hard α-keratin fibers,” Biophys. J., vol. 87, no. 1, pp. 640–647, 2004.

[26]	B. S. Harrap and E. F. Woods, “Soluble derivatives of feather keratin. 2. Molecular weight and conformation,” Biochem. J., vol. 92, no. 1, p. 19, 1964.

[27]	R. B. Fraser and D. A. Parry, “Molecular packing in the feather keratin filament,” J. Struct. Biol., vol. 162, no. 1, pp. 1–13, 2008.

[28]	P. V. Peplow, S. N. G. P. J. Dias, A. D. Roddick-Lanzilotta, and R. J. Kelly, “Orthopaedic materials derived from keratin,” US7297342 B2, 20-Nov-2007.

[29]	M. Feughelman, Mechanical properties and structure of alpha-keratin fibres: wool, human hair and related fibres. UNSW press, 1997.

[30]	D. Istrate, C. Popescu, M. E. Rafik, and M. Möller, “The effect of pH on the thermal stability of fibrous hard alpha-keratins,” Polym. Degrad. Stab., vol. 98, no. 2, pp. 542–549, 2013.

[31]	P. Bhavsar et al., “Superheated Water Hydrolysis of Waste Wool in a Semi-Industrial Reactor to Obtain Nitrogen Fertilizers,” ACS Sustain. Chem. Eng., vol. 4, no. 12, pp. 6722–6731, 2016.

[32]	M. Zoccola, A. Montarsolo, R. Mossotti, A. Patrucco, and C. Tonin, “Green hydrolysis as an emerging technology to turn wool waste into organic nitrogen fertilizer,” Waste Biomass Valorization, vol. 6, no. 5, pp. 891–897, 2015.

[33]	A. Nakamura, M. Arimoto, K. Takeuchi, and T. Fujii, “A rapid extraction procedure of human hair proteins and identification of phosphorylated species,” Biol. Pharm. Bull., vol. 25, no. 5, pp. 569–572, 2002.

[34]	I. J. O’donnell and E. O. P. Thompson, “Studies on reduced wool,” Aust. J. Biol. Sci., vol. 17, no. 4, pp. 973–978, 1964.

[35]	J. L. Bailey and R. D. Cole, “Studies on the reaction of sulfite with proteins,” J. Biol. Chem., vol. 234, no. 7, pp. 1733–1739, 1959.

[36]	A. Vasconcelos, G. Freddi, and A. Cavaco-Paulo, “Biodegradable materials based on silk fibroin and keratin,” Biomacromolecules, vol. 9, no. 4, pp. 1299–1305, 2008.

[37]	R. C. de Guzman, M. R. Merrill, J. R. Richter, R. I. Hamzi, O. K. Greengauz-Roberts, and M. E. Van Dyke, “Mechanical and biological properties of keratose biomaterials,” Biomaterials, vol. 32, no. 32, pp. 8205–8217, 2011.

[38]	A. Idris, R. Vijayaraghavan, U. A. Rana, D. Fredericks, A. F. Patti, and D. R. MacFarlane, “Dissolution of feather keratin in ionic liquids,” Green Chem., vol. 15, no. 2, pp. 525–534, 2013.

[39]	A. Ghosh and S. R. Collie, “Keratinous materials as novel absorbent systems for toxic pollutants,” Def. Sci. J., vol. 64, no. 3, p. 209, 2014.

[40]	R. Li and D. Wang, “Preparation of regenerated wool keratin films from wool keratin–ionic liquid solutions,” J. Appl. Polym. Sci., vol. 127, no. 4, pp. 2648–2653, 2013.

[41]	K. E. Moore, D. N. Mangos, A. D. Slattery, C. L. Raston, and R. A. Boulos, “Wool deconstruction using a benign eutectic melt,” RSC Adv., vol. 6, no. 24, pp. 20095–20101, 2016.

[42]	A. Vasconcelos and A. Cavaco-Paulo, “Wound dressings for a proteolytic-rich environment,” Appl. Microbiol. Biotechnol., vol. 90, no. 2, pp. 445–460, 2011.

[43]	T. Amiya, A. Kawaguchi, T. Miyamoto, and H. Inagaki, “Ordered structure of high-glycine proteins from reduced Merino wool,” Seni Gakkaishi, vol. 36, no. 11, pp. T479–T483, 1980.

[44]	R. Cecil, “Intramolecular bonds in proteins. I. The role of sulfur in proteins,” Proteins Compos. Struct. Funct., vol. 1, p. 379e476, 1963.

[45]	J. A. Maclaren and B. Milligan, “Wool science. The chemical reactivity of the wool fibre,” 1981.

[46]	J. M. Cardamone, “Investigating the microstructure of keratin extracted from wool: Peptide sequence (MALDI-TOF/TOF) and protein conformation (FTIR),” J. Mol. Struct., vol. 969, no. 1, pp. 97–105, 2010.

[47]	J. Yin, S. Rastogi, A. E. Terry, and C. Popescu, “Self-organization of oligopeptides obtained on dissolution of feather keratins in superheated water,” Biomacromolecules, vol. 8, no. 3, pp. 800–806, 2007.

[48]	M. Zoccola et al., “Microwave-assisted chemical-free hydrolysis of wool keratin,” Text. Res. J., vol. 82, no. 19, pp. 2006–2018, 2012.

[49]	N. L. Eremeev et al., “Enzymatic hydrolysis of keratin-containing stock for obtaining protein hydrolysates,” Appl. Biochem. Microbiol., vol. 45, no. 6, p. 648, 2009.

[50]	I. Kilpeläinen, H. Xie, A. King, M. Granstrom, S. Heikkinen, and D. S. Argyropoulos, “Dissolution of wood in ionic liquids,” J. Agric. Food Chem., vol. 55, no. 22, pp. 9142–9148, 2007.

[51]	Z. Meng, X. Zheng, K. Tang, J. Liu, Z. Ma, and Q. Zhao, “Dissolution and regeneration of collagen fibers using ionic liquid,” Int. J. Biol. Macromol., vol. 51, no. 4, pp. 440–448, Nov. 2012.

[52]	X. Liu, C. Zhang, W. Xu, H. Liu, and C. Ouyang, “Blend films of silk fibroin and water-insoluble polyurethane prepared from an ionic liquid,” Mater. Lett., vol. 65, no. 15, pp. 2489–2491, 2011.

[53]	S. H. Lee, M. Miyauchi, J. S. Dordick, and R. J. Linhardt, “Preparation of biopolymer-based materials using ionic liquids for the biomedical application,” in Ionic Liquid Applications: Pharmaceuticals, Therapeutics, and Biotechnology, ACS Publications, 2010, pp. 115–134.

[54]	H. Xie, S. Li, and S. Zhang, “Ionic liquids as novel solvents for the dissolution and blending of wool keratin fibers,” Green Chem., vol. 7, no. 8, pp. 606–608, 2005.

[55]	A. Idris, R. Vijayaraghavan, U. A. Rana, A. F. Patti, and D. R. MacFarlane, “Dissolution and regeneration of wool keratin in ionic liquids,” Green Chem., vol. 16, no. 5, pp. 2857–2864, 2014.

[56]	J. Chen, K. Vongsanga, X. Wang, and N. Byrne, “What happens during natural protein fibre dissolution in ionic liquids,” Materials, vol. 7, no. 9, pp. 6158–6168, 2014.

[57]	A. Ghosh, S. Clerens, S. Deb-Choudhury, and J. M. Dyer, “Thermal effects of ionic liquid dissolution on the structures and properties of regenerated wool keratin,” Polym. Degrad. Stab., vol. 108, pp. 108–115, 2014.

[58]	X. Fan, Value-added products from chicken feather fiber and protein. Auburn University, 2008.

[59]	Y.-X. Wang and X.-J. Cao, “Extracting keratin from chicken feathers by using a hydrophobic ionic liquid,” Process Biochem., vol. 47, no. 5, pp. 896–899, 2012.

[60]	A. Idris, R. Vijayaraghavan, A. F. Patti, and D. R. MacFarlane, “Distillable protic ionic liquids for keratin dissolution and recovery,” ACS Sustain. Chem. Eng., vol. 2, no. 7, pp. 1888–1894, 2014.

[61]	H. A. Benson, “Transdermal drug delivery: penetration enhancement techniques,” Curr. Drug Deliv., vol. 2, no. 1, pp. 23–33, 2005.

[62]	R. P. Oertel, “Protein conformational changes induced in human stratum corneum by organic sulfoxides: an infrared spectroscopic investigation,” Biopolymers, vol. 16, no. 10, pp. 2329–2345, 1977.

[63]	V. H. Price and E. Menefee, “On the effect of dimethyl sulfoxide on hair keratin,” J. Invest. Dermatol., vol. 49, no. 3, pp. 297–301, 1967.

[64]	J. P. Tam, Oxidative folding of peptide and protein substrates using hydrocarbon sulfoxides. Google Patents, 1992.

[65]	M. R. J, “Process for preparing keratin protein,” US2993794 A, 25-Jul-1961.

[66]	R. Gupta and P. Ramnani, “Microbial keratinases and their prospective applications: an overview,” Appl. Microbiol. Biotechnol., vol. 70, no. 1, p. 21, 2006.

[67]	T. Korni\l\lowicz-Kowalska and J. Bohacz, “Biodegradation of keratin waste: theory and practical aspects,” Waste Manag., vol. 31, no. 8, pp. 1689–1701, 2011.

[68]	T. Korni\l\lowicz-Kowalska, “Studies on the decomposition of keratin wastes by saprotrophic microfungi. I. Criteria for evaluating keratinolytic activity,” Acta Mycol., vol. 32, no. 1, pp. 51–79, 1997.

[69]	I. A. Cavello, R. A. Hours, N. L. Rojas, and S. F. Cavalitto, “Purification and characterization of a keratinolytic serine protease from Purpureocillium lilacinum LPS# 876,” Process Biochem., vol. 48, no. 5, pp. 972–978, 2013.

[70]	D. K. Sahoo, A. Das, H. Thatoi, K. C. Mondal, and P. K. D. Mohapatra, “Keratinase production and biodegradation of whole chicken feather keratin by a newly isolated bacterium under submerged fermentation,” Appl. Biochem. Biotechnol., vol. 167, no. 5, pp. 1040–1051, 2012.

[71]	D. G. Syed, J. C. Lee, W.-J. Li, C.-J. Kim, and D. Agasar, “Production, characterization and application of keratinase from Streptomyces gulbargensis,” Bioresour. Technol., vol. 100, no. 5, pp. 1868–1871, 2009.

[72]	I. Takiuchi, D. Higuchi, Y. Sei, and M. Koga, “Immunological studies of an extracellular keratinase,” J. Dermatol., vol. 10, no. 4, pp. 327–330, 1983.

[73]	J. Kunert, “Biochemical mechanism of keratin degradation by the actinomycete Streptomyces fradiae and the fungus Microsporum gypseum: a comparison,” J. Basic Microbiol., vol. 29, no. 9, pp. 597–604, 1989.

[74]	Z. Ignatova, A. Gousterova, G. Spassov, and P. Nedkov, “Isolation and partial characterisation of extracellular keratinase from a wool degrading thermophilic actinomycete strain Thermoactinomyces candidus,” Can. J. Microbiol., vol. 45, no. 3, pp. 217–222, 1999.

[75]	P. Ramnani, R. Singh, and R. Gupta, “Keratinolytic potential of Bacillus licheniformis RG1: structural and biochemical mechanism of feather degradation,” Can. J. Microbiol., vol. 51, no. 3, pp. 191–196, 2005.

[76]	N. Eslahi, F. Dadashian, and N. H. Nejad, “An investigation on keratin extraction from wool and feather waste by enzymatic hydrolysis,” Prep. Biochem. Biotechnol., vol. 43, no. 7, pp. 624–648, 2013.

[77]	P. Ramnani and R. Gupta, “Keratinases vis-à-vis conventional proteases and feather degradation,” World J. Microbiol. Biotechnol., vol. 23, no. 11, pp. 1537–1540, 2007.

[78]	N. Fakhfakh, N. Ktari, R. Siala, and M. Nasri, “Wool-waste valorization: production of protein hydrolysate with high antioxidative potential by fermentation with a new keratinolytic bacterium, Bacillus pumilus A1,” J. Appl. Microbiol., vol. 115, no. 2, pp. 424–433, 2013.

[79]	N. Fakhfakh, N. Ktari, A. Haddar, I. H. Mnif, I. Dahmen, and M. Nasri, “Total solubilisation of the chicken feathers by fermentation with a keratinolytic bacterium, Bacillus pumilus A1, and the production of protein hydrolysate with high antioxidative activity,” Process Biochem., vol. 46, no. 9, pp. 1731–1737, 2011.

[80]	R. Ohba, T. Deguchi, M. KISHIKAWA, F. ARSYAD, S. MORIMURA, and K. KIDA, “Physiological functions of enzymatic hydrolysates of collagen or keratin contained in livestock and fish waste,” Food Sci. Technol. Res., vol. 9, no. 1, pp. 91–93, 2003.

[81]	S. Yamashoji, H. Yoshida, and G. Kajimoto, “Effects of amino acids on the photosensitized oxidation of linoleic acid in an aqueous ethanol solution,” Agric. Biol. Chem., vol. 43, no. 7, pp. 1505–1511, 1979.

[82]	R. Fontoura, D. J. Daroit, A. P. Correa, S. M. Meira, M. Mosquera, and A. Brandelli, “Production of feather hydrolysates with antioxidant, angiotensin-I converting enzyme-and dipeptidyl peptidase-IV-inhibitory activities,” New Biotechnol., vol. 31, no. 5, pp. 506–513, 2014.

[83]	A. Gousterova et al., “Degradation of keratin and collagen containing wastes by newly isolated thermoactinomycetes or by alkaline hydrolysis,” Lett. Appl. Microbiol., vol. 40, no. 5, pp. 335–340, 2005.

[84]	S. Fellahi, T. I. Zaghloul, E. Feuk-Lagerstedt, and M. J. Taherzadeh, “A bacillus strain able to hydrolyze alpha-and beta-keratin,” J. Bioprocess. Biotech., vol. 4, no. 7, p. 1, 2014.

[85]	P. Dalev, “An enzyme-alkaline hydrolysis of feather keratin for obtaining aprotein concentrate for fodder,” Biotechnol. Lett., vol. 12, no. 1, pp. 71–72, 1990.

[86]	P. Mokrejs, O. Krejci, P. Svoboda, and V. Vasek, “Modeling technological conditions for breakdown of waste sheep wool,” Rasayan J Chem, vol. 4, no. 4, pp. 728–735, 2011.

[87]	P. Mokrejs, P. Svoboda, J. Hrncirik, D. Janacova, and V. Vasek, “Processing poultry feathers into keratin hydrolysate through alkaline-enzymatic hydrolysis,” Waste Manag. Res., vol. 29, no. 3, pp. 260–267, 2011.

[88]	M. Veselá and J. Friedrich, “Amino acid and soluble protein cocktail from waste keratin hydrolysed by a fungal keratinase of Paecilomyces marquandii,” Biotechnol. Bioprocess Eng., vol. 14, no. 1, pp. 84–90, 2009.

[89]	E. Tiwary and R. Gupta, “Rapid conversion of chicken feather to feather meal using dimeric keratinase from Bacillus licheniformis ER-15,” J Bioprocess Biotech, vol. 2, no. 123, p. 2, 2012.

[90]	K. Katoh, M. Shibayama, T. Tanabe, and K. Yamauchi, “Preparation and physicochemical properties of compression-molded keratin films,” Biomaterials, vol. 25, no. 12, pp. 2265–2272, 2004.

[91]	J. H. Bradbury, “The structure and chemistry of keratin fibers,” Adv. Protein Chem., vol. 27, pp. 111–211, 1973.

[92]	R. D. B. Fraser, T. P. MacRae, and G. E. Rogers, Keratins: their composition, structure, and biosynthesis. Charles C. Thomas, 1972.

[93]	S. Kim, P. Wong, and P. A. Coulombe, “A keratin cytoskeletal protein regulates protein synthesis and epithelial cell growth,” Nature, vol. 441, no. 7091, pp. 362–365, 2006.

[94]	S. Parcell, “Sulfur in human nutrition and applications in medicine,” Altern. Med. Rev., vol. 7, no. 1, pp. 22–44, 2002.

[95]	M. E. Van Dyke, Nerve regeneration employing keratin biomaterials. Google Patents, 2015.

[96]	J. E. Gagner, W. Kim, and E. L. Chaikof, “Designing protein-based biomaterials for medical applications,” Acta Biomater., vol. 10, no. 4, pp. 1542–1557, 2014.

[97]	H. Weigmann, Y. Kamath, and S. Ruetsch, “Characterization ofsurface deposits on human hair fibers,” J Soc Cosmet Chem, vol. 41, pp. 379–390, 1990.

[98]	Y. Wang, W. Zhang, J. Yuan, and J. Shen, “Differences in cytocompatibility between collagen, gelatin and keratin,” Mater. Sci. Eng. C, vol. 59, pp. 30–34, 2016.

[99]	S. Xu, C. Zhang, A. Zhang, H. Wang, H. Rao, and Z. Zhang, “Fabrication and biological evaluation in vivo of an injectable keratin hydrogel as filler materials,” J. Bioact. Compat. Polym., vol. 31, no. 2, pp. 179–190, 2016.

[100]	J. Zhang et al., “Isolation and characterization of biofunctional keratin particles extracted from wool wastes,” Powder Technol., vol. 246, pp. 356–362, 2013.

[101]	S. J. Lee and M. van Dyke, “Protocol for Self-Assembled Human Hair Keratins,” in A Manual For Biomaterials/Scaffold Fabrication Technology, World Scientific, 2007, pp. 141–151.

[102]	S. Hamasaki, A. Tachibana, D. Tada, K. Yamauchi, and T. Tanabe, “Fabrication of highly porous keratin sponges by freeze-drying in the presence of calcium alginate beads,” Mater. Sci. Eng. C, vol. 28, no. 8, pp. 1250–1254, 2008.

[103]	X. Yang, H. Zhang, X. Yuan, and S. Cui, “Wool keratin: A novel building block for layer-by-layer self-assembly,” J. Colloid Interface Sci., vol. 336, no. 2, pp. 756–760, 2009.

[104]	Y. Ozaki, Y. Takagi, H. Mori, and M. Hara, “Porous hydrogel of wool keratin prepared by a novel method: An extraction with guanidine/2-mercaptoethanol solution followed by a dialysis,” Mater. Sci. Eng. C, vol. 42, pp. 146–154, 2014.

[105]	R. Nakata, Y. Osumi, S. Miyagawa, A. Tachibana, and T. Tanabe, “Preparation of keratin and chemically modified keratin hydrogels and their evaluation as cell substrate with drug releasing ability,” J. Biosci. Bioeng., vol. 120, no. 1, pp. 111–116, Jul. 2015.

[106]	L. Ajay Sharma, M. A. Ali, R. M. Love, M. J. Wilson, and G. J. Dias, “Novel keratin preparation supports growth and differentiation of odontoblast-like cells,” Int. Endod. J., vol. 49, no. 5, pp. 471–482, 2016.

[107]	Y. Li, Y. Wang, J. Ye, J. Yuan, and Y. Xiao, “Fabrication of poly (ε-caprolactone)/keratin nanofibrous mats as a potential scaffold for vascular tissue engineering,” Mater. Sci. Eng. C, vol. 68, pp. 177–183, 2016.

[108]	H. Zhu, R. Li, X. Wu, K. Chen, and J. Che, “Controllable fabrication and characterization of hydrophilic PCL/wool keratin nanonets by electronetting,” Eur. Polym. J., vol. 86, pp. 154–161, 2017.

[109]	M. E. Van Dyke, C. R. Blanchard, S. F. Timmons, A. J. Siller-Jackson, and R. A. Smith, Water absorbent keratin and gel formed therefrom. Google Patents, 2001.

[110]	L. Sando, M. Kim, M. L. Colgrave, J. A. Ramshaw, J. A. Werkmeister, and C. M. Elvin, “Photochemical crosslinking of soluble wool keratins produces a mechanically stable biomaterial that supports cell adhesion and proliferation,” J. Biomed. Mater. Res. A, vol. 95, no. 3, pp. 901–911, 2010.

[111]	J. M. Cardamone, P. Erazo-Majewicz, and N. Naouli, Compositions and methods for treating a keratin based substrate. Google Patents, 2014.

[112]	F. Cilurzo, F. Selmin, A. Aluigi, and S. Bellosta, “Regenerated keratin proteins as potential biomaterial for drug delivery,” Polym. Adv. Technol., vol. 24, no. 11, pp. 1025–1028, 2013.

[113]	E. Fortunati et al., “Keratins extracted from Merino wool and Brown Alpaca fibres: Thermal, mechanical and biological properties of PLLA based biocomposites,” Mater. Sci. Eng. C, vol. 47, pp. 394–406, 2015.

[114]	A. Aluigi et al., “Methylene Blue Doped Films of Wool Keratin with Antimicrobial Photodynamic Activity,” ACS Appl. Mater. Interfaces, vol. 7, no. 31, pp. 17416–17424, 2015.

[115]	T. Posati et al., “Developing keratin sponges with tunable morphologies and controlled antioxidant properties induced by doping with polydopamine (PDA) nanoparticles,” Mater. Des., vol. 110, pp. 475–484, 2016.

[116]	C. Ferroni et al., “Wool keratin 3D scaffolds with light-triggered antimicrobial activity,” Biomacromolecules, vol. 17, no. 9, pp. 2882–2890, 2016.

[117]	J. Li et al., “Synthesis and characterization of wool keratin/hydroxyapatite nanocomposite,” J. Biomed. Mater. Res. B Appl. Biomater., vol. 100, no. 4, pp. 896–902, 2012.

[118]	C. D. Tran and T. M. Mututuvari, “Cellulose, chitosan, and keratin composite materials. Controlled drug release,” Langmuir, vol. 31, no. 4, pp. 1516–1526, 2015.

[119]	A. Salama and M. El-Sakhawy, “Regenerated cellulose/wool blend enhanced biomimetic hydroxyapatite mineralization,” Int. J. Biol. Macromol., vol. 92, pp. 920–925, 2016.

[120]	J. G. Rouse and M. E. Van Dyke, “A review of keratin-based biomaterials for biomedical applications,” Materials, vol. 3, no. 2, pp. 999–1014, 2010.

[121]	R. Atkin, P. Davies, J. Hardy, and B. Vincent, “Preparation of aqueous core/polymer shell microcapsules by internal phase separation,” Macromolecules, vol. 37, no. 21, pp. 7979–7985, 2004.

[122]	P. J. Dowding, R. Atkin, B. Vincent, and P. Bouillot, “Oil core- polymer shell microcapsules prepared by internal phase separation from emulsion droplets. I. Characterization and release rates for microcapsules with polystyrene shells,” Langmuir, vol. 20, no. 26, pp. 11374–11379, 2004.

[123]	P. B. O’Donnell and J. W. McGinity, “Preparation of microspheres by the solvent evaporation technique,” Adv. Drug Deliv. Rev., vol. 28, no. 1, pp. 25–42, 1997.

[124]	K. Shimokawa, K. Saegusa, Y. Wada, and F. Ishii, “Physicochemical properties and controlled drug release of microcapsules prepared by simple coacervation,” Colloids Surf. B Biointerfaces, vol. 104, pp. 1–4, 2013.

[125]	K. S. Suslick and M. W. Grinstaff, “Protein microencapsulation of nonaqueous liquids,” J. Am. Chem. Soc., vol. 112, no. 21, pp. 7807–7809, 1990.

[126]	C. Tomaro-Duchesneau, S. Saha, M. Malhotra, I. Kahouli, and S. Prakash, “Microencapsulation for the Therapeutic Delivery of Drugs, Live Mammalian and Bacterial Cells, and Other Biopharmaceutics: Current Status and Future Directions,” Journal of Pharmaceutics, 2013. [Online]. Available: https://www.hindawi.com/journals/jphar/2013/103527/. [Accessed: 13-Aug-2017].

[127]	S. Avivi and A. Gedanken, “Are sonochemically prepared α-amylase protein microspheres biologically active?,” Ultrason. Sonochem., vol. 14, no. 1, pp. 1–5, 2007.

[128]	S. Avivi and A. Gedanken, “The preparation of avidin microspheres using the sonochemical method and the interaction of the microspheres with biotin,” Ultrason. Sonochem., vol. 12, no. 5, pp. 405–409, 2005.

[129]	X. Cui et al., “Multi-stimuli responsive smart chitosan-based microcapsules for targeted drug delivery and triggered drug release,” Ultrason. Sonochem., vol. 38, pp. 145–153, 2017.

[130]	S. Freitas, H. P. Merkle, and B. Gander, “Microencapsulation by solvent extraction/evaporation: reviewing the state of the art of microsphere preparation process technology,” J. Controlled Release, vol. 102, no. 2, pp. 313–332, 2005.

[131]	Y. L. Lianyan Wang, “Microspheres and Microcapsules for Protein Delivery: Strategies of Drug Activity Retention,” http://www.eurekaselect.com. [Online]. Available: http://www.eurekaselect.com/115574/article. [Accessed: 13-Aug-2017].

[132]	K. S. Suslick, M. W. Grinstaff, K. J. Kolbeck, and M. Wong, “Characterization of sonochemically prepared proteinaceous microspheres,” Ultrason. Sonochem., vol. 1, no. 1, pp. S65–S68, 1994.

[133]	D. Torres, L. Boado, D. Blanco, and J. L. Vila-Jato, “Comparison between aqueous and non-aqueous solvent evaporation methods for microencapsulation of drug–resin complexes,” Int. J. Pharm., vol. 173, no. 1, pp. 171–182, 1998.

[134]	S. Yan, X. Zhang, Y. Sun, T. Wang, X. Chen, and J. Yin, “In situ preparation of magnetic Fe 3 O 4 nanoparticles inside nanoporous poly (l-glutamic acid)/chitosan microcapsules for drug delivery,” Colloids Surf. B Biointerfaces, vol. 113, pp. 302–311, 2014.

[135]	C. Goldenstedt et al., “Delivery by shock waves of active principle embedded in gelatin-based capsules,” Ultrason. Sonochem., vol. 15, no. 5, pp. 808–814, 2008.

[136]	L. M. Dowling, W. G. Crewther, and D. A. Parry, “Secondary structure of component 8c-1 of α-keratin. An analysis of the amino acid sequence,” Biochem. J., vol. 236, no. 3, pp. 705–712, 1986.

[137]	L. Tang, J. O. Sierra, R. Kelly, R. S. Kirsner, and J. Li, “Wool-derived keratin stimulates human keratinocyte migration and types IV and VII collagen expression,” Exp. Dermatol., vol. 21, no. 6, pp. 458–460, 2012.

[138]	M. E. Van Dyke, Wound healing compositions containing keratin biomaterials. Google Patents, 2012.

[139]	F. Nunez et al., “Vasoactive Properties of Keratin-Derived Compounds,” Microcirculation, vol. 18, no. 8, pp. 663–669, Nov. 2011.

[140]	L. Burnett and C. Johnson, “Angiogenesis promoted by alpha-keratose,” WO2013025940 A1, 21-Feb-2013.

[141]	C. S. Ki, E. H. Gang, I. C. Um, and Y. H. Park, “Nanofibrous membrane of wool keratose/silk fibroin blend for heavy metal ion adsorption,” J. Membr. Sci., vol. 302, no. 1, pp. 20–26, 2007.

[142]	R. Lei, X. Jie, X. Jun, and Z. Ruiyun, “Structure and properties of polyvinyl alcohol amidoxime chelate fiber,” J. Appl. Polym. Sci., vol. 53, no. 3, pp. 325–329, 1994.

[143]	O. N. Tretinnikov and S. A. Zagorskaya, “Determination of the degree of crystallinity of poly (vinyl alcohol) by FTIR spectroscopy,” J. Appl. Spectrosc., pp. 1–6, 2012.

[144]	U. M. Subramanian, S. V. Kumar, N. Nagiah, and U. T. Sivagnanam, “Fabrication of polyvinyl alcohol-polyvinylpyrrolidone blend scaffolds via electrospinning for tissue engineering applications,” Int. J. Polym. Mater. Polym. Biomater., vol. 63, no. 9, pp. 476–485, 2014.

[145]	M. Ye, P. Mohanty, and G. Ghosh, “Biomimetic apatite-coated porous PVA scaffolds promote the growth of breast cancer cells,” Mater. Sci. Eng. C, vol. 44, pp. 310–316, 2014.

[146]	Y. Dou, B. Zhang, M. He, G. Yin, Y. Cui, and I. N. Savina, “Keratin/polyvinyl alcohol blend films cross-linked by dialdehyde starch and their potential application for drug release,” Polymers, vol. 7, no. 3, pp. 580–591, 2015.

[147]	C. Tonin, A. Aluigi, C. Vineis, A. Varesano, A. Montarsolo, and F. Ferrero, “Thermal and structural characterization of poly (ethylene-oxide)/keratin blend films,” J. Therm. Anal. Calorim., vol. 89, no. 2, pp. 601–608, 2007.

[148]	P. Alexander, R. F. Hudson, and M. Fox, “The reaction of oxidizing agents with wool. 1. The division of cystine into two fractions of widely differing reactivities,” Biochem. J., vol. 46, no. 1, p. 27, 1950.

[149]	W. R. Sanderson, “Hydrogen Peroxide in Waste Minimisation—Current and Potential Contributions,” Handb. Green Chem. Technol., pp. 258–305, 2008.

[150]	S. Bi, L. Xingfang, and S. Danhong, “The mechanism of oxidative unhairing using hydrogen peroxide,” in The 5th Asian International Conference of Leather Science and Technology, KOREA, 2002.

[151]	W. E. Savige, J. Eager, J. A. Maclaren, and C. M. Roxburgh, “The S-monoxides of cystine, cystamine and homocystine,” Tetrahedron Lett., vol. 5, no. 44, pp. 3289–3293, 1964.

[152]	M. Yamada et al., Process for solubilizing animal hair. Google Patents, 1994.

[153]	A. R. Katritzky, N. G. Akhmedov, and O. V. Denisko, “^ 1H and^ 1^ 3C NMR spectroscopic study of oxidation of D, L-cystine and 3, 3’-dithiobis (propionic acid) with hydrogen peroxide in aqueous solution,” Magn. Reson. Chem., vol. 41, no. 1, pp. 37–41, 2003.

[154]	L. J. Wolfram, K. Hall, and I. Hui, “The mechanism of hair bleaching,” J Soc Cosmet Chem, vol. 21, pp. 875–900, 1970.

[155]	P. M. Schrooyen, P. J. Dijkstra, R. C. Oberthür, A. Bantjes, and J. Feijen, “Partially carboxymethylated feather keratins. 1. Properties in aqueous systems,” J. Agric. Food Chem., vol. 48, no. 9, pp. 4326–4334, 2000.

[156]	P. M. Schrooyen, P. J. Dijkstra, R. C. Oberthür, A. Bantjes, and J. Feijen, “Partially carboxymethylated feather keratins. 2. Thermal and mechanical properties of films,” J. Agric. Food Chem., vol. 49, no. 1, pp. 221–230, 2001.

[157]	P. M. Schrooyen, P. J. Dijkstra, R. C. Oberthür, A. Bantjes, and J. Feijen, “Stabilization of solutions of feather keratins by sodium dodecyl sulfate,” J. Colloid Interface Sci., vol. 240, no. 1, pp. 30–39, 2001.

[158]	K. Yamauchi, A. Yamauchi, T. Kusunoki, A. Kohda, and Y. Konishi, “Preparation of stable aqueous solution of keratins, and physiochemical and biodegradational properties of films,” J. Biomed. Mater. Res. A, vol. 31, no. 4, pp. 439–444, 1996.

[159]	X.-C. Yin, F.-Y. Li, Y.-F. He, Y. Wang, and R.-M. Wang, “Study on effective extraction of chicken feather keratins and their films for controlling drug release,” Biomater. Sci., vol. 1, no. 5, pp. 528–536, 2013.

[160]	T. Fujii, S. Takayama, and Y. Ito, “A novel purification procedure for keratin-associated proteins and keratin from human hair,” J. Biol. Macromol., vol. 13, pp. 92–106, 2013.

[161]	H. Xu, Z. Shi, N. Reddy, and Y. Yang, “Intrinsically water-stable keratin nanoparticles and their in vivo biodistribution for targeted delivery,” J. Agric. Food Chem., vol. 62, no. 37, pp. 9145–9150, 2014.

[162]	A. J. Poole, R. E. Lyons, and J. S. Church, “Dissolving feather keratin using sodium sulfide for bio-polymer applications,” J. Polym. Environ., vol. 19, no. 4, pp. 995–1004, 2011.

[163]	K. Wrześniewska-Tosik and J. Adamiec, “Biocomposites with a content of keratin from chicken feathers,” Fibres Text. East. Eur., vol. 15, no. 1, p. 60, 2007.

[164]	P. M. M. Schrooyen and R. Oberthur, Keratin-based products and methods for their productions. Google Patents, 2007.

[165]	P. Hill, H. Brantley, and M. Van Dyke, “Some properties of keratin biomaterials: kerateines,” Biomaterials, vol. 31, no. 4, pp. 585–593, 2010.

[166]	S. Reichl, “Films based on human hair keratin as substrates for cell culture and tissue engineering,” Biomaterials, vol. 30, no. 36, pp. 6854–6866, 2009.

[167]	B. Srinivasan, R. Kumar, K. Shanmugam, U. T. Sivagnam, N. P. Reddy, and P. K. Sehgal, “Porous keratin scaffold–promising biomaterial for tissue engineering and drug delivery,” J. Biomed. Mater. Res. B Appl. Biomater., vol. 92, no. 1, pp. 5–12, 2010.

[168]	S. Xu, L. Sang, Y. Zhang, X. Wang, and X. Li, “Biological evaluation of human hair keratin scaffolds for skin wound repair and regeneration,” Mater. Sci. Eng. C, vol. 33, no. 2, pp. 648–655, 2013.

[169]	T. Tanabe, N. Okitsu, A. Tachibana, and K. Yamauchi, “Preparation and characterization of keratin–chitosan composite film,” Biomaterials, vol. 23, no. 3, pp. 817–825, 2002.

[170]	F. Selmin, F. Cilurzo, A. Aluigi, S. Franzè, and P. Minghetti, “Regenerated keratin membrane to match the in vitro drug diffusion through human epidermis,” Results Pharma Sci., vol. 2, pp. 72–78, 2012.

[171]	L.-T. Zhou, G. Yang, X.-X. Yang, Z.-J. Cao, and M.-H. Zhou, “Preparation of regenerated keratin sponge from waste feathers by a simple method and its potential use for oil adsorption,” Environ. Sci. Pollut. Res., vol. 21, no. 8, pp. 5730–5736, 2014.

[172]	R. J. Kelly, C. Marsh, M. A. Ali, and G. F. Sigurjonsson, Porous keratin construct and method of making the same. Google Patents, 2012.

[173]	Y. Nomura, H. Nakato, Y. Ishii, and K. SHIRAI, “Characterization of S-sulfokeratein from pig hair and its use as a modifier of type I collagen gel,” Biosci. Biotechnol. Biochem., vol. 66, no. 6, pp. 1382–1385, 2002.

[174]	S. Kalbag and C. Karunatilake, Use of sulfitolysis in high performance peptide mapping. Google Patents, 2003.

[175]	C. Tonin et al., “Study on the conversion of wool keratin by steam explosion,” Biomacromolecules, vol. 7, no. 12, pp. 3499–3504, 2006.

[176]	M. Ianelli, “3 Microwave Heating as a Tool for Sustainable Polymer Chemistry,” Microw. Heat. Tool Sustain. Chem., p. 53, 2010.

[177]	V. K. Pasupuleti and S. Braun, “State of the art manufacturing of protein hydrolysates,” in Protein hydrolysates in biotechnology, Springer, 2008, pp. 11–32.

[178]	J. Li et al., “Toxicity study of isolated polypeptide from wool hydrolysate,” Food Chem. Toxicol., vol. 57, pp. 338–345, 2013.

[179]	W. K. Kim and P. H. Patterson, “Nutritional value of enzyme-or sodium hydroxide-treated feathers from dead hens,” Poult. Sci., vol. 79, no. 4, pp. 528–534, 2000.

[180]	N. Arivithamani, S. A. Mary, M. S. Kumar, and V. R. G. Dev, “Keratin hydrolysate as an exhausting agent in textile reactive dyeing process,” Clean Technol. Environ. Policy, vol. 16, no. 6, pp. 1207–1215, 2014.

[181]	A. Converti et al., “A NEW KINETIC AND THERMODYNAMIC APPROACH TO PHENOL BIOSORPTION BY CHITOSAN AND KERATIN.,” Environ. Eng. Manag. J. EEMJ, vol. 14, no. 5, 2015.

[182]	E. S. Cooperman and  t V. Johnsen, “Penetration of protein hydrolysates into human hair strands,” Cosmet Perfum., vol. 88, no. 7, pp. 19–22, 1973.

[183]	N. Reddy, L. Chen, Y. Zhang, and Y. Yang, “Reducing environmental pollution of the textile industry using keratin as alternative sizing agent to poly (vinyl alcohol),” J. Clean. Prod., vol. 65, pp. 561–567, 2014.

[184]	X. Wang and C. M. Parsons, “Effect of processing systems on protein quality of feather meals and hog hair meals,” Poult. Sci., vol. 76, no. 3, pp. 491–496, 1997.

[185]	P. Sierpinski et al., “The use of keratin biomaterials derived from human hair for the promotion of rapid regeneration of peripheral nerves,” Biomaterials, vol. 29, no. 1, pp. 118–128, 2008.

[186]	A. Yamauchi and K. Yamauchi, “Formation and properties of wool keratin films and coatings,” Protein-Based Films Coat., pp. 253–74, 2002.

[187]	E. O. P. Thompson and I. J. O’donnell, “Studies on oxidised wool. I. A comparison of the completeness of oxidation with peracetic and performic acid,” Aust. J. Biol. Sci., vol. 12, no. 3, pp. 282–293, 1959.

[188]	J. M. Gillespie and F. G. Lennox, “Keratin derivatives extracted from wool with alkaline thioglycollate solutions,” Aust. J. Biol. Sci., vol. 8, no. 1, pp. 97–113, 1955.

[189]	C. Earland and C. S. Knight, “Studies on the structure of keratin II. The amino acid content of fractions isolated from oxidized wool,” Biochim. Biophys. Acta, vol. 22, no. 3, pp. 405–411, 1956.

[190]	M. C. Corfield, A. Robson, and B. Skinner, “The amino acid compositions of three fractions from oxidized wool,” Biochem. J., vol. 68, no. 2, p. 348, 1958.

[191]	W. N. Marmer and R. L. Dudley, “The oxidative degradation of keratin (wool and bovine hair),” J. Am. Leather Chem. Assoc., vol. 101, no. 11, pp. 408–416, 2006.

[192]	Y. Tsuda and Y. Nomura, “Properties of alkaline-hydrolyzed waterfowl feather keratin,” Anim. Sci. J., vol. 85, no. 2, pp. 180–185, 2014.

[193]	J. Nachtigal and C. Robbins, “Intermediate oxidation products of cystine in oxidized hair,” Text. Res. J., vol. 40, no. 5, pp. 454–457, 1970.

[194]	F. J. Douthwaite, D. M. Lewis, and U. Schumacher-Hamedat, “Reaction of cystine residues in wool with peroxy compounds,” Text. Res. J., vol. 63, no. 3, pp. 177–183, 1993.

[195]	J. M. Gillespie and P. H. Springell, “The distribution of readily reducible disulphide bonds in wool,” Biochem. J., vol. 79, no. 2, p. 280, 1961.

[196]	E. O. P. Thompson and I. J. O’donnell, “Quantitative reduction of disulphide bonds in proteins using high concentrations of mercaptoethanol,” Biochim. Biophys. Acta, vol. 53, no. 2, pp. 447–449, 1961.

[197]	J. M. Swan, “Thiols, disulphides and thiosulphates: some new reactions and possibilities in peptide and protein chemistry,” Nature, vol. 180, no. 4587, pp. 643–645, 1957.

[198]	L. J. Wolfram and D. L. Underwood, “The equilibrium between the disulfide linkage in hair keratin and sulfite or mercaptan,” Text. Res. J., vol. 36, no. 11, pp. 947–953, 1966.

[199]	P. Erra, N. Gomez, L. M. Dolcet, M. R. Julia, D. M. Lewis, and J. H. Willoughby, “FTIR analysis to study chemical changes in wool following a sulfitolysis treatment1,” Text. Res. J., vol. 67, no. 6, pp. 397–401, 1997.

[200]	“Treatment of Keratin Fibers, US Patent, No. 3644084 - Google Search.” [Online]. Available: https://www.google.com.sg/search?q=+Treatment+of+Keratin+Fibers%2C+US+Patent%2C+No.+3644084&oq=+Treatment+of+Keratin+Fibers%2C+US+Patent%2C+No.+3644084&gs_l=psy-ab.3...6566.6566.0.6799.1.1.0.0.0.0.0.0..0.0....0...1.1.64.psy-ab..1.0.0....0.IzPnCgYdoe0. [Accessed: 09-Oct-2017].

[201]	R. J. Kelly et al., Composite materials containing keratin. Google Patents, 2010.

[202]	W. L. January, Modification of keratin to the s-sulfo form. Google Patents, 1971.

[203]	J. M. Swan, “The reaction of protein thiol and disulphide groups with cupric sulphite solutions,” Aust. J. Chem., vol. 14, no. 1, pp. 69–83, 1961.

[204]	F. Castino and G. Bussolati, “Thiosulphation for the histochemical demonstration of protein-bound sulphydryl and disulphide groups,” Histochemistry, vol. 39, no. 1, pp. 93–96, 1974.

[205]	Y. Nagai and T. Nishikawa, “Solubilization of Feather Keratin by a Copper-amine Complex: The Action of Cupri-ethylenediamine on Feather Keratin,” Agric. Biol. Chem., vol. 34, no. 11, pp. 1676–1682, 1970.

[206]	R. J. Kelly et al., Production of soluble keratin derivaties. Google Patents, 2006.

[207]	A. M. Fleischner, Keratin hydrolysate formulations and methods of preparation thereof. Google Patents, 1989.

[208]	T. M. Florence, “Degradation of protein disulphide bonds in dilute alkali,” Biochem. J., vol. 189, no. 3, pp. 507–520, 1980.

[209]	L. N. Jones, D. E. Rivett, and D. J. Tucker, “Wool and related mammalian fibers,” in Handbook of Fiber Chemistry, Third Edition, CRC Press, 2006.

[210]	E. Wojciechowska, A. W\lochowicz, and A. Wese\lucha-Birczyńska, “Application of Fourier-transform infrared and Raman spectroscopy to study degradation of the wool fiber keratin,” J. Mol. Struct., vol. 511, pp. 307–318, 1999.

[211]	L. Coderch, A. Pinazo, and P. Erra, “Degradative Wool Shrinkproofing Processes: Part I: Protein Modification,” Text. Res. J., vol. 62, no. 5, pp. 302–306, 1992.

[212]	M. Zoccola, N. Lu, R. Mossotti, R. Innocenti, and A. Montarsolo, “Identification of wool, cashmere, yak, and angora rabbit fibers and quantitative determination of wool and cashmere in blend: a near infrared spectroscopy study,” Fibers Polym., vol. 14, no. 8, pp. 1283–1289, 2013.

[213]	J. Workman Jr and L. Weyer, Practical guide to interpretive near-infrared spectroscopy. CRC press, 2007.

[214]	C. Vineis, A. Aluigi, and C. Tonin, “Outstanding traits and thermal behaviour for the identification of speciality animal fibres,” Text. Res. J., vol. 81, no. 3, pp. 264–272, 2011.

[215]	T. Freytag, A. Dashevsky, L. Tillman, G. E. Hardee, and R. Bodmeier, “Improvement of the encapsulation efficiency of oligonucleotide-containing biodegradable microspheres,” J. Controlled Release, vol. 69, no. 1, pp. 197–207, 2000.

[216]	S. Manju and K. Sreenivasan, “Hollow microcapsules built by layer by layer assembly for the encapsulation and sustained release of curcumin,” Colloids Surf. B Biointerfaces, vol. 82, no. 2, pp. 588–593, 2011.

[217]	S. Wieland-Berghausen, U. Schote, M. Frey, and F. Schmidt, “Comparison of microencapsulation techniques for the water-soluble drugs nitenpyram and clomipramine HCl,” J. Controlled Release, vol. 85, no. 1, pp. 35–43, 2002.

[218]	Y. Yeo and K. Park, “A new microencapsulation method using an ultrasonic atomizer based on interfacial solvent exchange,” J. Controlled Release, vol. 100, no. 3, pp. 379–388, 2004.

[219]	C. Earland and C. S. Knight, “Studies on the structure of keratin: I. The analysis of fractions isolated from wool oxidized with peracetic acid,” Biochim. Biophys. Acta, vol. 17, pp. 457–461, 1955.

[220]	Q. Li et al., “Biological stimuli responsive drug carriers based on keratin for triggerable drug delivery,” J. Mater. Chem., vol. 22, no. 37, pp. 19964–19973, 2012.

[221]	M. Zhou, T. S. H. Leong, S. Melino, F. Cavalieri, S. Kentish, and M. Ashokkumar, “Sonochemical synthesis of liquid-encapsulated lysozyme microspheres,” Ultrason. Sonochem., vol. 17, no. 2, pp. 333–337, 2010.

[222]	C. Dai, B. Wang, and H. Zhao, “Microencapsulation peptide and protein drugs delivery system,” Colloids Surf. B Biointerfaces, vol. 41, no. 2, pp. 117–120, 2005.

[223]	R. C. de Guzman et al., “Bone regeneration with BMP-2 delivered from keratose scaffolds,” Biomaterials, vol. 34, no. 6, pp. 1644–1656, 2013.

[224]	A. Nesterenko, I. Alric, F. Silvestre, and V. Durrieu, “Vegetable proteins in microencapsulation: A review of recent interventions and their effectiveness,” Ind. Crops Prod., vol. 42, pp. 469–479, 2013.

[225]	A. Nesterenko, I. Alric, F. Silvestre, and V. Durrieu, “Influence of soy protein’s structural modifications on their microencapsulation properties: α-Tocopherol microparticle preparation,” Food Res. Int., vol. 48, no. 2, pp. 387–396, 2012.

[226]	L.-Y. Wang, Y.-H. Gu, Z.-G. Su, and G.-H. Ma, “Preparation and improvement of release behavior of chitosan microspheres containing insulin,” Int. J. Pharm., vol. 311, no. 1, pp. 187–195, 2006.

[227]	C. R. Blanchard, S. F. Timmons, and R. A. Smith, Keratin-based hydrogel for biomedical applications and method of production. Google Patents, 1999.

[228]	K. Yamauchi and A. Khoda, “Novel proteinous microcapsules from wool keratins,” Colloids Surf. B Biointerfaces, vol. 9, no. 1–2, pp. 117–119, 1997.

[229]	L. Burnett and S. A. Boyd, Methods for extracting keratin proteins. Google Patents, 2012.

[230]	D. S. Jones and K. J. Pearce, “Contribution of process variables to the entrapment efficiency of propranolol hydrochloride within ethylcellulose microspheres prepared by the solvent evaporation method as evaluated using a factorial design,” Int. J. Pharm., vol. 131, no. 1, pp. 25–31, 1996.

[231]	D. S. Jones and K. J. Pearce, “An investigation of the effects of some process variables on the microencapsulation of propranolol hydrochloride by the solvent evaporation method,” Int. J. Pharm., vol. 118, no. 2, pp. 199–205, 1995.

[232]	D. Perumal, “Microencapsulation of ibuprofen and Eudragit® RS 100 by the emulsion solvent diffusion technique,” Int. J. Pharm., vol. 218, no. 1, pp. 1–11, 2001.

[233]	Y. Nakano et al., “Structure and mechanical properties of chitosan/poly (vinyl alcohol) blend films,” in Macromolecular symposia, 2007, vol. 258, pp. 63–81.

[234]	M. X. Gou and X. H. Yang, “Preparation and characterization of wool keratin/PVA blended films,” in Advanced Materials Research, 2011, vol. 175, pp. 132–136.

[235]	G. G. D. Silva, P. J. A. Sobral, R. A. Carvalho, P. V. A. Bergo, O. Mendieta-Taboada, and A. Habitante, “Biodegradable films based on blends of gelatin and poly (vinyl alcohol): effect of PVA type or concentration on some physical properties of films,” J. Polym. Environ., vol. 16, no. 4, pp. 276–285, 2008.