Natural stone decay evaluation a comparison of two artificial ageing test

Bellopede R., Marini P.

Natural stone has always been one of the main materials used in architecture for its singular beauty and durability. However over time, even such a durable material, ornametal and structural stone elements decay due essentially to climate factors such as atmospheric pollution, salt solution, freezing–thaw action, thermal shock or acid rains.

The resistance to decay of natural stone doesn’t concern only a worsening of its aesthetical properties, but mostly a decreasing in their mechanical strength. To detect and to analyse the dominant destructive factors for stone durability is important to forecast the further progress of the deterioration in the long term. For this reason the comparison of the results of artificially ageing tests executed in laboratory with the long term natural weathering is useful in the study of structural analysis of natural stone historical building elements.

Six different kind of stone and in particular marble, sandstone, limestone, gneiss, granite and tephra, have been tested by means of two different artificial ageing tests: determination of resistance to ageing by means of thermal shock and freeze and thaw cycles.

In order to assess the variation of mechanical resistance, flexural strength tests and under concentrate load and ultrasonic test have been performed before and after the artificial ageing cycles. The tested stone gave different variations in mechanical strength for the two different artificial ageing test. These different behaviour have been explained by means the analysis of petrographic characteristic of the stone tested.

Finally a comparison of the natural weathering of gneiss and marble in the climate of the northern Europe have been made.

Topic:11. In-situ and laboratory experimental results

Keywords: ………………

Come si potrebbe sviluppare

Obiettivo fare una classifica della durabilità di marmi, arenarie, gneiss,granito rispetto al freeze thaw a allo shock termico e valutare la corrispondenza di tali test con l’invecchiamento naturale.

Scoutmoor sandstone  prove di gelività a differenti dimensioni variazione max del 15? 10*50*200mm 1%; 10*80*300mm 15%; 25*50*150mm 9,4%; 50*50*300mm 5%

NDT on natural stone

A identification test on a luserna stone

Luserna (Domenino ,Lopica, Maurino) per lopica c’è corrispondenza tra freeze-thaw e thermal shock nessuna variazione

Travertino – mondial marmi minima variazione con th shock  e con freeze thaw

Granitoi montorfano con th sh nessuna variazione

Tefrite 2014-12 si gelività no shock termico

Calcare Jordan Marble 2007-14 -2% per shock termico e -10% flexuralstrength ma alla fine del flexural strength distacchi su provini

Calcarenite 2005-7 solo thermal shock: nessuna variazione

Cloritoscisto 2001 sol thermal shock: nessuna variazione

Aranaria di Vicoforte piccole variazioni con  thermal shock piccole con .freze-thaw?

Moloson freeze-thaw si fratture

Marmo gioia e buca/cervaiole

In sito si può parlare della situazione dei marmi e della luserna e magari dei nuovi calcari importati…..

References:

Inese Sidraba, New Materials for Conservation of Stone Monuments in Latvia ???? (Red granite Balmoral Red and grey granite Nystad have dense, homogenous texture. The physical/mechanical properties of granite: total porosity >1%; water absorption about 0,15%; compressive strength – 180 MPa; The investigation pointed at the bio and chemical corrosion of the travertine, deformationof lead sealing at the joints between granite blocks due to vibrations caused by traffic, deterioration of lime mortar between travertine slabs, efflorescence from the open granite joints of external stonework. The evaluation of the factors for the cracking of the jointing material points to the following possible causes:• the thermal swelling and shrinkage of the building materials due to the fluctuations of the temperature and the non compatibility of the thermal expansion properties of granite and jointing material. The coefficient of the linear thermal expansion of the granite is 8 x 10-6 m/m0C, while the epoxy based materials have higher linear expansion of about 20 x 10-6 m/m0C;• the mechanical vibrations caused by the nearby traffic;• insufficient elasticity of the epoxy based material to adapt the changes of the granite parameters.)

J. M. S. Matias and C. A. S. Alves, 2001, Decay patterns of granite stones in Braga monuments (NW Portugal) in Historical Constructions, P.B. Lourenço, P. Roca (Eds.), Guimarães (Decay patterns of biotite-rich medium to fine-grained (frequently porphyritic) granite stones are related to weathering inherited from the quarry (expressed by yellowing), to the presence of heterogeneous elements (enclaves and phenocrysts) and to grain size variations. Fine-grained leucogranitic stones decay is mainly controlled by tectonic foliation. The characteristics of stone application, including how and where was stone used, influence decay patterns by favouring salt pollution concentration, biological colonisation and fixation of atmospheric pollutants. Erosive decay features (linked mainly to salt pollution) and stone coatings (linked to biological action and atmospheric and organic pollution) are widespread decay forms that affect granite stones on Braga buildings. Study of decay features allows identification of the main decay patterns that affect granite monuments of Braga. For biotite-rich, medium to fine-grained, frequently porphyritic, granite stones, decay is related to yellowing (with more pronounced and extensive erosive decay and also more frequent black crust formation on more yellowed stones), grain size variation (coarser grain stones show more intense erosive decay) and the presence of heterogeneous elements (differential erosion of phenocrysts and enclaves). Tectonic foliation of fine-grained leucogranitic stones conditions the distribution of fissures, flakes and biological colonisation on these stones. Erosive decay is strongly linked to salt pollution, being favoured by features that allow solutions accumulation and circulation (architectural details and mortar joints). Intensity of salt pollution resulting from local characteristics also affects erosive decay, as is shown by more intense decay inside buildings, associated with salt efflorescences and by decay of pavement slabs, associated with buried corpses. Chromatic modifications (related to biological colonisation, black crusts and patinas) are a major problem affecting stone applied at exterior elements. Biological colonisation shows a widespread occurrence on these monuments stones and constitutes the main discoloration factor, being its distribution related to substrate moisture and sun exposure. Black crusts are related to atmospheric pollution and its distribution seems related to the intensity of surrounding traffic. The studied patinas show varied characteristics and genesis related to diverse agents.

D.M. Freire-Lista, R. Fort, M.J. Varas-Muriel, 2015, Freeze-thaw fracturing in building granites, Cold Regions Science and Technology . doi: 10.1016/j.coldregions.2015.01.008---(su graniti in generale: Nonetheless, the FT test had an adverse effect on the petrophysical and mechanical properties of all the granites, in which microcracking was the main sign of the decay induced by the test. Resistance to FT was greatest in CO due to its texture and especially to its lesser initial cracking, while ZA was the least resistant to FT testing. This lesser durability was attributable to the greater initial cracking and high feldspar crystal content in ZA).

Jing Ni, You-Liang Chen, Peng Wang, Su-Ran Wang, Bin Peng, Rafig Azzam, 2017, Effect of chemical erosion and freeze–thaw cycling on the physical and mechanical characteristics of granites, Bull Eng Geol Environ, 76:169–179, DOI 10.1007/s10064-016-0891-5. (It is obvious that deterioration of the granites increases steadily with an increasing number of freeze–thaw cycles. The biggest effect of chemical processes and cyclic freeze–thaw on the physical and mechanical properties of granite was observed in HNO3 solution.)

A.C. Inigo ∗, S. Vicente-Tavera, Different degrees of stone decay on the inner and outer walls of a Cloister Building and Environment 36 (2001) 911–917 (Granite rocks. One outside the building (E) and the other two inside it, at the Southern (I–S) and Northern (I–N) ends of its East gallery. At these points, the 5uctuations in relative humidity and temperature were found to be very low, accounting for the lower degree of decay of the stone used to construct the building. This con7rms the decay observed on the outside of the building due to fracturing and granular disintegration owing to the tensions generated by sharp changes in temperature, above all in materials of di!erent mineralogical composition and hence with di!erent expansion coeT-cients [1,11,13,14] (Cloister balustrade). However, inside the Cloister, at the parts where there is no degradation owing to the crystallization of salts, no appreciable deterioration of this type is seen. It should be stressed that rainwater does not impinge on this zone directly, reducing problems of frost damage and biodeterioration. Attempts were made to reproduce this type of process in simulation chambers with controlled conditions. After 65 cold/heat (–20–80◦C) cycles under dry conditions no appreciable degree of alteration was seen in the blocks, indicating the slowness of thermoclasty. The phenomenon occurs faster if the changes in temperature are accompanied by cycles of wetting/drying, leading to frost damage.)

A.C. I~nigo a,b,*, M.A. Vicente a,b,1, V. Rives c,b 2000. Weathering and decay of granitic rocks: its relation to their pore network. Mechanics of Materials 32 (2000) 555±560 ( If low porous granites are used, artifcial ageing has only a minor, limited eect on their pore network; however, changes in pore size distribution (diameter < 10 nm) are observed in samples where a pore network already exists in the unaltered samples. Changes in porosity observed upon artifcial ageing are similar to those observed in historical buildings after natural decay.)

Momeni,  G. R. Khanlari, M. Heidari,  R. Bagheri,  E. Bazvand 2015. Assessment of physical weathering effects on granitic ancient monuments, Hamedan, Iran. Environ Earth Sci (2015) 74:5181–5190 (The deterioration effect of sodium sulfate on loss of engineering properties was evaluated more effectively than that of magnesium sulfate. Simulation of the Ganjnameh inscriptions behavior subjected to the weathering tests indicated that deterioration effect of sulfate solutionwas more effective than that of other weathering processes. Sodium sulfate has more effects than magnesium sulfate on engineering properties. Meanwhile, magnesium sulfate effect on weight loss was more significant than that of sodium sulfate. Consequently, a cracking mechanism for sodium sulfate and a corrosion mechanism for magnesium sulfate were proposed. Simulation of the Ganjnameh inscriptions behaviour under heating and cooling, freezing and thawing, magnesium sulfate weathering, and acidic rainfall indicated that the degradability effects of sulfate solutions were more pronounced than other weathering processes. After 60 cycles, nearly all of the cuneiform characters were damaged.)

Enrico Sassoni • Elisa Franzoni, 2014. Sugaring marble in the Monumental Cemetery in Bologna (Italy):characterization of naturally and artificially weathered samplesand first results of consolidation by hydroxyapatiteAppl. Phys. A (2014) 117:1893–1906 DOI 10.1007/s00339-014-8629-3 1.1 (Causes and consequences of marble sugaring The so-called sugaring of marble is a degradation phenomenon that often affects marble elements, both in historic monuments and modern buildings. The name derives from the fact that sugaring consists in marble granular disintegration, so that, with just the pressure of a finger,marble can be reduced to a sugar-like powder of isolated calcite grains . The sugaring marbles collected from the Monumental Cemetery in Bologna are affected by diffused microcracking, which is presumably to be ascribed to environmental thermal weathering originated by repeated temperature excursions. These micro-cracks, opened at grain boundaries, are responsible for grain loosening and detachment. With respect to the unweathered substrate, the sugaring surface exhibits a dramatic increase in open porosity (from 1.3 to 5.0 %) and average pore radius (from 0.059 to 8.047 lm). Consequently, the ultrasonic pulse velocity of the weathered marble sample results rather low (2.2 km/s).)

Federica Rosso 1,3,*, Anna Laura Pisello 2,*, Weihua Jin 3, Masoud Ghandehari 3, Franco Cotana 2and Marco Ferrero 1Cool Marble Building Envelopes: The Effect of Aging on Energy Performance and Aesthetics.sustanaibility, MDPI. (The assessment confirmed the results of previous work by authors [18], where Bianco Carrara was more sensitive to the aggressive solutions with low pH, compared to Statuario marble. However, degradation increased the cooling potential of non-polished Bianco Carrara Marble. Therefore, for the investigated time span, this led to slightly improved energy performance (4.3% energy demand for cooling). This improvement was equal to the effect of polishing process in increasing reflectance, which permitted the same energy reduction for non polished degraded samples and polished samples. Polished samples also demonstrated the advantage of being less sensitive to degradation: the degradation process did not significantly impact their aesthetics performance. With respect to temperatures, the increased solar reflectance capability in degraded samples resulted in decrease of indoor operation temperatures by 0.5 C, as well as the contribution of the surface polishing. This research provided preliminary conclusion that degradation of marble construction elements by means of exposure to simulated acid rains leads to modified energy performance and aesthetics, i.e., change in color perception (DE > 5), and consequent change in energy performance (4% up to 5% reduction of cooling energy due to the degradation). This was similar to the result obtained by the polishing process. The indoor operation temperatures were up to 0.5 C lower in non-polished marble after degradation and in the polished marble without degradation.)

Bonazza ⁎, C. Sabbioni, P. Messina, C. Guaraldi, P. De Nuntiis. Science of the Total Environment 407 (2009) 4506–4512Climate change impact: Mapping thermal stress on Carrara marble in Europe. (Marble and granite are demonstrated to be the stones most affected by thermoclastism (Gómez-Heras et al., 2006; Malaga-Starzec et al., 2002; Schouenburg et al., 2003; Siegesmund et al., 2007, 2008). However, field tests performed by Viles (2005) aimed at monitoring weathering on marble and granite blocks in the Central Namib Desert, found evidence of a greater resistance of granites with respect to marbles under natural conditions. The susceptibility of marbles derives from the anisotropy in the thermal response of calcite, which expands parallel to the c-axis and contracts normal to the c-axis. Consequently, the polycrystalline thermal expansion behaviour of marbles can vary from almost isotropic, for a marble with weak texture, to strongly anisotropic, for a marble with a strong texture with or without residual strain  (Siegesmund et al., 2000; Weiss et al., 2003). Mapping thermal stress: The results obtained evidence on how the Mediterranean Basin will generally continue to experience the highest level of risk, in some cases with more than 300 events per year, meaning almost one event per day. In addition, Central Europe and the south of England will be increasingly affected in the future, while a decreasing risk is predicted for northern Europe and some areas of the European landmass. The mostmarked change in thermal stress risk across the century is the general increase throughout the Mediterranean Basin and Europe— particularly Spain, France, Italy, and the Balkan Peninsula–Turkey and North Africa, with a maximum increase of 50 events per year.)

M. Realini” a, R. Negrotti”, L. Appolloniab, D. Vaudanb, Deposition of particulate matter on stone surfaces: an experimental verification of its effects on Carrara marble The Science of the Total Environment 167 (1995) 67-72 (The deposition of particulate matter causes a decay both in Milan and Aosta, despite the difference in the amount of deposition. A decay parameter has been calculated from the results of chemical and gravimetrical analyses: it is a useful parameter to evaluate the effects of the environment on the stone.)