## Slide 1
Ion-doped mesoporous bioactive glasses as antibacterial agents in tissue regeneration
Alessandra Bari1, Carlotta Pontremoli1, Sonia Fiorilli1, Joanna Shepherd2, Giorgio Iviglia3, Sheila MacNeil4, Chiara Vitale- Brovarone*1
1 Department of Applied Science and Technology, Politecnico di Torino, Corso Duca degli Abruzzi 24, 10129 Torino, Italy
2 School of Clinical Dentistry, The University of Sheffield, 19 Claremont Crescent, Sheffield S10 2TA, UK
3Nobil Bio Ricerche Srl, 14037 Portacomaro, Italy
4 Department of Engineering Materials, Kroto Research Institute, University of Sheffield, Broad Lane, Sheffield S3 7HQ, UK

## Slide 2
Alessandra Bari_10th November 2017
Outline
Mesoporous Bioactive Glasses (MBGs)
Ion-doped MBGs synthesis methods
Morphological and structural characterization of the samples
Ion release test
Antibacterial tests
Conclusion and remarks
Viable count test
Disk diffusion test

## Slide 3
Excellent specific surface area values
Large accessible volume
Uniform pores (range 2-8 nm)
High surface concentration of hydroxyl groups (-OH): surface modification and drug incorporation
Mesoporous Bioactive Glasses (MBGs)
+
Therapeutic ions
C. Wu, J. Chang J, Controlled Rel (2014) 193, 282-295.
The aim of the MOZART project is to develop mesoporous nanomatrices doped with therapeutic ions and drugs to be used as smart platform in the treatment of delayed bone healing and non-healing skin wounds.
Alessandra Bari_10th November 2017
Ion-doped MBGs

## Slide 4
Ion-doped MBGs particles
3 h
Under stirring
SiO2-CaO system doped with therapeutic ions (Cu2+, Ce3+, Ag+)
Aerosol-assisted Spray drying synthesis
Base catalyzed Sol-gel synthesis
L. Pontiroli, M. Dadkhah, G. Novajra, I. Tcacencu, S. Fiorilli, C. Vitale-Brovarone, Mater. Lett. 190 (2017) 111–114.
C. Wu, J. Chang, W. Fan, J. Mater. Chem. 22 (2012) 16801–16809.
Atomizing of the solution
Quick solvent evaporation by heating a carrier gas (nitrogen)
Calcination of the obtained powder
Silica precursor: | TEOS
Templating agent | P123
Polar solvent | Distilled water in HCl (pH 2)
Calcium precursor | CaNT
Silica precursor: | TEOS
Templating agent | CTAB
Polar solvent | Distilled water in NH4OH
Calcium precursor | CaNT
Mixing CTAB, NH4OH in distilled water
Addition of TEOS and calcium precursor
Calcination of the obtained powder
Ion | Ion precursor | Biological function
Copper[1] | Copper chloride (CuCl2) | Antibacterial Pro-Osteogenic Pro-angiogenic
Silver[2] | Silver nitrate (AgNO3) | Antibacterial
Cerium[3] | Cerium chloride (CeCl3 · 7H2O) | Antibacterial Pro-Osteogenic
[1] C. Wu, Y. Zhou, M. Xu, P. Han, L. Chen, J. Chang, Y. Xiao, Biomaterials 34 (2013) 422–433.
[2] M. Kawashita, S. Tsuneyama, F. Miyaji, T. Kokubo, H. Kozuka, K. Yamamoto, Biomaterials 21 (2000) 393-398
[3] D. S. Morais, S. Fernandes, P. S. Gomes, M. H. Fernandes, P. Sampaio, M. P. Ferraz, J. D. Santos, M. A. Lopes, N. Sooraj Hussain, Biomed. Mater. 10 (2015) 055008
Alessandra Bari_10th November 2017

## Slide 5
Aerosol-assisted Spray drying synthesis
N2 adsorption-desorption analysis @77K of MBG_Cu2%_SD | 
Specific surface area * | 226 m2 g-1
Pore size ** | 8-11 nm
Pore Volume | 0.05 cm3 g-1
2Theta [degree]
Intensity [a.u.]
Wide angle XRD analysis of MBG_Cu2%_SD
Average size: 1-5 μm
FE-SEM analysis
Homogeneous element distribution
EDS mapping analysis
*calculated through the BET model
** DFT method
MBG_Cu2%_SD
MBG_Cu2%_SD
IV type isotherm
Incorporation of ions confirmed by EDS measurements
No crystalline phases
Chart: P/P0
| 0.0052044193350479 | 0.00706341444849406 | 0.0092438192441484 | 0.0100998306274414 | 0.0308166482835464 | 0.0498486510963532 | 0.0701832584329726 | 0.0906899489935028 | 0.0997692666851056 | 0.125199708606841 | 0.149936112531216 | 0.17544196341845 | 0.200238667185573 | 0.225671271894138 | 0.251238271617228 | 0.277896880943756 | 0.30131789796118 | 0.33448189596414 | 0.366532705413171 | 0.40009521484375 | 0.433812308253918 | 0.467234486826566 | 0.501285854018143 | 0.533615851234039 | 0.567205184229857 | 0.59971111599511 | 0.633269569400174 | 0.665145087394508 | 0.698572093848124 | 0.735076871036236 | 0.777160674600384 | 0.808995067638688 | 0.844570088372821 | 0.878326940786638 | 0.901156844177687 | 0.951277666363606 | 0.989521812952658 | 0.989521812952658 | 0.939966962747366 | 0.889560514817325 | 0.838770527865286 | 0.801471436234815 | 0.7509651951856 | 0.703583836721987 | 0.645143061193874 | 0.586138944965949 | 0.548567243071966 | 0.49919648335046 | 0.446888651503068 | 0.395842132777661 | 0.29819575646648 | 0.199142162601735 | 0.099830458085084
 | 33.5639 | 35.3778 | 37.029 | 37.5713 | 45.2572 | 49.133 | 52.2225 | 54.7696 | 55.7823 | 58.3534 | 60.5883 | 62.727 | 64.6824 | 66.6293 | 68.5269 | 70.4774 | 72.2353 | 74.7628 | 77.3217 | 80.2364 | 83.3387 | 86.6218 | 90.111 | 93.4489 | 97.0094 | 100.9089 | 106.1273 | 113.8994 | 127.4973 | 145.6297 | 157.1995 | 159.698 | 160.9519 | 161.8575 | 162.3928 | 163.5776 | 165.5381 | 165.5381 | 163.358 | 162.3856 | 161.632 | 161.1149 | 160.346 | 157.7577 | 140.8446 | 126.5864 | 122.5337 | 119.073 | 90.9971 | 80.2989 | 72.1337 | 64.7755 | 55.9839
Chart: Diameter (nm)
Alessandra Bari_10th November 2017

## Slide 6
Base catalyzed Sol-gel synthesis
Chart: Ce SD 2% MTG
Average size: 100-150 nm
N2 adsorption-desorption analysis @77K of MBG_Cu2%_SG | 
Specific surface area* | 740 m2 g-1
Pore size** | 4 nm
Pore Volume | 0.5 cm3 g-1
FE-SEM analysis
*calculated through the BET model
** DFT method
Excellent specific surface area value
MBG_Cu2%_SG
MBG_Cu2%_SG
IV type isotherm
No crystalline phases
Wide angle XRD analysis of MBG_Cu2%_SG
2Theta [degree]
Intensity [a.u.]
Incorporation of ions confirmed by EDS measurements
Chart: P/P0
Chart: Diameter (nm)
Alessandra Bari_10th November 2017

## Slide 7
Chart: Ce SD 2% MTG
Medium: Tris HCl 0.1 M (pH 7.4)
Concentration: 250 μg/mL
Time points: 3 h, 24 h, 3 d, 7 d and 14 d
1.30 ppm
1.13 ppm
Sustained release of silver ions from samples containing 0.1 %mol and 2%mol
Burst release of copper ions
within 3 h of soaking in buffer
Sample | Release (%)
MBG_Cu2%_SD MBG_Cu2%_SG | 48.8% 95.4 %
MBG_Ag0.1%_SD MBG_Ag0.1%_SG | 100% 100%
Chart: Time (days)
| 0.0 | 0.125 | 1.0 | 3.0 | 7.0 | 14.0
MBG_Ag 0.1%_SG | 0 | 0.66077 | 1.0361 | 1.0637 | 1.1016 | 1.137
MBG_Ag 0.1%_SD | 0 | 0.30327 | 0.86185 | 1.1862 | 1.2874 | 1.3034
4.77 ppm
2.44 ppm
Cu2+ concentration (ppm)
MBG_Cu 2%_SD
MBG_Cu 2%_SG
MBG_Ag 0.1%_SG
MBG_Ag 0.1%_SD
Ion release test
Alessandra Bari_10th November 2017

## Slide 8
Alessandra Bari_10th November 2017
Two different experimental conditions
2 mg/mL of each samples were incubated for 24h with the bacterial suspension
Several dilutions of this medium were placed in the agar plates
After 24 h, the number of formed colonies were counted
Antibacterial test: Viable count test
Chart: Ce SD 2% MTG
Chronic wounds = wounds locked into a state of chronic inflammation and bacterial infection.
Research of Sheila MacNeil’s group is focused on tissue engineering of soft tissues and the antimicrobial scenario in chronic wounds
[1] M. Fazli et al. J Clin Microbiol 47 (2009) 4084–4089
[2] R. Köck et al. Euro Surveill 15 (2010) 19688
[3] Sheila MacNeil, NATURE 445 (2007) 874
SUSPENSION to evaluate the antibacterial effect due to the direct contact with the particles
SUPERNATANT 1 day and SUPERNATANT 3 days  to evaluate the antibacterial properties ascribable to the released ions
S. Aureus S235 (Gram +) and P.Aeruginosa SOM1 (Gram -) : most common bacteria isolated from chronic wounds. [1]
MRSA-Methicillin Resistant Staphylococcus Aureus (Gram +) : accounts for a large portion of hospital-acquired infections. [2]

## Slide 9
Alessandra Bari_10th November 2017
Antibacterial test: Viable count test
Chart: Ce SD 2% MTG
MBG_Cu2%_SG
MBG_Cu2%_SD
Direct contact with spray drying particles  survival rate ~ 0%
Released ions from sol-gel sample more effective than direct contact with particles

## Slide 10
Alessandra Bari_10th November 2017
Antibacterial test: Viable count test
Chart: Ce SD 2% MTG
MBG_Ag2%_SG
MBG_Ag2%_SD
Chart: 
| Suspension
S. Aureus 235 | 0.017143
P. Aeruginosa SOM1 | 0
MRSA | 0.0005
Chart: 
| Suspension
S. Aureus 235 | 1.1786
P. Aeruginosa SOM1 | 0.00065
MRSA | 3.0625
SUPERNATANT 1 day and SUPERNATANT 3 days
Ongoing
Direct contact with silver-doped particles  Survival rate of all bacteria strains ~ 0%

## Slide 11
Alessandra Bari_10th November 2017
Antibacterial test: Disk diffusion test
Chart: Ce SD 2% MTG
Agar plates were inoculated with Staphylococcus epidermidis RP62A (ATCC 35984) (10 mL of 10x109 CFU/mL)
500 µg/mL and 1000 µg/mL of Ag-containing samples were placed on the agar surface
After incubation (37°C for 72 h), growth inhibition zone was evaluated
MBG_Ag 2%_SG
MBG_Ag 0.1%_SG
Antibacterial effect proportional to ionic concentration and particles concentration
500 𝜇g/mL
1000 𝜇g/mL
500 𝜇g/mL
1000 𝜇g/mL

## Slide 12
Conclusion and remarks
Chart: Ce SD 2% MTG
Novel copper, cerium and silver-doped MBGs characterized by very high surface area values, tunable pore size and spheroidal shapes were produced by two different routes
The release kinetics and the final amount of released ions depended on the ion and the synthesis method
The amount of released ion was sufficient to ensure a significant reduction of Gram-positive and Gram-negative viable colonies
The non-specific mode of action of these matrices against both Gram + and Gram - bacteria strains and the ability to incorporate drugs make these samples powerful multifunctional materials for biomedical application.
Alessandra Bari_10th November 2017

## Slide 13
Thanks for your
kind attention
Ackowledgments
This activity has received funding from MOZART project H2020-NMP-PILOTS-2015
Alessandra Bari_10th November 2017
IRIS group
Chiara Vitale Brovarone
Sonia Fiorilli
Giorgia Novajra
Alessandra Bari
Carlotta Pontremoli
Giulia Molino
Giorgia Montalbano
alessandra.bari@polito.it
chiara.vitale@polito.it

## Slide 14
Alessandra Bari_10th November 2017
Ion release test
Chart: Ce SD 2% MTG
Medium: Tris HCl 0.1 M (pH 7.4)
Concentration: 250 μg/mL
Time points: 3 h, 24 h, 3 d, 7 d and 14 d
Copper
Silver
10.5 ppm
7.53 ppm
Copper
Silver
10.5 ppm
7.53 ppm
Silver
10.5 ppm
7.53 ppm

## Slide 15: Effects of ions on biofilm formation
Alessandra Bari_10th November 2017
Chart: Ce SD 2% MTG
Copper
Silver
10.5 ppm
7.53 ppm
Copper
Silver
10.5 ppm
7.53 ppm