## Slide 1
Chart: Ce SD 2% MTG
Ion-doped mesoporous bioactive glass nanoparticles for wound healing applications
Alessandra Baria, Sonia Fiorillia, Carlotta Pontremolia, Joanna Shepherdb, Anthony J. Bullockc, Sheila MacNeilc, Chiara Vitale- Brovarone*a
a Department of Applied Science and Technology, Politecnico di Torino, Corso Duca degli Abruzzi 24, 10129 Torino, Italy
b School of Clinical Dentistry, The University of Sheffield, 19 Claremont Crescent, Sheffield S10 2TA, UK
c Department of Engineering Materials, Kroto Research Institute, University of Sheffield, Broad Lane, Sheffield S3 7HQ, UK
Introduction & Aim of the work
Bioactive glasses (BGs) have been extensively studied for bone repair. Besides, recent research has also shown their positive effects on wound healing. Among BGs, mesoporous bioactive glasses (MBGs) are receiving increasing attention as tissue-regeneration systems. Their high surface area and accessible pore volume give the possibility of incorporating and releasing therapeutic ions to impart biological properties, such as pro-angiogenic effects (cerium [1], copper [2]) or antibacterial activities (copper) [3].
The aim of this work is to develop mesoporous bioactive glasses doped with cerium and copper in order to obtain a multifunctional platform for tissue regeneration.
To evaluate ions antimicrobial potential, MIC and viable count test were run with copper and cerium salts.
Salts
Ce(NO3)3 · 6H2O
Cu(NO3)2 · 2.5H2O
AgNO3
CuSO4
Nanoparticles
Base-catalyzed sol-gel method [4]
Ce US 2% MTG: 85 SiO2/ 13 CaO/ 2 CeO (%mol)
Cu US 2% MTG: 85 SiO2/ 13 CaO/ 2 CuO (%mol)
Spray-drying procedure [5]
Ce SD 2% MTG: 85 SiO2/ 13 CaO/ 2 CeO (%mol)
Cu SD 2% MTG: 85 SiO2/ 13 CaO/ 2 CuO (%mol)
Why Ce and Cu?
Cerium Copper
Pro-angiogenic - Antibacterial
Antibacterial
Antibacterial test: Salts
1) MIC test
Materials & Methods
FESEM
XRD
N2 adsorption-desorption analysis
Release test in Tris-HCl (3h, 1, 3, 8 days)
Viable count
Results
Sample | S. Aureus 235 | P. Aeruginosa SOM 1 | MRSA
Ce(NO3)3 · 6H2O | 6.250 mg/ml | 3.120 mg/ml | 6.250 mg/ml
AgNO3 | 0.078 mg/ml | 0.078 mg/ml | 0.078 mg/ml
CuSO4 | 1.560 mg/ml | 3.125 mg/ml | 3.125 mg/ml
Cu(NO3)2 · 2.5H2O | 3.125 mg/ml | 3.125 mg/ml | 3.125 mg/ml
Chart: S235 cfu/ml
ctrl | 260000000
CeNO3 | 39000000
AgNO3 | 6500
CuSO4 | 1500
CuNO3 | 8500
Chart: P. Aeruginosa SOM1 cfu/ml
ctrl | 4000000000
CeNO3 | 500000000
AgNO3 | 95000000
CuSO4 | 0
CuNo3 | 0
Chart: MRSA cfu/ml
ctrl | 120000000
CeNO3 | 45000000
AgNO3 | 0
CuSO4 | 0
CuNO3 | 0
Antibacterial studies on salts showed that silver and copper have good antimicrobial properties against Gram Positive and Gram negative strains.
These ions, incorporated in the mesoporous glass frameworks, obtained by two different synthesis routes, imparted good antibacterial properties.
Conclusion
On going
The Angiogenesis capacity of the nanomatrices will be tested on fertilised chick eggs by Chorionic Allantoic Membrane assay (CAM).
Kroto Research Institute, University of Sheffield, Sheffield
The activity leading to this work has received funding from H2020-NMP-PILOTS-2015 under grant agreement no. 685872 (MOZART).
[1] J.P. Garner, P.S. Heppell., Burns 31 (2005) 539–547
[2] A. Hoppe et al., Biomaterials 32 (2011) 2757-74
[3] C. Wu et al., Biomaterials 34 (2013) 422-433
[4] M. Shi et al., Acta Biomater. 30 (2016) 334–344
[5] C. Vitale-Brovarone et al., KeyEngMat 631 (2015) 43-47
[6] P.G. et al., Clinical Microbiology Reviews (2001)
[7] O. Zeions et al., Nanotoxicology 3 (2009) 284–295
References
Salts
Bacteria strains:
S. Aureus S235 (Gram-positive)
P. Aeruginosa SOM1 (Gram-negative)
MRSA-Methicillin Resistant Staphylococcus Aureus (Gram-positive)
Viable count
From the viable count, it is possible to notice that:
Cu salts have the same effect against Gram + and Gram -
Ag is more effective against Gram +
Ce showed not satisfying results against all strains considering the values of cfu/ml (higher than the limit of 10^5 CFU/ml regarded as “infection”) [6]
Nanoparticles
Spray dryer samples:
500-5000 nm
Sol-gel samples: 100 nm
Release test
Acknowledgements
chiara.vitale@polito.it
alessandra.bari@polito.it
MIC test
Ag salt is more effective compared to copper and cerium salt
The MIC values for Gram + and Gram - are almost the same for Ag and Cu salts
Ce salt seems to be more effective against Gram -
No oxidic form
From viable count, it is possible to notice that:
Antibacterial effect against Staphylococcus Aureus S.235 is more evident and still present after 3 days
Survival rate increases after 3 days of soaking against MRSA and SOM1, suggesting that ions probably created some compounds with other elements present in the medium which are not able to act against these bacteria strains.
Chart: S. 235
| suspension | 1 day | 3 days | 8 days
CuSD | 0.788 | 200 | 1.6 | 5
CeSD | 103 | 0.0606 | 8.5 | 0
CuUS | 8.79 | 0.0576 | 0.0225 | 0.0307
CeUS | 78.8 | 4.24 | 15.5 | 0.03
Chart: SOM 1
| suspension | 1 day | 3 days | 8 days | 15 days
CuSD | 33.3 | 200 | 20 | 75
CeSD | 43.3 | 44.4 | 7.6 | 0.313
CuUS | 23.3 | 200 | 16 | 200
CeUS | 133 | 0.0222 | 8 | 100
Chart: MRSA
| suspension | 1 day | 3 days | 8 days | 15 days
CuSD | 3.03 | 4.0556 | 10.7692 | 5
CeSD | 5.45 | 0.37222 | 11.5385 | 20.4167
CuUS | 39.4 | 0.037778 | 36.9231 | 216.6667
CeUS | 78.8 | 0.5 | 24.6154 | 100
2) Viable count test
Sample | Pore size (nm) | Surface area - BET (m2/g) | Pore volume (cc/g)
Ce US 2% MTG | 5.7 | 505 | 0.6
Cu US 2% MTG | 4 | 535 | 0.5
Ce SD 2% MTG | 8.7 | 470 | 0.6
Cu SD 2% MTG | 5.5 | 189 | 0.3
Nanoparticles