COPOLYMERS WITH HIGH PERFLUOROPOLYALKYLETHERS (PFPAES) CONTENT BY PHOTO-INDUCED CATIONIC POLYMERIZATION
Giuseppe Trusiano1, Alessandra Vitale1, Christine Joly-Duhamel2, Chadron M. Friesen3, Roberta Bongiovanni1
1 Department of Applied Science and Technology, Politecnico di Torino, 10129 Torino, Italy

2 Institut Charles Gerhardt, UMR CNRS 5253, Ingénierie et Architectures Macromoléculaires, Ecole Nationale Supérieure de Chimie de Montpellier, 34296 Montpellier Cedex 5, France

3Department of Chemistry, Trinity Western University, Langley, British Columbia V2Y 1V1, Canada
Abstract
Perfluoropolyalkylethers (PFPAEs) show low polarizability, strong electronegativity, high C-F bond energy, and exceptional chain mobility thanks to the oxygen bridges; they represent a special class of fluoropolymers with remarkable properties (low glass transition temperature, high thermal stability, excellent chemical inertness, low surface energy, tunable mechanical properties) (1–3). Commercially available PFPAEs are mostly obtained from the photooxidation of perfluoroolefins. In this work PFPAEs were synthesized by anionic polymerization of dodecafluorooctanedioyl difluoride, chain extended with different alkyl groups and functionalized with vinyl ether or epoxy end groups (Fig. 1a).

A trivinyl ether resin (trimethylolpropane trivinyl ether) and a triepoxide resin (trimethylolpropane triglycidyl ether) were added (20 wt%) to the PFPAE vinyl ethers and to the PFPAE epoxides, respectively. The mixtures were photo-cured (Fig. 1b) and the non-fluorinated resins acted as crosslinking agent, improving the mechanical properties of the photocured networks. The UV-curing process of the copolymers with high PFPAE content was monitored by Photo-DSC and FT-IR-ATR spectroscopies; the crosslinked networks were characterized by DSC, TGA, refractive index, insoluble fraction and surface measurements.
[image: image1.emf]OCFCF2OCF3OCF3F2COCFCF2OCF3FCOCF3OOOOqOOCFCF2OCF3nFCOCF3F2C6OCFCF2OCF3mFCOCF3OOOppqn6mp= 1, 2, 3q = 1, 2, 3

[image: image2.png]Mixing and pouring Thinning

/\
Reactive mixture: ‘
PFPAE monomer + §

Resin +

—

AN

Film thickness: 50 — 100 pm

Substrate or mould UV light

Photo-Initiator

]
\ 4
. H,0 L CieHas -@- exposure
CA=115° CA= 80° =

ﬂ | =150 mW/cm?
t=5min

Photocured Network

FTIR — ATR conversion=90—-98 %





Fig. 1 Scheme of UV-induced photo-copolymerization process, and example of the water and hexadecane wettability of the PFPAE copolymers.
The copolymers showed an evident biphasicity (two Tgs: Tg1 < –60 °C, Tg2 > 20 °C), low refractive index (n ≈ 1.31), good chemical and thermal resistance, and low surface energy (Fig. 1b). Such properties can be usefully exploited in highly demanding applications such as photonic devices and fuel cell membranes. 

References 

(1) Vitale A.; Bongiovanni R.; Ameduri B. Chem. Rev. 2015, 115, 8836–8866. 
(2) Friesen C. M.; Ameduri B. Prog. Polym. Sci. 2018, 81, 238–280.
(3) Trusiano G.; Rizzello M.; Vitale A.; Burgess J.; Friesen C.M.; Joly-Duhamel C.; Bongiovanni R. Prog. Org. Coatings, 2019, 132, 257–263.
b)





a)








